MATBOX: Microstructure Analysis Toolbox documentation

An introduction to microstructure analysis through an open-source MATLAB application

v0.91

March 18, 2021

Francois L. E. Usseglio-Viretta

Center for Integrated Mobility Sciences, National Renewable Energy Laboratory (NREL)

**About the authors/contacts:**

To report bugs, suggest new algorithms or simply provide feedbacks or comments, all of them being appreciated, please send an email to the main developer: [Francois.UsseglioViretta@nrel.gov](mailto:Francois.UsseglioViretta@nrel.gov) with the email object starting with the text [MATBOX].

Contributions (excluding third-party software):

* Main developer and documentation writer: Francois Usseglio-Viretta (NREL)
* GUI development of the particle generation module: Prehit Patel
* Meshing module code adapted for monolithic mesh: Jeffery Allen (NREL)
* Contrast correction documentation/examples for *adapthisteq* in the ROI, filering and segmentation module: Elizabeth Bernhardt

**About the National Renewable Energy Laboratory:**

The National Renewable Energy Laboratory is a national laboratory of the U.S. Department of Energy, Office of Energy Efficiency and Renewable Energy, operated by the Alliance for Sustainable Energy, LLC. Please visit <https://www.nrel.gov/index.html> for more information, as well as the transportation research / energy storage home page <https://www.nrel.gov/transportation/energy-storage.html> to see how NREL is contributing to the development of high-performance, cost-effective, and safe energy storage systems to power the next generation of electric-drive vehicles.

**Acknowledgments**

This software was authored by the National Renewable Energy Laboratory, operated by Alliance for Sustainable Energy, LLC, for the U.S. Department of Energy (DOE) under Contract No. DE-AC36-08GO28308. Funding for algorithm development was pro-vided by the U.S. DOE Vehicle Technologies Office’s Computer-Aided Engineering of Batteries (CAEBAT) program1 (program manager Brian Cunningham). Application of the algorithm for fast-charge analysis was provided by the eXtreme Fast Charge Cell Evaluation of Lithium-Ion Batteries (XCEL) program (program manager Samuel Gillard).

I would like to thank my NREL colleagues, Donal Finegan, Andrew Colclasure and Jeffery Allen, as well as Samuel Cooper from University College London, for interesting discussions and suggestions about microstructure analysis. I would particularly like to thank my NREL supervisor, Kandler Smith, for its support and guidance all along the development of this toolbox. Lastly, I would like to thank Matt Keyser, our group manager, for giving me the opportunity to work at NREL.

**License and third-party software included in the toolbox:**

* The present toolbox

This toolbox uses BSD license. NREL Software Record number SWR-20-76. License file is in the repository root folder.

* Third-party licenses

The toolbox uses third-party open-source software: Taufactor2, from Dr. Samuel Cooper for tortuosity factor calculations and Iso2mesh3, from Dr. Qianqian Fang for microstructure meshing, respectively used in the microstructure characterization and meshing modules. In addition, the toolbox uses third-party algorithms: xlscol4 from Kevin Crosby, DataHash5 from Jan, Noiselevel6 from Masayuki Tanaka, and Screencapture7 from Yair Altman, respectively used to help exporting data in excel files, compare microstructure states in iterative algorithms through their hash value, estimate image noise level before and after image filtering, and copy figure from MATLAB App design. Algorithm from Dr. Aashutosh N. Mistry8 is used for one of the methods employed in the microstructure generation module, for additive phase generation.

Taufactor, xlscol, DataHash, Noiselevel, Screencapture, and Mistry’s algorithm use BSD license and are included in the toolbox repository.

Iso2mesh uses GPLv2 and is not included in the toolbox repository. User will have to download Iso2mesh manually. Installation steps are detailed in §III.

Third-party licenses are available in the ‘Third-party licenses’ folder.

Please contact us if you would like to implement your algorithm in this toolbox.

**How to cite:**

If you produce results using the toolbox, or use some or parts of the algorithms contained within the toolbox, please quote them accordingly:

* **For any results produced with the toolbox, please quote**: F. L. E. Usseglio-Viretta et al., *MATBOX: An Open-source Microstructure Analysis Toolbox for microstructure generation*, segmentation, characterization, visualization, correlation, and meshing, SoftwareX, in preparation
* **If you are generating additive phase with the energy criterion method, then please also quote**: A. N. Mistry, K. Smith, and P. P. Mukherjee, *Secondary Phase Stochastics in Lithium-Ion Battery Electrodes*, ACS Appl. Mater. Interfaces 10(7) pp. 6317-6326 (2018), https://doi.org/10.1021/acsami.7b17771
* **If you are calculating tortuosity factor, then please also quote**: S.J. Cooper, A. Bertei, P.R. Shearing, J.A. Kilner, and N.P. Brandon, *TauFactor: An open-source application for calculating tortuosity factors from tomographic data*, SoftwareX, Volume 5, 2016, Pages 203-210
* **If you are generating unstructured mesh, then please also quote**: Q. Fang and D. A. Boas, *Tetrahedral Mesh Generation From Volumetric Binary and Gray-scale Images*, Proceedings of IEEE International Symposium on Biomedical Imaging 2009, 2009, Pages 1142-1145

Table of Contents

[I. Introduction 11](#_Toc66988001)

[II. The open-source microstructure community 16](#_Toc66988002)

[1. Open-source data 16](#_Toc66988003)

[2. Other open-source microstructure software 16](#_Toc66988004)

[III. Installation and requirements 17](#_Toc66988005)

[IV. How to use the toolbox 18](#_Toc66988006)

[V. Microstructure generation 19](#_Toc66988007)

[1. Why microstructure generation and module purpose 19](#_Toc66988008)

[a. Particle scale 19](#_Toc66988009)

[b. Additive scale 20](#_Toc66988010)

[2. Particle generation 20](#_Toc66988011)

[a. Algorithm explained 20](#_Toc66988012)

[b. How to use 25](#_Toc66988013)

[c. Examples of generated microstructures 29](#_Toc66988014)

[3. Additive phase generation 30](#_Toc66988015)

[a. Deterministic ‘bridge’ approach 30](#_Toc66988016)

[b. Energy based approach 34](#_Toc66988017)

[c. How to use 37](#_Toc66988018)

[d. Examples of generated additives 41](#_Toc66988019)

[VI. Filtering and segmentation 43](#_Toc66988020)

[1. Module purpose 43](#_Toc66988021)

[2. Importing a volume, saving progress, and keeping tracks of change 43](#_Toc66988022)

[3. Region of interest and microstructure visualization 45](#_Toc66988023)

[4. Modifying image format 51](#_Toc66988024)

[5. Upscaling and downscaling 53](#_Toc66988025)

[6. Quantifying image quality 55](#_Toc66988026)

[a. Grey level histogram and spatial homogeneity 55](#_Toc66988027)

[b. Phase separability 59](#_Toc66988028)

[c. Image noise 61](#_Toc66988029)

[7. Contrast enhancement 61](#_Toc66988030)

[a. Saturate extreme. 61](#_Toc66988031)

[b. Set custom grey level range 61](#_Toc66988032)

[c. Advanced contrast enhancement 63](#_Toc66988033)

[8. Image filtering 66](#_Toc66988034)

[a. Anisotropic diffusion filter 66](#_Toc66988035)

[b. Non-local mean filter 66](#_Toc66988036)

[9. Segmentation 67](#_Toc66988037)

[a. Volume segmentation 67](#_Toc66988038)

[i. Global thresholding 68](#_Toc66988039)

[ii. Local thresholding slice per slice 69](#_Toc66988040)

[b. Microstructure properties sensitivity with thresholding 71](#_Toc66988041)

[c. Phase reassignment 74](#_Toc66988042)

[VII. Microstructure characterization and homogenization 75](#_Toc66988043)

[1. Definition, unicity, limitations, and pseudo-parameters 75](#_Toc66988044)

[a. Microstructure characterization and microstructure homogenization 78](#_Toc66988045)

[2. About voxel size dependence and representative volume element analysis 79](#_Toc66988046)

[a. Image resolution and fractal issue 79](#_Toc66988047)

[b. The representativity issue and the concept of representative volume element 81](#_Toc66988048)

[i. Definition and methodology 81](#_Toc66988049)

[ii. RVE aspect ratio 82](#_Toc66988050)

[iii. RVE sensitivity with field of view 85](#_Toc66988051)

[iv. Alternative approach (not recommended) 86](#_Toc66988052)

[3. Module purpose and strength 88](#_Toc66988053)

[4. How to use 90](#_Toc66988054)

[a. With the graphic user interface (standard use) 90](#_Toc66988055)

[i. Import volumes 90](#_Toc66988056)

[ii. Choose microstructure properties to calculate 91](#_Toc66988057)

[iii. Save options, and run calculations 92](#_Toc66988058)

[b. Use algorithms as standalone functions from the command window 93](#_Toc66988059)

[c. Use raw algorithms without graphical results 93](#_Toc66988060)

[d. Link with other modules 94](#_Toc66988061)

[i. Link with Microstructure and results visualization module 94](#_Toc66988062)

[ii. Link with Properties correlation module 94](#_Toc66988063)

[e. Results organization 94](#_Toc66988064)

[5. Microstructure properties 95](#_Toc66988065)

[a. Volume fraction 96](#_Toc66988066)

[b. Connectivity 100](#_Toc66988067)

[c. Tortuosity factor 106](#_Toc66988068)

[d. Specific surface area 109](#_Toc66988069)

[i. Direct method 109](#_Toc66988070)

[e. Specific interface area 112](#_Toc66988071)

[f. Particle size 114](#_Toc66988072)

[i. Spherical assumption, continuum Particle Size Distribution (c-PSD) and particle level description 114](#_Toc66988073)

[ii. Euclidean distance map fitting method (EDMF). 117](#_Toc66988074)

[iii. Watershed method, discrete Particle Size Distribution (d-PSD) 119](#_Toc66988075)

[iv. Pseudo-Coulomb Repulsive field (PCRF) method, discrete Particle Size Distribution (d-PSD) 123](#_Toc66988076)

[g. Particle morphology deduced from particle identification 125](#_Toc66988077)

[h. Domain topology deduced from particle identification 125](#_Toc66988078)

[6. Module organization 126](#_Toc66988079)

[a. File hierarchy 126](#_Toc66988080)

[b. Typical file organization 126](#_Toc66988081)

[7. User-modification of the characterization module 131](#_Toc66988082)

[a. Integrate a new algorithm in the toolbox 131](#_Toc66988083)

[i. Prepare your algorithm 131](#_Toc66988084)

[ii. Create function that will call your algorithm in the toolbox 131](#_Toc66988085)

[iii. Update the GUI 132](#_Toc66988086)

[b. Modify an existing algorithm 133](#_Toc66988087)

[c. Save a 3D array to be used in the visualization module 134](#_Toc66988088)

[d. Save a new result in the summary table 135](#_Toc66988089)

[e. Save a result to be used in the correlation module 137](#_Toc66988090)

[VIII. Microstructure and results visualization 138](#_Toc66988091)

[1. Tiff data (grey-level and segmented volumes) 138](#_Toc66988092)

[2. Comparing grey-level and segmented volumes 141](#_Toc66988093)

[3. Microstructure characterization result 142](#_Toc66988094)

[IX. Properties correlation 147](#_Toc66988095)

[X. Create mesh for FEM 155](#_Toc66988096)

[1. Purpose of the module and restrictions 155](#_Toc66988097)

[2. Utilization 155](#_Toc66988098)

[3. Re-create the mesh in a dedicated FEM software 168](#_Toc66988099)

[a. Creating the mesh for a FEM model using FEniCS 168](#_Toc66988100)

[4. Example of mesh created with the module 170](#_Toc66988101)

[5. Common Iso2mesh error and workaround 173](#_Toc66988102)

[XI. Useful Standalone Functions 174](#_Toc66988103)

[XII. Knows issues/Frequently Asked Questions 177](#_Toc66988104)

[XIII. References 179](#_Toc66988105)

[1. Getting started with microstructure analysis 179](#_Toc66988106)

[2. Documentation references 179](#_Toc66988107)

# Introduction

Microstructure is a generic term used to describe a multi-phase/heterogenous medium, whatever its scale. It actually does not restrict to microstructure scale. This toolbox has been developed to support lithium ion battery modeling, for which the heterogeneous medium is a porous electrode, and the relevant scale is the microstructure, thus the toolbox name. Because of this electrode-centered approach, algorithms proposed in this toolbox are relevant for electrode microstructures, although they may be relevant for other medium as well.

Electrodes performances are strongly correlated with their microstructure, which then justify their analysis. To investigate their microstructure, they must be observed first experimentally. A large variety of imaging techniques exist9. While the experimental imaging is out of the scope of this document, it is important readers non familiar with electrode microstructures have a basic knowledge of the main techniques. Three are often reported in the battery/electrode literature: Scanning Electron Microscopy (SEM) for 2D imaging, and Focused Ion Beam Scanning Electron Microscopy (FIB-SEM) and X-ray computed tomography10,11 (CT) for 3D imaging. These imaging techniques are not limited to electrode materials12.

While some information can be extracted from a 2D image, anisotropic (i.e. with an orientation) and connectivity-related (e.g., diffusion, percolation) properties require a 3D volume to be accurately quantified. Field of view, i.e., the 3D volume imaged, is typically ranging from ~1e3 to ~1e6 µm3, with a voxel (pixel in 3D) size ranging from ~1e3 to ~1e6 nm3, with smaller voxel size associated with smaller field of view. Typical electrode materials have particle diameter ranging from ~1e1 nm (e.g. silicon anode) to ~1e1 µm (e.g., graphite anode and nickel manganese cobalt oxides cathode). The raw data obtained from 3D imaging experiment is a 3D array for which each voxel has a brightness value, that reflects the local sensitivity of the medium in regards with the imaging experiments. While analysis can be done at this stage, it is not the desired state as voxels do not identify each phase precisely. There is instead a distribution of grey level value (usually represented through a histogram). Volume are then ‘segmented’ or ‘binarized’ so that each voxel is assigned to a given phase, typically the pore or void domain, and the solid phase. If there are more than one solid phase, then each solid phase has its own voxel unique value to distinguish it from the other solid phases. This step is called segmentation. Figure 1 provides an example of a battery electrode microstructure.

|  |
| --- |
|  |
| *Figure I-1. (Top left) 3D visualization of a nickel manganese cobalt oxide electrode. (Top right, bottom left) the volume is initially described with gray level values. Bounds depend on the image datatype. In this case the image has been saved in 16 bits unsigned integer, thus from 0 to 65535. (Bottom right). After segmentation, each voxel has a non-ambiguous phase identification. Volume taken for this example comes from the NREL open source microstructure library*13*. Images have been generated with the present toolbox.* |

Microstructure analysis encompasses different activities or tasks, covered to a certain extent by the toolbox modules briefly introduced below and illustrated in figure I-2:

* *Microstructure generation* (cf. §V). Three-dimensional microstructure imaging requires expensive equipment, time, and skilled workers that limit availability and quantity of data. Furthermore, the microstructure design space is restricted by existing electrode materials, preventing upstream microstructure scale modeling. Microstructure generation algorithms allow to numerically generate 3D microstructures that can be used for design space analysis otherwise not possible. It is valuable to evaluate ‘what if’ microstructures that can later motivate manufacturers to experimentally test promising architectures. Microstructure generation includes active material generation and additives generation.
* *Filtering and segmentation* (cf. §VI). Before analyzing microstructure data, several preliminary tasks are required. The field of view may be cropped and/or rotated to select the region of interest. Data type may be converted for ease and size reduction. Volume may be upscaled or downscaled to match the desired image resolution. Image quality can be evaluated through different metrics, that in turn can indicate what segmentation approach is best suited. Image quality can be improved through contrast correction and/or image filtering in order to facilitate segmentation. Lastly, segmentation identifies phases from gray level values. In addition, microstructure parameters sensitivity analysis with the segmentation can be performed to provide error estimation.
* *Microstructure characterization and homogenization* (cf. §VII). Microstructure characterization and homogenization consists in extracting relevant parameters for macroscale models, such as particle size or effective diffusion, from the complex microstructure. Module offers automated voxel size dependence and representative volume element analysis, as well as batch calculations to characterize multiple volumes in a row.
* *Microstructure and results visualization* (cf. §VIII). Other modules generate 2D graph figures to illustrate results. However, 3D visualization may be more relevant in some occasion. This module produces 3D visualizations of the microstructure itself and of microstructure parameters defined voxel-wise. It also provides an overlay visual comparison of gray level and segmented volumes. Results can be saved both in static images and in videos.
* *Properties correlation* (cf. §IX). Establishing correlations between microstructure properties provides a better understating of their intrinsic relationships, help identifying independent parameters, and allow predicting microstructure properties. The most classic example would be the tortuosity factor as a function of porosity. This module allows you to load selected results from multiple microstructure characterization calculations quickly to produce correlation matrix-type figures. This module is especially valuable if your database contains dozens of microstructures and can reveal unsuspected correlations.
* *Create mesh for FEM* (cf. §X). Microstructure scale finite element modeling requires a mesh representation of the microstructure. This module produces un-structured, tetrahedron-based, 3D mesh of full-cell microstructure, with mesh density control. Please note this module does not do finite element modeling.

|  |
| --- |
|  |
| *Figure I-2. Illustration of the Microstructure analysis toolbox modules* |

Toolbox modules are connected through their inputs/outputs, as described in figure I-3. The characterization module occupies a central place as it can takes inputs from the generation module and the filtering and segmentation module, while its outputs are used for the properties correlation module and the microstructure and results visualization module.

|  |
| --- |
|  |
| *Figure I-3. Microstructure analysis toolbox module inputs/outputs connectivity.* |

This documentation can also be considered as an entry point for newcomers in the microstructure field as it provides introduction, comments, references for each section while also describing algorithms in detail. At the end of this document, you can find a list of references, sorted by topics, that could help you getting started in the wonderful world of microstructure analysis (cf. §XII-1).

# The open-source microstructure community

Information below may be outdated at the time you read it, as it concerns third parties.

## Open-source data

Having access to numerous microstructure volumes is extremely valuable as not only it allows researchers to develop and test algorithms even though they do not have the experimental capabilities to produce such data in the first place, but it also allows establishing correlation between different microstructure properties as such statistics analysis requires a lot of data to be relevant. Lastly, it makes easier to reproduce and validate works done by other groups, as data is shared. Copyrights/open-source policy/legal information are specific for each institution, please make sure to understand them before starting using their data. As well, please adequately quote the institutions when you are using their data. Below is a non-exhaustive list of microstructure data library:

**- National Renewable Energy Laboratory** (NREL) hosts a variety of Lithium ion cathode (nickel manganese cobalt [NMC]) and anode (graphite) electrode data samples, calendered and uncalendered with different loadings. Gray level and segmented data are both available at the NREL battery microstructure library: <https://www.nrel.gov/transportation/microstructure.html>

- **ETH Zürich** hosts NMC-​based Porous Electrodes, Polyethylene (PE) Separator, Commercial Graphite Electrodes, and various commercial anodes at the ETH Zürich Battery Microstructure Project: <https://made.ee.ethz.ch/research/open-source-data-and-software/battery-microstructure-project.html>

## Other open-source microstructure software

NREL is not the only institution developing open-source microstructure-related software. Many other projects are listed below (non-exhaustive list):

- **ImageJ**, <https://imagej.net/Welcome>, and **Fiji**, <https://fiji.sc/> are open platforms for scientific image analysis, with a lot of plugins thanks to their large community.

- **Neper**, <http://www.neper.info/>is a software package for polycrystal 3D generation and meshing.

- **PoreSpy**, <http://porespy.org/> is a collection of image analysis python tool used to extract information from 3D images of porous materials.

- **Openpnm**, <http://openpnm.org/>, an open source pore network modeling package.

- **The Microscopy Image Browser**, <http://mib.helsinki.fi/index.html>, is a high-performance Matlab-based software package for advanced image processing, segmentation and visualization of multi-dimensional (2D-4D) light and electron microscopy datasets.

# Installation and requirements

Copy the folder Microstructure\_analysis\_toolbox in your computer and add it to the MATLAB path, including subfolders (MATLAB ribbon interface: Set Path/Add with subfolders).

Third-party software installation:

* Iso2mesh: Copy <https://github.com/fangq/iso2mesh> in your computer and add the folder in your MATLAB path. Or download from <https://github.com/fangq/iso2mesh>. Make sure to choose the binary for your OS (Windows, Unix, or MacOS).
* TauFactor is already included in the toolbox. Although if you want to use it as a standalone app, or be sure to use the last UpToDate version of TauFactor, please download it from the MATLAB file exchange.
* Other third-party codes are already included in the toolbox repository.

The toolbox has been tested with MATLAB 2019b. The MATLAB toolbox “Image Processing” is required.

The toolbox has been tested in Windows. The meshing module performs better in a Unix environment (e.g., Ubuntu) due to a better RAM memory management. Some work is still required to ensure the code would work in a Unix environment (especially adjusting folder paths ‘\’ vs. ‘/’).

# How to use the toolbox

Open the file Microstructure\_analysis\_toolbox\src\Main\_menu\ Microstructure\_analysis\_tool.m with MATLAB and run it. The main menu will be displayed, from which you can choose what module to run (cf. Fig. IV-1). Each module has their own graphic-user interface. Please refer to their respective section (cf. §V-X) for help. You can also click on the ‘About’ button to go to the toolbox homepage, located in the NREL website, and on the ‘Open repository’ button to go to the GitHub repository webpage to check if an update is available. The documentation button will open this document.

|  |  |  |
| --- | --- | --- |
| |  | | --- | |  | | *Figure IV-1. Microstructure analysis toolbox main menu* | |

# Microstructure generation

## Why microstructure generation and module purpose

### Particle scale

Microstructure generation allows investigating various microstructures otherwise not available through experimental imaging or even manufacturing. Different methods are available in the literature14,15, that can be classed, for instance, according to the type of microstructure produced. Some methods prioritize credibility over control: the generated microstructures look very similar to a real microstructure, but with a limited control of the particle features14,15. Other methods prioritize control over credibility: the generated microstructures look obviously generated, but with a fine control of the particle features. Both approaches are valuable and choosing one is dependent on your application.

From a microstructure design space analysis point of view, controlling finely the particle features is very interesting. For instance, if you are asking questions such as ‘What is the impact of X on Y?’, with for example X being the particle size distribution or the particle alignment and Y the effective diffusion coefficient or some metric of the electrochemical cell performance, being able to finely choose X is important. Furthermore, determining particles metrics from a microstructure volume is very challenging, and strongly depends on the chosen method (cf. §VII-5f), therefore choosing X beforehand as an input parameter of the generation algorithm is very valuable. Say otherwise, with a credibility over control approach, X can still be determined afterwards but with uncertainty, while with a control over credibility approach, X is an input and does not require to be calculated. The in-house generation algorithm of this module has been developed in the frame of a microstructure design space analysis, to investigate ‘what if’ electrodes in order to find promising lithium ion battery electrodes suitable for fast charge application. Therefore, the algorithm proposed in this module follows the control over credibility approach.

Another possible application of microstructure generation consists in testing existing microstructure parameter relationships or establishing new ones. For instance, tortuosity factor-porosity and specific surface area-particle diameter relationships. These correlations are microstructure dependent (e.g., they are different if the microstructure is sphere-based or ellipsoid-based) and have a range of validity (e.g., high porosity range). Generation algorithm can produce numerous microstructures to test shape dependence and investigate a large parameter range. Such microstructure parameter relationships are very valuable as they are typically used in macroscale electrochemical models. A control over credibility approach suits better such problem as microstructure parameters need to be clearly determined to be relevant.

### Additive scale

Experimental imaging has intrinsic limitations depending on the method selected that may result in not being able to distinguish one or several phases of the medium. For instance, computed tomography of lithium ion battery electrodes such as NMC and graphite do not resolve the additive phases (carbon-black, for improved electron conductivity and binder, for mechanical integrity), that are not distinguishable from the pore domain16. Such additives have practical impact, as they modify the effective electrolyte diffusion coefficient and the interfacial electrochemically active area between the active material and the electrolyte8,16,17. Therefore, not being able to represent them hinders electrochemical model predictions. To remedy this issue, the additive phase can be generated in the pore domain of a microstructure. Various strategies have been considered in the literature, physics-based8 and deterministic18 approaches.

In this module, an original simple in-house deterministic approach is proposed in addition to the physics-based approached reported in8.

## Particle generation

### Algorithm explained

The algorithm allows generating microstructures with the following specifications:

* N-solid-phase microstructure generation ellipsoid-based algorithm.
* Volume fractions, particle size distribution, particle elongation distribution, and particle orientation distribution defined for each slice along the microstructure thickness. It allows generating graded microstructures (i.e., with properties varying along their thickness) with in-plane heterogeneities (since distributions functions are defined per slice).

The algorithm main numerical features are described below:

* Stochastic (i.e. probabilistic) iterative algorithm, with particles generated sequentially.
* Each time a new particle is generated, all probabilities for the slices that cut through the new particle are updated accordingly to match the user-defined volume fraction, particle size, elongation, and orientation distribution targets. For instance, after a particle is generated, the probability that a particle of the same phase is generated later in the same region is decreased accordingly in order to match the user-defined volume fraction targets (as a result probabilities for the other phases are adjusted too). Ideally, with an infinite domain’s size such probability correction would not be required: if you toss a coin an infinite number of times, each side appears with a probability of 50% in average. But if you only consider the first ten times, it is very likely the probability will be off. The correction used in the algorithm ensures that volume fraction targets (and similarly for size, orientation and alignment distributions targets) are achieved even though the volume size is limited and that we ‘toss’ particles only a limited number of time. It allows generating microstructures that match user-defined parameters with a relatively low domain’s size, effectively reducing CPU time. Nevertheless, such correction artificially reduces heterogeneity: performing representative volume element analysis with such generated microstructures is not recommended.

Updating probability to generate a particle that belongs to the phase *i* within the slice *x* is done as follow. First the remaining volume fraction is deduced, and a random number is picked from 0 to 1 to test if a particle will be generated locally. As the generation process is moving on, the current volume fraction will increase, and eventually reach the target volume fraction, thus preventing overshooting the target volume fraction.

Updating probabilities of a distribution function, i.e., the probability a parameter (such as particle diameter) takes a value among n different values is done by normalizing the distribution function depending on the current distribution:

For instance, if the local target size distribution is 40% with a diameter v1 and 60% with a diameter v2 (n=2) and that during the generation process, we have generated 10% particles with a diameter v1 and 50% with a diameter v2, (we still need to generate the remaining 40%, 100% corresponding to reaching the target volume fraction of the current phase), then the probability distribution considered at this stage of the generation process is: (0.4-0.1)/(0.4-0.1 + 0.6-0.5)=0.75 for v1 and (0.6-0.5)/(0.4-0.1 + 0.6-0.5)=0.25 for v2. At this stage, the chance to select the diameter v1 are higher since we have already almost reached the target for v2.

* Particle overlapping is controlled independently for each phase *i* - phase *j* permutation, with a gradation allowing fine control of the overlapping. If overlapping is authorized, there is the risk a particle gets overlapped successively by other particles, up to the point its initial morphology has been excessively degraded. To avoid this, you can set a constraint to the minimum volume a particle must conserve, taking as reference its volume when first generated. Overlapping is particularly interesting as it enables generating microstructures with very high percolation or connectivity (similarly with computed tomography lithium ion battery electrodes) and allows reaching high density microstructures (effectively avoiding packing density limit).

|  |
| --- |
|  |
| *Figure V-1. Particle overlapping. Color is coded with particle id.* |

* Naïve user-defined parameters that correspond to an impossible microstructure will lead the algorithm to stall. For instance, a bi-phase microstructure (pore and one solid) with unisize non-overlapping sphere and a porosity of 10% is theoretically impossible due to packing density.
* The generation order can be tuned to avoid the algorithm to stall for some microstructures that could be challenging to generate without generation order control. To illustrate this, let us consider the case of a bi-phase material (pore and one solid) with a bi-modal size distribution for the solid, with the small particles being significantly smaller compared with the large particles. If we try generating the solid without order control, we may generate smaller particles that will block the introduction of the larger ones. Chance of success are much higher if we decide to first generate the large particles, and only then the small ones, as illustrated in the figure below. To reproduce this generation behavior, the user can define several ‘generation pass’ the algorithm will iterate on. For each pass, the user can decide the volume fraction ratio each phase should reach before the algorithm moves to the next phase. In our example, instead of generating a bi-phase, the user would generate a tri-phase material (pore, small particles, large particles,) and ask for 2 generation pass, with for the first pass a ratio 0.0 for the small particles and 1.0 for the large particles, and for the second pass, a ratio 1.0 for both phases. Once done, the two solid phases can be easily merged.

Loop over pass

Loop over phase

While volume fraction(phase) target ratio (pass) x target volume fraction(phase)

Generate new particle

|  |
| --- |
|  |
| *Figure V-2. Controlling generation order increase chance of success* |

* Once the generation is finished, an in-house upscaling algorithm can be used. It is much faster to generate using a coarse grid resolution, and then upscale to the desired image resolution while generating directly at the fine scale.

|  |
| --- |
|  |
| *Figure V-3. Custom upscaling algorithm works for n-phase and reduce aliasing* |

The generation algorithm is available in function\_generate\_ellipsoid\_microstructure.m and is presented in detail in figure V-4.

|  |
| --- |
|  |
| *Figure V-4. Microstructure generation pseudo-code algorithm* |

### How to use

Click on the ‘microstructure generation’ button from the main menu GUI, and then click on ‘ellipsoids-based’. GUI is still in BETA but is usable.

Please follow instructions provided in each tab. Additional information is provided below.

In the first tab, (‘Phase and volume fractions’), you need to enter the domain’s size and the scaling factor. The generated volume in the example below will a 3D array of size (100,100,150), that will be upscaled afterwards to a size of (200,200,300). The voxel size is only indicative, as the algorithm is adimensional. You then need to enter the number of solid phase as well as their id (code) and name. In the example below, the generated volume would be three-phase materials: {pore, solid 1, solid 2}.

|  |
| --- |
|  |
| *Figure V-5a. Domain ‘size and number of phases.* |

On the right side of the tab, you can choose the volume fractions for the solid phases.

|  |
| --- |
|  |
| *Figure V-5b. Volume fractions are defined for few user-selected slices (here 3: z=0, 0.4 and 1, along the third-axis), and linearly interpolated in between. Graph shows the parameter inputs.* |

Before moving the next tab, make sure to validate your choice by clicking on ‘Click to save all the input parameters’.

On the second tab (‘Particle size’), you can specify for each phase the size distribution

|  |
| --- |
|  |
| *Figure V-5c. Particle size is defined for three slices, and linearly interpolated in between. For instance, for the middle position (z=0.5) 40% of the particle phase have a 11-voxels length diameter D3, 40% a 17-voxels length diameter D3, and 20% a 29-voxels length diameter D3. The two other tables control particle elongation D1/D2 and D1/D3. Percentages correspond to the phase volume, and not to the number of particles.* |

On the right side of the tab, you can visualize a particle example to help you choosing the diameter parameters.

|  |
| --- |
|  |
| *Figure V-5d. Particle visualization for a given set of particle diameter and elongation.* |

You need to provide the diameter information for each phase (and save them) before moving to the next tab.

The third tab (‘Particle orientation’), is similar with the diameter tab. As well, you can plot a particle example to have a better insight on the orientation parameters.

In the fourth tab (‘Particle overlapping’), you can set the phase overlapping, the minimum volume to conserved, and the order of generation.

|  |
| --- |
|  |
| *Figure V-5e. Overlapping factor between particles of phase 1 is 0.5, and 0.25 between particles of phase 1 and 2. No overlapping is allowed between particles of phase 2.* |
|  |
| *Figure V-5d. Particle overlapping is restricted so that any particle of both phase conserve at least 50% of its initial volume when initially generated.* |
|  |
| *Figure V-5e. In the first pass, all the solid 2 will be generated. In the second pass, the solid 1 will be generated.* |

In the next tab (‘Post-processing and Save options’), select your save folder, and choose if you wish to calculate the tortuosity factor once the generation will be finished. To run the generation process, enter the number of times you wish to run the generation algorithm in the ‘run code’ tab, then click on the button ‘Generate Microstructure’. After generation is finished, figures are automatically displayed that show the difference between the input parameters and what has been obtained.

In the ‘generated microstructures’ tab, volume fractions as well as tortuosity factor (if the option has been checked) are displayed for each generated volume, which is useful to verify the algorithm reproducibility. If you observe a significant difference between volumes, you need to increase the domain’s size and/or to reduce the absolute diameter length (i.e., increasing the number of particles in the domain).

### Examples of generated microstructures

Figure below illustrates generation capabilities offered by the particle generation algorithm. While microstructures look obviously generated, features such as particle size and alignment are clearly identifiable as they are inputs (control over credibility approach, cf. §V-1a). Bilayers can be easily generated using four slices for the various microstructure parameters to setup a step function. For instance, position along direction 3: {0, 0.39, 0.41, 1} associated with volume fraction {0.6, 0.6, 0.3, 0.3}. Pore former are simply obtained by re-assigning one of several phases to the background after the generation.

Example files are available in the repository at \Data\_example\Numerically generated\.

|  |
| --- |
|  |
| *Figure V-6. (Top left) bi-modal size distribution, (top right) ellipsoids with a preferential orientation, (bottom left) bi-layer with different porosity, particle size, particle alignment and orientation between the two layers, and (bottom right) bi-layer with pore former. Images have been generated using the visualization module (cf. §VIII).* |

## Additive phase generation

### Deterministic ‘bridge’ approach

Additive phase is generated assuming it is preferentially located between particles non far from each other, so that it will create bridges between particles. First the pore particle size is calculated using a spherical approach (method detailed in §VII-5f-i). The original algorithm then iterates over a distance *d*, marking pore voxels for which . If the as marked voxels are not enough to reach the additive target volume fraction, then all of them are assigned to the additive phase and then *d* is incremented until the additive volume fraction is reached. If too many voxels have been identified, only a subset of them are assigned to the additive phase to match its target volume fraction.

The sphere-size tends to assign numerous one-voxel size particles at the phase boundary. To avoid generating a thin-like additive surface – which is not the goal of this particular generation algorithm – the user can specify a minimum distance (‘minimum distance from boundary in voxel length’, by default 1) for which voxels are not considered below.

The user can add some stochasticity in the process by only adding, for each increment of d, only a ratio of all the voxels that verify the criterion . In this case, voxels are added connected cluster per connected cluster until reaching the ratio. The parameter ‘Randomize cluster selection’ control the level of stochasticity (with a default value of 0, i.e. false, otherwise the value between 0 and 1 corresponds to the ratio).

binary\_phase=zeros(size(Microstructure)); % Initialization

binary\_phase(Microstructure == background\_id) = 1;

[distance\_bnd2bnd] = Function\_particle\_size\_CPSD\_Algorithm(binary\_phase);

distance\_bnd2bnd(distance\_bnd2bnd==0)=9e9; % Remove background

distance\_bnd2bnd(distance\_bnd2bnd<=minimum\_dist\*sqrt(3))=9e9;

ntot = numel(Microstructure);

current\_additive\_volumefraction = 0; % Initialize

d=0; % Initialize

while current\_additive\_volumefraction < target\_volume\_fraction

d=d+1; % Increment distance

if d>minimum\_dist\*sqrt(3)

potential\_additives = distance\_bnd2bnd<=d;

n = sum(sum(sum(potential\_additives)));

if n>0

if randomize\_level==0

if n/ntot <= target\_volume\_fraction-current\_additive\_volumefraction

Microstructure(potential\_additives)=additive\_id;

else

[L,ncluster] = bwlabeln(potential\_additives,18);

cluster\_possibility=1:1:ncluster;

while current\_additive\_volumefraction <= target\_volume\_fraction

cluster\_choice=randi(length(cluster\_possibility));

Microstructure(L==cluster\_possibility(cluster\_choice))=additive\_id;

current\_additive\_volumefraction = sum(sum(sum(Microstructure==additive\_id)))/ntot;

cluster\_possibility(cluster\_choice)=[];

end

end

else

[L,ncluster] = bwlabeln(potential\_additives,18);

cluster\_possibility=1:1:ncluster;

volume\_increment=0; % initalize

while volume\_increment <= (1-randomize\_level)\*n

cluster\_choice=randi(length(cluster\_possibility));

loc = L==cluster\_possibility(cluster\_choice);

Microstructure(loc)=additive\_id;

volume\_increment = volume\_increment + sum(sum(sum( loc )));

cluster\_possibility(cluster\_choice)=[];

end

end

end

end

distance\_bnd2bnd(Microstructure==additive\_id)=9e9;

current\_additive\_volumefraction = sum(sum(sum(Microstructure==additive\_id)))/ntot;

end

|  |
| --- |
|  |
| *Figure V-7a. (Top left) Sphere-size of the pore domain. (Others) Pore voxels for which are assigned to the additive phase iteratively.* |

Surface irregularities typically lead to small irrelevant additives and pore regions at the particle surface. These regions are corrected applying erosion steps sequentially, as described below:

* User can specify an erosion distance (‘erosion depth in voxel length’) to assign additive regions with a spherical size below this erosion distance to the background.

binary\_phase=zeros(size(Microstructure)); % Initialization

binary\_phase(Microstructure == additive\_id) = 1;

[distance\_bnd2bnd] = Function\_particle\_size\_CPSD\_Algorithm(binary\_phase);

distance\_bnd2bnd(distance\_bnd2bnd==0)=9e9; % Remove background Microstructure(distance\_bnd2bnd<(erosiondepth\*sqrt(3)+0.0001))=background\_id;

* Because the initial generation has been restricted with a minimum distance (‘minimum distance from boundary in voxel length’), the algorithm results in tiny pores between the solid and the additive phases. A similar approach is used to remove them:

binary\_phase=zeros(size(Microstructure)); % Initialization

binary\_phase(Microstructure == background\_id) = 1;

[distance\_bnd2bnd] = Function\_particle\_size\_CPSD\_Algorithm(binary\_phase);

distance\_bnd2bnd(distance\_bnd2bnd==0)=9e9; % Remove background

Microstructure(distance\_bnd2bnd<minimum\_dist\*sqrt(3)+0.0001)=additive\_id;

* This last operation has likely added more additive than required. Additive connectivity is calculated, and clusters (from smaller to larger) are iteratively removed until the target volume fraction is reached.

delta = round(sum(sum(sum( Microstructure==additive\_id ))) - numel(Microstructure)\*target\_volume\_fraction);

erosion\_cluster = true;

while delta>0

app.TextArea.Value = {'Resorbing volume fraction','difference...'}; pause(0.01);

binary\_phase=zeros(size(Microstructure));

if erosion\_cluster==false

% Random voxel erosion

binary\_phase(Microstructure==background\_id) = 1;

distance\_map = bwdist(binary\_phase,'chessboard');

distance\_map(Microstructure ~= additive\_id)=2;

idx = find(distance\_map<2);

if length(idx)<=delta

Microstructure(idx)=background\_id;

else

tmp = randi(length(idx),delta,1);

Microstructure(idx(tmp))=background\_id;

end

else

% Cluster erosion

binary\_phase(Microstructure==additive\_id) = 1;

[L,~] = bwlabeln(binary\_phase,18);

% Determine cluster size

[C,~,ic] = unique(L);

a\_counts = accumarray(ic,1);

size\_cluster = [C, a\_counts];

size\_cluster = sortrows(size\_cluster,2); % Sort in ascending order

while size\_cluster(1,2)<delta && delta>0

Microstructure(L==size\_cluster(1,1))=background\_id; % Smallest cluster is removed

delta = round(sum(sum(sum( Microstructure==additive\_id ))) - numel(Microstructure)\*target\_volume\_fraction);

size\_cluster(1,:)=[]; % Smallest cluster is removed from the list

end

erosion\_cluster = false; % Switch to voxel erosion

end

delta = round(sum(sum(sum( Microstructure==additive\_id ))) - numel(Microstructure)\*target\_volume\_fraction);

end

|  |
| --- |
|  |
| *Figure V-7b. (Top left) Initial generation, (Top right) after additive voxel erosion, (bottom left) after pore voxel erosion, and (bottom right) after additive cluster-per-cluster iterative erosion* |

Once all erosions steps are applied, most additives are located between neighbored particles, as intended. Note that

### Energy based approach

Method is presented in details in8, and has been developed by Aashutosh Mistry (Chemical Sciences & Engineering Division, Argonne National Laboratory, Lemont, Illinois 60439, United States, ORCID: 0000 – 0002 – 4359 – 4975) and Partha P. Mukherjee (School of Mechanical Engineering, Purdue University, West Lafayette, Indiana 47907, United States, ORCID: 0000 – 0001 – 7900 – 7261).

Candidate voxels (candidate voxels have at least one solid neighbor and are within the background phase) assignment to the additive phase is based on an energy towards deposition on the pre-existing active material network or on the pre-deposited new additive phase. A user-defined morphology parameter (adimensional, [0,1]) is used to bias the energy towards deposition for the candidate voxel *k*, , preferentially on existing active material () or on pre-deposited additive phase ():

|  |  |
| --- | --- |
|  | [V-1] |

With the number of voxels adjacent to the candidate voxel that belong to the phase *i*. The two extremes values, 0 and 1, maximize the deposition energy for candidate voxels which are surrounded, respectively, by the pre-existing solid network or by the previously deposited additive phase. Therefore, a near 0 value will result in generating a thin layer of additive phase at the particle surface, while a near 1 value will result in generating a dendritic-like additive phase. The local energy deposition is normalized by dividing by 6 as due to the cuboid voxel representation of the microstructure. The energy deposition cumulative function is then calculated, considering only candidate voxel with a non-zero energy deposition:

|  |  |
| --- | --- |
|  | [V-2] |

The cumulative function is used to select candidate voxels, preferentially those with a high energy deposition, that will be assigned to the additive phase as explained in the figure below.

|  |
| --- |
|  |
| *Figure V-7c* Candidate voxels are assigned to the additive phase based on the energy cumulative function according to a stochastic (i.e., a random) process. |

The key point being that candidate voxels with low energy deposition corresponds to a flat region of the cumulative function. Therefore, these candidate voxels have a lower probability to be selected compared with voxels with higher energy deposition that correspond to the sharp variation of the curve. Note that this property is true only for a non-random energy deposition among the candidate voxels (empirically verified for microstructures). The average energy deposition among the selected voxels is then higher than the average energy deposition among the candidate voxels. The stochastic process allows for some candidate voxels to be selected even though they have a low energy deposition. This choice is motivated from the fact that low energy events are possible but with a lower probability and then should not be discarded entirely from the deposition process.

The initial candidate voxels are typically not enough to reach the additive phase volume fraction target. Therefore, the deposition process is iterative (the whole loop of figure V-7c), with each new round of deposition starting with updating the energy deposition since the microstructure has been modified with the voxels assigned to the additive phase from the previous iteration. Each round of deposition adds a maximum fraction of the additive phase volume target volume fraction (by default 1%). The user can select a larger value, resulting in less iterations, while a smaller value will require more iterations but will provide a more progressive growth of the additive phase as the energy map will be actualized more often.

The deposition process is summarized in the figure V-7d.

Articles based on this code:

* Mistry, Smith & Mukherjee (2018) doi: 10.1021/acsami.7b17771
* Mistry, Smith & Mukherjee (2018) doi: 10.1021/acsami.8b08993
* Usseglio-Viretta *et al.* (2018) doi: 10.1149/2.0731814jes
* Trembacki *et al.* (2018) doi: 10.1149/2.0981813jes
* Mistry & Mukherjee (2019) doi: 10.1039/C8CP05109G
* Mistry, Verma & Mukherjee (2019) doi: 10.1021/acsami.9b05468
* Mistry, Smith & Mukherjee (2020) doi: 10.1021/acsami.9b23155
* Mistry *et al.* (2020) doi: 10.1149/1945-7111/ab8fd7

|  |
| --- |
|  |
| *Figure V-7d* *A flow chart explaining the flow of logic and data between different routines to add CBD phase in an active material skeleton*8,19*.* |

### How to use

Click on the ‘microstructure generation’ button from the main menu GUI, and then click on ‘Additives’ to load the additive generation module. In the first tab (‘Load volume and volume fraction’), load a tif segmented volume, select the background phase within which the additive phase will be generated (by default the first phase), enter the volume fraction of the additive phase, and lastly enter the code to assign for voxels that will belong to the additive phase. The target volume fraction is deduced from the dense volume fraction and the nanoporosity:

|  |  |
| --- | --- |
|  | [V-3] |
|  | | |
| *Figure V-8a. Load volume tab* | | |

Depending on the generation method you want to use, go to the second tab (‘Between neighbours particles’) or the third tab (‘Energy criterion’). Each tab allows you to modify the method’s parameters (within their bounds) from their default values. Parameters are described in the previous sections.

|  |
| --- |
|  |
| *Figure V-8b. Option to generate additive phase between neighbours particles.* |
|  |
| *Figure V-8c. Option to generate additive phase using energy criterion.* |

The ‘Outcome’ tab allows the user to verify the generation process, both globally through the volume fractions, but also locally by visualizing the modified microstructure. It’s also the place where you can save the modified microstructure.

|  |
| --- |
|  |
| *Figure V-8d. Verify generation outcome and save modified microstructure.* |
|  |
| *Figure V-8e. Interactive figure provided with the ‘Visualize’ button (energy criterion method, ).* |

The last tab provides general information about the module, and how to quote results produced with it.

|  |
| --- |
|  |
| *Figure V-8f. General information about the additive phase module, and quotation instructions.* |

### Examples of generated additives

Example files are available in the repository at \Data\_example\From computed tomography with additives numerically generated\.

|  |
| --- |
|  |
|  |
| *Figure V-9. Additive phase (0.1 volume fraction) added to an existing microstructure. Images have been generated using the visualization module (cf. §VIII). (Top) 3D view of microstructure with additive generated with the bridge approach, and (bottom row) 2D views comparing the different approaches/parameters.* |

# Filtering and segmentation

## Module purpose

Image filtering20,21 and segmentation22,23 have their own field of research and are abundantly covered in the literature. Other open-source software, such as ImageJ (cf. §II), have extensive library of numerical methods to filter and segment 2D and 3D images. This module does not have the ambition to provide an exhaustive list of methods. Instead it focuses on delivering a user-friendly experience to improve productivity of various pre-characterization tasks, that can be time-consuming and frustrating with less intuitive tools. While methods currently available in this module are quite simple, they nevertheless proved to be enough to segment NMC and graphite electrode volumes from the NREL microstructure library13. For more advanced methods, the user is invited to rely on ImageJ. Module instructions are provided in the first tab.

## Importing a volume, saving progress, and keeping tracks of change

Most tabs are empty until you load a volume. To do so, click to Volume/Load volume in the menu selection. Once the volume has been loaded, basic information is displayed in the first tab. In the second tab named ‘Save/display options’ you can select the save folder, if you want to save figures generated during various tasks (e.g. grey-level histogram), and the figure font name. Note that the ‘current file name’ uses the same name of the loaded file, but concatenated with ‘\_step\_X.tif’, with X being initially equal to 1 as the step 1 corresponds to the volume loading. Each time a task *that modifies the microstructure volume* (e.g., cropping) is performed the step number is incremented and the history log (see last tab, named ‘History’) is updated. If you click to Volume/Save volume/Default location, the current state of the volume is saved in the save folder using the ‘current file name’. Furthermore, when a volume is saved, the history log is saved as well in an excel file in the same folder and with the same name (except for the file extension). This avoid overwriting files and help keeping tracks of changes. This is particularly valuable to remind how a volume has been segmented months after having done it. You can also save volumes using Volume/Save volume/Custom location to manually select a folder and name. It is sometimes interesting to save a volume at different steps to document the various steps required for its segmentation.

Tasks that change the volume data (e.g. cropping, filtering etc.) require the user to click on the blue button ‘Do’ to realize them. Once done, the ‘Do’ button is greyed out while the orange ‘Undo’ button and the green ‘Save’ button are enabled. If not in your current tab, you can always visualize the modified volume in the ‘Region of Interest/View’ tab. If you are satisfied with the change, please click on the ‘Save’ button. Be careful as you cannot undone changes after clicking on the save button. History log and 'current file name’ are updated only after clicking on the save button. If you are not satisfied with the change, please click on the ‘Undo’ button. Note that you cannot perform any other changing tasks until you have either clicked on the ‘Save’ or ‘Undo’ buttons as other ‘Do’ buttons are greyed too.

|  |
| --- |
|  |
| *Figure VI-1. First tab after a volume has been successfully loaded* |
|  |
| *Figure VI-2. Example of an history log after few basic steps* |

## Region of interest and microstructure visualization

Visualization and basic region of interest (ROI) operations are accessible in the ‘Region of Interest / View’ tab. Visualization options are located at the bottom right. ‘Save current 2D view’ will simply save the current visualization with the title indicating the slice number. Note that figures are saved only if the option is checked in the second tab. ‘Plot and save 3D view (orthogonal slices)’ shows a good overview of the microstructure communicable through a unique picture. Plotting the orthogonal slices is done using the MATLAB built-in function *slice*, which is very RAM expensive, and may not be appropriate for very large volume. ‘3D view’ calls the MATLAB built-in function *volshow*, mostly valuable for segmented volume. Since figure names are concatenated with the step number, saving during the imaging processing is a good way to keep a visual track of the various modifications applied to the volume.

|  |
| --- |
|  |
| *Figure VI-3. Region of interest selection and microstructure view* |

|  |
| --- |
|  |
| *Figure VI-4. Figure generated with* ‘Plot and save 3D view (orthogonal slices)’. |
|  |
| *Figure VI-5. Figure generated with ‘3D view’ for a segmented volume.* |

You can perform several operations in this tab:

* *Cropping*. You can enter directly cropping bounds in the table of the ‘Crop volume’ section. Bounds are represented with red dashed line to help the user choosing them. Voxel size is purely optional and is used to multiply the domain’s size (value is reported in the length column), to provide the physical dimension of the domain. If the background value is known (in this example: 0), an auto-cropping can be realized by first selecting the auto-crop option from the menu selection (‘Cylindrical FOV’ or ‘After rotation’) and then on clicking on the ‘Crop background’ button. Auto-cropping requires the background to be consistent along all slices. To finalize the cropping, you must click on the ‘Do’ button.

|  |
| --- |
|  |
| *Figure VI-6a. Cropping bounding automatically detected using the ‘cylindrical FOV’ menu selection. The third axis must be normal with the field of view as in this figure (use swapping axis otherwise to make it so). First slice is used to detect the background. The cylindrical FOV is typical for Computed tomography experiments.* |
|  |
| *Figure VI-6b. Cropping bounding automatically detected using the ‘After rotation’ menu selection. Only bounds of axis 1 and 2 will be found, so you may have to swap axis to set your volume orientation as in this image, crop axis 3, and then do the auto-cropping.* |

* *Flip or swap axis*. ‘Flip’ returns an axis, while ‘swap’ switches two axis. This is valuable to orient a microstructure according to your axis convention. This is particularly relevant when analyzing several volumes, for which imaging experiments may have different orientations. For instance, for electrode battery one can systematically uses the third axis for the electrode thickness.

|  |
| --- |
|  |
| *Figure VI-7a. (Left) Before and (right) after swapping axis 1 with axis 3.* |
|  |
| *Figure VI-7b. (Left) Before and (right) after flipping axis 3.* |

* *Rotation*. Imaging experiments usually try to keep the material orientation, if any. For electrode battery, it means aligning one axis with the electrode thickness, that is normal to the current collector plane. However, alignment is often slightly off and you may have to correct it especially if you are interesting with calculating oriented properties such as tortuosity factors. To do so, you can use the ‘Rotation’ section of the tab. First select the axis rotation, and then choose your angle rotation. Red dashed lines are draw automatically to indicate the angle rotation (if you do not see them, you are using the wrong angle axis rotation). Because rotation uses a lot of RAM, a good practice consists in cropping your volume first, and then do the rotation. You may also swap axis before doing the rotation for ease. The MATLAB documentation provides details about geometric transformations (see <https://www.mathworks.com/help/images/matrix-representation-of-geometric-transformations.html>). The pseudocode below explains how rotations are applied.

angle\_rad = deg2rad(angle\_deg); % Angle in radians

-For 3D volume:

transformation matrix that rotates the image around the 1st axis

t = [cos(angle\_rad) 0 -sin(angle\_rad) 0

0 1 0 0

sin(angle\_rad) 0 cos(angle\_rad) 0

0 0 0 1];

transformation matrix that rotates the image around the 2nd axis

t = [1 0 0 0

0 cos(-angle\_rad) sin(-angle\_rad) 0

0 -sin(-angle\_rad) cos(-angle\_rad) 0

0 0 0 1];

Transformation matrix that rotates the image around the 3rd axis

t = [ cos(angle\_rad) sin(angle\_rad) 0 0

-sin(angle\_rad) cos(angle\_rad) 0 0

0 0 1 0

0 0 0 1];

-For 2D image:

Transformation matrix that rotates the image around the 3rd axis

t = [ cos(angle\_rad) sin(angle\_rad) 0

-sin(angle\_rad) cos(angle\_rad) 0

0 0 1];

Then pass the matrix to the affine3d object constructor.

t\_form = affine3d(t);

Microstructure = imwarp(Microstructure,t\_form); Apply geometric transformation to image

|  |
| --- |
|  |
| *Figure VI-8. (Left) Before and (right) after a 6.5-degree rotation normal to axis 2 used to align the volume. Note dimensions have changed.* |

Once the rotation done, you may have to crop the useless background added during the geometric transformation. You can do it manually or use the auto-crop feature presented in the ‘cropping’ section.

* *Background detection*. The background is not always clearly identified. Although, background is often much more uniform compared to the microstructure combined pore and solid material phases. In the ‘Background detection’ section, you can set parameters (standard deviation threshold and mean filter range) used to identify background based on this assumption. First, standard deviation is averaged using a 2D mean filter: large background regions only contain background, while large microstructure regions contain both pore and solid phase(s) with significant different grey level values. If the grey level value dispersion within the background is inferior to the grey level value dispersion within the microstructure, then the average standard deviation will be lower within the background and a threshold can identify it. The identification can be done only for the first slice of the 3rd axis and then used for the others slice to speed up the calculation (relevant if the background location is identical among all slices), or slice per slice. Below is a pseudocode of the background identification process:

sdImage = stdfilt(Microstructure(:,:,k)); % Calculate standard deviation of slice k

sdImage\_filtered = medfilt2(sdImage,[Median\_filter\_range Median\_filter\_range]); % Apply moving averge filter on square regions of size Median\_filter\_range\* Median\_filter\_range

index\_background=find(sdImage\_filtered<Std\_threshold); % Threshold it and find coordinates

Microstructure(index\_background,k)=Set\_identified\_background\_value;

|  |
| --- |
|  |
| *Figure VI-9. (Left) Before and (right) after background identification.* |

* *Remove/modify slices*. This section is useful if some intermediate slides are corrupted or abnormally blurred. You can remove these slices or replace with interpolated values. Interpolating is recommended as removing slices will create a discontinuity within the electrode. See section ‘Modify some slices along’.

|  |
| --- |
|  |
| *Figure VI-10. (Left) Before, (center) after removing slices, and (right) after interpolating slices.* |

## Modifying image format

Microstructure data can be saved in various formats. For segmented volume, the format of choice is 8-bit unsigned integer arrays, as the number of different phases is typically inferior to 256 and positive. For grey-level volumes, the choice depends on the image quality and noise. Typically, it is recommended to use a format that provides just enough granularity to perform the segmentation. For instance, if moving the segmentation threshold of 1 grey-level, from the reference threshold, changes too much the volume fractions, it indicates the image has been compressed too much. On the other side, using a too large data range use more storage space, and algorithms that iterate over grey level values will be slower. Therefore, finding a compromise is required. You can quantify the segmentation sensitivity with the threshold in the ‘Segmentation (sensitivity)’ tab (cf. §VI-9b), if required. You can also compare the shape of the grey-level histogram (cf. §VI-6) before/after format change, as a change would reveal a too high compression. An indicator of an over or under sized data format is the utilization ratio, which is the number of grey-level value used over the data range length. In the figure VI-11, the 16-bit unsigned image uses ~73% of the 65536 possible values, and ~89.5% of the 256 possible values once converted in an 8-bit unsigned format. After compression, the image looks nearly identical suggesting the 8-bit unsigned format is enough. You can convert image format in the tab ‘Format conversion’, with the following choices:

|  |  |
| --- | --- |
| Choice | MATLAB command |
| 8-bit unsigned integer arrays | Microstructure =uint8(Microstructure) |
| 8-bit unsigned integer arrays (rescale) | Microstructure =im2uint8(Microstructure) |
| 16-bit unsigned integer arrays | Microstructure = uint16(Microstructure) |
| 16-bit unsigned integer arrays (rescale) | Microstructure = im2uint16(Microstructure) |
| 32-bit unsigned integer arrays | Microstructure = uint32(Microstructure |
| 64-bit unsigned integer arrays | Microstructure = uint64(Microstructure |
| double precision array (rescale) | Microstructure = im2double(Microstructure |

Please refer to the MATLAB documentation for the operators used. Always check the microstructure in the ‘Region of Interest / View’ tab before clicking the ‘Save’ button to make sure you did not degraded the image. Please note that can you also specify a custom data range (without modifying the data format) in the ‘contrast correction’ tab (cf. §VI-7).

|  |
| --- |
|  |
| *Figure VI-11. (Left) Before, and (right) after format conversion from 16 bits unsigned integer to un 8 bits unsigned integer with the rescale choice. Note that with the default 8bit conversion, not rescale, (i.e., uinnt8), the result is a uniform 255. (Bottom) Table indicates volume values bounds, format, utilization ratio and size.* |

## Upscaling and downscaling

You can perform 3D microstructure upscaling and downscaling in the ‘Up/down scaling’ tab. Initial voxel size is optional, as you only need to enter the scaling factor (new voxel size = initial voxel size x scaling factor) and choose the data type (grey-level of label). Image resolution change is done with the file function\_scaling.m (src\Miscellaneous) and is used by other modules as well. Upscaling algorithm is mostly used in the generation module (it is faster to generate a microstructure with a coarse representation, and then upscale it, rather than generate it directly at the fine resolution), while downscaling is mostly used in microstructure characterization (to reduce calculation time for some CPU expensive algorithms and to perform image resolution analysis). Both upscaling and downscaling algorithms are used in the meshing module. Changing image resolution algorithm depends on the image type:

* For a grey-level image, a linear interpolation is used using the MATLB built-in function *imreszie3.* Figure VI-12a illustrates it.

Microstructure\_resized = imresize3(Microstructure,scaling\_factor,'linear')

* For a segmented image, linear interpolation is not recommended as it will generate irrelevant intermediate value if more than two phases exist (cf. Fig. VI-12b). The function imresize3 could be used instead with the option ‘nearest’ (Nearest-neighbor interpolation) to remove this issue. Although it is suboptimal for upscaling segmented image. Instead an in-house custom scaling algorithm is employed, that will refine the interface (cf. Fig. VI-12c):

domain\_size = size(Microstructure);

% Create a binary volume

binary\_volume = zeros(domain\_size);

binary\_volume(Microstructure~=background)=1;

% Upscale or downscale it

allphases=imresize3(binary\_volume,scaling\_factor,'linear');

idx\_void = allphases<=0.5;

allphases(idx\_void)=0;

allphases(allphases>0.5)=-1; % The shape we want to reach, with the phase information

phases\_id = unique(Microstructure);

phases\_id(phases\_id == background)=[];

number\_phase = length(phases\_id); % Minus background

for current\_phase=1:1:number\_phase

% Create a binary volume

binary\_volume = zeros(domain\_size);

binary\_volume(Microstructure==phases\_id(current\_phase))=1;

% Upscale or downscale it

phase\_resized=imresize3(binary\_volume,scaling\_factor,'linear');

idx\_phase = phase\_resized>0.5;

phase\_resized(idx\_phase)=1;

phase\_resized(phase\_resized~=1)=0;

allphases(logical(phase\_resized))=phases\_id(current\_phase);

end

% -1 values are the voxels that refine the interface, but they still miss the phase information

assigned\_resizedvolume = zeros(size(allphases));

assigned\_resizedvolume(allphases>0)=1;

[~,Idx\_distance\_map] = bwdist(assigned\_resizedvolume);

unassigned\_idx = find(allphases==-1);

Idx\_distance\_map(unassigned\_idx);

allphases(unassigned\_idx) = allphases(Idx\_distance\_map(unassigned\_idx));

% And finally for the pore

allphases(idx\_void)=0;

Microstructure\_resized = allphases;

You can move the slider to explore the microstructure volume to compare side by side before and after the image resolution change before validating your change (cf. Fig. VI-12a).

|  |
| --- |
|  |
| *Figure VI-12a. Downscaling (scaling factor=2.5 >1) of a grey-level 3D microstructure. Note that the scaling factor can be any real number. Imaged had initially 201 slices, now 81.* |
|  |
| *Figure VI-12b. Downscaling (scaling factor=2.5 >1) of a segmented 3D microstructure.* |
|  |
| *Figure VI-12c. Upscaling (scaling factor=0.5 <1) of a segmented 3D microstructure.* |

## Quantifying image quality

Evaluating the image quality is an essential step before segmentation, as it will help choosing the adequate segmentation method. You have access to image quality estimators in the menu/Calculate and in the ‘Image quality’ tab.

### Grey level histogram and spatial homogeneity

Grey level histogram is a simple representation of the grey level value distribution within an image. Ideally, phases would be clearly marked with distinct peaks separated by valleys. For such an ideal case phase information is not ambiguous, not convoluted, and segmentation is straightforward. One objective of contrast enhancement and image filtering consists in improving the grey level histogram. Such an example can be found in24.

* Grey level histogram

You can choose to plot the probability density of the grey level using the MATLAB built-in function histogram, either with automatic binning (Calculate/Plot histogram/for the whole volume/histogram(x) – bin auto) or with one bin per unique value (Calculate/Plot histogram/for the whole volume/histogram(x) – on bin per value).

if 'one\_per\_uniquevalue'

nbins = length(unique(Microstructure));

h=histogram(Microstructure,nbins);

elseif 'auto'

h=histogram(Microstructure);

end

set(h,'LineStyle','none','Normalization','probability');

You can also choose to calculate the probability function with in-house functions (Calculate/Plot histogram/for the whole volume/histogram: probability density function). Normalized histogram is first calculated with function\_calculate\_histogram.m, then its probability density function is obtained with Function\_probability\_density.m, and plotted with function\_probability\_distribution\_figure, both files being located in src\Miscellaneous. You can manually edit the function parameters in the code (src\Filtering\_and\_segmentation\Segmentation.mlapp) if you want to filter differently the probability density function.

|  |
| --- |
|  |
| *Figure VI-13a. Probability density function of the grey level plotted with (Left) automatic binning, and (right) 1 bin per unique value. In this example, the two phases (pore and solid) are highly convoluted as no distinct peaks identified them clearly.* |
|  |
| *Figure VI-13b. (Left) Cumulative function, and (right) probability density function calculated with in-house functions. Cumulative function is smoothed with a moving average filter so that its derivative is less noisy.* |

Grey-level calculated on the whole volume may not be representative of the microstructure. User can calculate the grey-level slice per slice (Calculate/Plot histogram/for each slice) to see if peaks and valleys are coherent all along the volume dimensions. If significant deviations are spotted, then contrast correction can be used to trying remedying it. If unsuccessful, global threshold methods are not relevant for the volume, and other approaches are required (e.g., slice-per-slice thresholding).

|  |
| --- |
|  |
| *Figure VI-14a. Grey level histogram calculated slice per slice. No deviation for all axis.* |
|  |
| *Figure VI-14b. Grey level histogram calculated slice per slice for another volume, that exhibits deviation along its 3rd axis: global threshold cannot be used for segmentation!* |

* Grey-level spatial distribution

For non-graded electrode, the grey-level distribution should be spatially homogenous. User can check this by plotting average, extremums, and standard deviation of gray-level along volume dimension (Calculate/Plot grey/as a function of position).

|  |
| --- |
|  |
| *Figure VI-15a. Grey level plotted along volume axis (mean, standard deviation, and extremums). No deviation for all axis.* |
|  |
| *Figure VI-15b. Grey level plotted along volume axis (mean, standard deviation, and extremums) for another volume, that exhibits deviation along its 3rd axis: global threshold cannot be used for segmentation!* |

As well, user can plot the averaged two-dimensional map of the grey level (Calculate/Plot grey/in averaged 2D maps), performed with function\_2Dmap\_3Darray.m in src\Filtering\_and\_segmentation, as:

% Normal to axe 3

greylevel\_normal(3).map = zeros(domain\_size(1),domain\_size(2));

for x=1:1:domain\_size(1)

for y=1:1:domain\_size(2)

line=reshape(Microstructure(x,y,:),[domain\_size(3), 1]);

greylevel\_normal(3).map(x,y)=mean(line);

end

end

|  |
| --- |
|  |
| *Figure VI-16a. Average gray level with uniform brightness distribution* |
|  |
| *Figure VI-16b. Average gray level calculated for another volume that exhibits an in-plane deviation that should be corrected with contrast enhancement before segmentation* |

### Phase separability

Otsu’s algorithm25 is a histogram-based method used to segment images. Method is applied to microstructure in24. The algorithm consists in finding the threshold values that maximize the between-class variance (phases have different grey-level values between them) and minimize the intra-class variance (each phase have uniform grey-level values within). The total variance of the image is the sum of the two: . The phase separability criterion is then defined as and ranges from 0 (worst case: histogram is flat) to 1 (best case: each phase has a unique grey level value). The recommended thresholds are those maximizing . The Otsu’s algorithm is performed with the file Function\_otsu\_algorithm.m in src\Filtering\_and\_segmentation.

For a segmentation task, one is only interested in finding this maximum. For an image quality task, the slope near the maximum is the main interest. Ideally, would decrease sharply from its maximum, indicating the algorithm strongly recommend using this value. On the opposite, if the slope near the maximum is low, it indicates the algorithm almost equally recommends a wide range of threshold without a clear recommendation, which is likely due to phases being highly convoluted (i.e., poor image quality). In such a case, any threshold chosen within this wide maximum region is coherent with the Otsu’s method. Another metric interesting to evaluate the image quality is the evolution of the separability criterion along the volume dimensions. Non-constant values indicate the image quality is not uniform all along the microstructure dimension. A very low value locally suggest it may be adequate to crop this region due to its very poor quality that will bias the analysis. As well, it is interesting plotting the evolution of the recommended threshold slice per slice, based on the separability criterion calculated slice per slice. In case the threshold is varying significantly, a global threshold method is to be avoided in favor for a more local approach. You can calculate the separability criterion in the ‘Image quality’ tab (you need to select the number of phases, as it is the only algorithm parameter). Note that no segmentation is performed.

|  |
| --- |
|  |
| *Figure VI-17. (top left) Separability criterion calculated for the whole volume. While recommended threshold is 117, using a threshold ranging from 110 to 125 seems equally good (~6.3% of the grey level range). (Others) maximum separability criterion and associated threshold plotted slice per slice along volume dimensions.* |

### Image noise

Noise level is currently calculated with the function NoiseLevel.m from Masayuki Tanaka6. It is particularly relevant to quantify locally image noise to identify problematic regions, and to evaluate the impact of image filtering in noise removal. You can calculate image noise with Calculate/Plot noise level/for each slice.

|  |
| --- |
|  |
| *Figure VI-18. Image noise calculated slice per slice.* |

## Contrast enhancement

If the image quality is too low for segmenting the image, contrast enhancement algorithms can be employed to improve it. Few methods are available in the ‘contrast correction’ tab. You can compare side by side the impact of contrast correction moving the slider at the bottom of the tab. MATLAB provides interesting documentation on contrast correction: <https://www.mathworks.com/help/images/contrast-adjustment.html?s_tid=CRUX_lftnav>

### Saturate extreme.

Grey level threshold for which x % of the voxels have higher values is first found, then all these voxels are assigned to this threshold. The lower values are removed similarly. This is particularly relevant to remove the tails of the histogram that may use a very large range of grey level values. This allows to re-center the grey level values.

### Set custom grey level range

Sometimes the data format does not provide enough flexibility for the desired grey level granularity. For instance, you may consider 1024 grey level to be a good compromise between the 256 values offered by 8-bits and the 65536 by 16 bits (even though, if you use 1024 grey level values, you are using at least a 16-bit data format). You can specify your custom range, and then microstructure will be re-scaled accordingly. It is recommended to first saturate the extreme and then set your custom grey level range so that all the grey level range is used more equally.

max\_=max(Microstructure);

min\_=min(Microstructure);

initial\_delta=max\_-min\_;

final\_delta=Custom\_greyscale-1;

Microstructure= round( (((Microstructure\_undo-min\_) ./ initial\_delta) .\* final\_delta)+1 );

|  |  |
| --- | --- |
|  | |
|  | *Figure VI-19. (top) Contrast correction tab illustrated with saturate extreme and (bottom) microstructure after custom range (1024).* |

### Advanced contrast enhancement

In the top right section of the tab, you have access to other contrast correction methods. First select the method with the popup menu ‘Operation’ and then fill the parameter in the table on the far right. You can also choose to apply the contrast correction locally specifying bounds in the mid-table. Note that these functions are applied slice per slice along the third axis.

* **Adjust contrast**. Uses the MATLAB built-in function *imadjust*. J = imadjust(I,[low\_in high\_in],[low\_out high\_out],gamma) maps intensity values in I to new values in J such that values between low\_in and high\_in map to values between low\_out and high\_out, where gamma specifies the shape of the curve describing the relationship between the values in I and J. If you set the last parameter 1, then J = imadjust(I) saturates the bottom 1% and the top 1% of all pixel values.
* **Histogram equalization**. Uses the MATLAB built-in function *histeq*. 'J=histeq(I,n) transforms the grayscale image I, returning in J an grayscale image with n discrete gray levels. A roughly equal number of pixels is mapped to each of the n levels in J, so that the histogram of J is approximately flat. The histogram of J is flatter when n is much smaller than the number of discrete levels in I.
* **Contrast-limited adaptative histogram equalization**. Used the MATLAB built-in function *adapthisteq*. J = adapthisteq(I,…) enhances the contrast of the grayscale image I by transforming the values using contrast-limited adaptive histogram equalization (CLAHE). This algorithm identifies a ‘neighborhood’ around each pixel of an input image. These neighborhoods are referred to as *tiles* (or *contextual regions* as defined by Pizer et al.26 and Zuiderveld27) with the number of tiles along each in-plane axis set by NumTiles A and B in the parameter table. The algorithm applies a contrast transformation to each tile, as opposed to the entire image. The transform used maps each tile’s histogram of pixel values to a new histogram distribution, specified by the user (‘uniform’, ‘rayleigh’, and ‘exponential’, respectively to create a flat, a bell-shaped, or a curved histogram). Because adaptive histogram equalization tends to overamplify contrast in homogeneous regions, the clip limit (or contrast factor) is a useful parameter to lessen the amplification of noise when using this algorithm. The contrast is amplified proportionally to the slope of the grey level cumulative distribution function for each tile, and so by clipping each tile’s histogram before computing the cumulative distribution function, the noise amplification is limited. There is no explicit method to select the most adequate parameters for a given image, thus their determination requires some trial-error experimentations. The table below illustrates the impact of a selection of some parameters for an NMC electrode slice, with for this particular case the clip limit parameter providing the best image enhancement.

Please refer to the MATLAB documentation for more details about the built-in functions mentioned above. It is recommended to work with uint8 or uint16 file format.

|  |
| --- |
| *Table VI-1. Impact of CLAHE algorithm’s parameters on an NMC slice.* |
| |  |  |  | | --- | --- | --- | | **Parameter** *Other parameters with default values* | **Otsu’s separability criterion for a two-phase segmentation (1 is ideal), cf. §VI-6b** | **2D Slice** | | Original volume | 0.6466 |  | | Default parameters | 0.7072 |  | | NumTiles = [16 16] | 0.7078 |  | | ClipLimit = 0.04 | 0.7524 (maximum among the investigated parameter sets) |  | | NBins = 1024 | 0.7501 |  | | Rayleigh, alpha = 0.6 | 0.7007 |  | | Exponential, alpha = 0.1 | 0.7067 |  | |

‘Histogram equalization’ and ‘Contrast-limited adaptative histogram equalization’ are particularly valuable to correct contrast deviation, if any (c.f. §VI-6). Figure VI-20a illustrates through-plane and in-plane contract deviation correction, while Figure VI-20b illustrates ring artifact (defines as a radial variation of the grey level from the image center to its edges) correction.

|  |  |
| --- | --- |
|  | *Figure VI-20c. Example of (Top) through-plane and (bottom) in-plane grey level deviation correction achieved with contrast correction.* |
|  | |
| *Figure VI-20c. A depiction of the impact of contrast enhancement on segmentation. (Left): (a) Raw 2D slice, (b) tentative segmentation on the raw image reveals grey level is not uniform, (c) grey level image after applying CLAHE, and (d) segmentation on the contrast enhanced slice is now possible. (Right) Average grey-level along both in-plane axes, before (blue), and after (red) applying CLAHE. Note that while the ring artifact has been mostly removed by the contrast enhancement algorithm, it has also induced some noise. A subsequent image filtering step is then recommended.* | |

## Image filtering

Similarly with contrast enhancement, MATLAB provides also a detailed documentation about image filtering, available at <https://www.mathworks.com/help/images/linear-filtering.html>. Two popular image filtering algorithms are currently implemented in the GUI, in the ‘filtering’ tab. These algorithms can be CPU expensive, therefore, to avoid wasting time on tuning parameters on the whole volume, you can ask to apply filter on only one slice (‘Preview’ check box). If you run an algorithm slice per slice, the progress is printed within the tab.

### Anisotropic diffusion filter

The anisotropic diffusion filter has been developed by Perona and Malik20. It consists in considering grey level values as concentration or temperature values, for which a diffusion calculation is performed with anisotropic, locally defined, diffusion coefficient. The latter are related to the local gradient according to a user-defined function, with different choice possible (see conduction method popup menu). The main idea being a high diffusion coefficient is applied within uniform region (i.e. within phases) while a low diffusion coefficient is applied in fast-changing regions (i.e. phases’ edge) so that the filtering smooths the image within phases and enhance the contrast at the phases edge. Application of such algorithm on microstructure can be found in24 with illustration. You can apply the filter slice per slice or the whole volume directly. Parameters (number of iteration and gradient threshold) can be estimated or manually entered. The MATLAB built-in function *imdiffusefilt* and *imdiffuseest* are used respectively to calculate the diffusion and to estimate the parameters if asked.

[Gradient\_threshold,number\_iteration] = imdiffuseest(Microstructure,'Connectivity',Connectivity\_,'ConductionMethod',Conduction\_Method);

Microstructure = imdiffusefilt(Microstructure,'Connectivity',Connectivity\_,'ConductionMethod',Conduction\_Method,'GradientThreshold',Gradient\_threshold,'NumberOfIterations',number\_iteration);

### Non-local mean filter

Applies a non-local means-based filter to the grayscale image according to the algorithm introduced by Buades et al.21.

|  |
| --- |
|  |
| *Figure VI-21. Image filtering illustration with Non-local mean filter method. Additional help (tooltips) appears if you hover the mouse over parameter fields.* |

## Segmentation

### Volume segmentation

User must first enter the voxel size, the number of phases and the expected volume fraction if known. Two class of methods are available for the segmentation: global and local (slice per slice) thresholding.

|  |
| --- |
|  |
| *Figure VI-22a. Segmentation tab.* |

#### Global thresholding

Thresholds are set either (i) manually, (ii) to match the expected volume fractions, or (iii) according to Otsu’s algorithm (detailed in §VI-6b)25. Thresholds from choice (ii) and (iii) can be compared clicking on the button ‘Compare Otsu and expected volume fractions’. Errors of both methods are plotted together for compassion. Errors from ‘expected volume fractions’ choice is defined as volume fraction – expected volume fraction, with the reference value being the expected volume fraction. Error from Otsu’s algorithm is defined as the separability criterion – the maximum separability criterion with the reference value being the maximum separability criterion. The graph allows user to evaluate if Otsu’s algorithm is coherent with the expected volume fractions. If you cannot match the expected volume fractions using the associated option, it indicates the grey level range is not enough refined (image is too compressed for instance).

|  |
| --- |
|  |
| *Figure VI-22b. Volume fraction error compared between global thresholding methods (expected volume fraction and Otsu’s algorithm) illustrated with three phases.* |

#### Local thresholding slice per slice

Local threshold determined slice per slice is a relevant choice is the grey level exhibits a deviation along the third axis. If a deviation is spotted along another axis, simply swap axis. Thresholds are set slice per slice either (i) applying Otsu’s algorithm slice per slice or (ii) applying Otsu’s algorithm slice per slice but adding a global threshold correction so that the obtained volume fractions are those expected. To avoid a discontinuity from slice to slice, the function threshold=f(position along third axis) is smoothed using a moving average filter for which the user can choose the range.

|  |
| --- |
|  |
| *Figure VI-22c. Once segmentation has been calculated, the GUI is updated to show side-by-side the grey-level and the segmented image for comparison. Obtained volume fractions are showed in the top table.* |
|  |
| *Figure VI-22d. If the user clicks the ‘Save’ button, volume fractions are calculated slice per slice and displayed. Grey-level and segmented images are also compared side-by-side for the first, in the middle, and last slices for each direction to check segmentation quality is correct not only in the bulk but also at the domain’s edge.* |
|  |
| *Figure VI-22e. If the user clicks the ‘Save’ button and that local thresholding has been chose, then thresholds are also plotted along third axis position. If the choice ‘Local Otsu translated to match expected volume fraction’ has been chosen, then a third line is displaying showing the translated values used for the segmentation.* |

Note: even though the algorithm are n-phases, segmentation of more than two phases is likely to introduce a thin layer artifact at the phase interfaces. See figure 7 of reference28 for illustration. Numerical methods to remove such artifact exist28,29 and may be implemented in the future.

### Microstructure properties sensitivity with thresholding

An uncertainty may exist for the threshold choice, as several values may provide visually very similar segmentation. The question arises then on the error propagation from the segmentation error to the microstructure property error. Alternatively, a user may be very confident on the choice of his threshold but still want to know how much a slight change from its segmentation will impact the microstructure properties. A small variation would strengthen the microstructure characterization results, while a significant variation will decrease the level of confidence attributed to the results. In the ‘Segmentation (sensitivity)’ tab, the user can set up such a segmentation sensitivity analysis for a two phase materials (pore and solid) on four microstructure parameters typically used in macroscale modeling: the porosity, the particle diameter (using a simple spherical assumption), the specific surface area, and the tortuosity factor. To avoid calculating properties on obviously incorrect segmented volumes, the user can specify the lower and upper bound of the porosity. To reduce calculation times, the user can specify the maximum number of thresholds considered between the two bounds. Then, the user can choose if he wants to calculate the four parameters or only some of them. Lastly, the user enters the voxel size and click on the ‘Calculate parameter sensitivity with threshold’. For simplicity sake, a simple global threshold swap is performed. Progress is indicated within the tab. Results are displayed as each parameter is investigated. Because a grey-level do not have the same signification for every microstructure (a unit variation is much more important for a 8-bits than for a 16-bits volume), grey levels axis are represented both with their absolute value but also as a percentage of their range as:

unique\_values = unique(Microstructure);

range\_greyscale = max(unique\_values)-min(unique\_values)+1;

range\_greylevel=100\*unique\_values/range\_greyscale;

|  |
| --- |
|  |
| *Figure VI-23a. Microstructure properties sensitivity with global threshold tab.* |
|  |
| *Figure VI-23b. Volume fractions are by default calculated for the whole grey level space. Grey dashed line represents the value for the expected porosity indicated by the user.* |
|  |
| *Figure VI-23c. Microstructure property sensitivity with global threshold illustrated for pore tortuosity. (Left) calculated value, and (right) error.* |
|  |
| Figure VI-23d. (Left) Relative error, (center) relative error change per grey-level change and (Right) relative error change per percent of the grey-level range |

### Phase reassignment

Once segmentation is completed, you can manually reorder the phases in the ‘Phase re-assignment’ tab.

# Microstructure characterization and homogenization

## Definition, unicity, limitations, and pseudo-parameters

Microstructure characterization is applied on segmented volumes, for which each voxel identifies a phase. Microstructure characterization can be considered as a dimension reduction calculation. Microstructure volume is, from the numerical analysis point of view, a very large dimensional space: each element of volume (voxel) has a value that identifies what phase exists in this location. While this description is very accurate, at the extent of the image resolution, it is however impractical for describing in a quantitative and concise way the features or properties of a microstructure. These properties can be used for discussion and comparison (“this microstructure has a higher [property name] compared with this one”) and modeling (“this [property name] is a parameter model”). Therefore, the properties to quantify from the microstructure depend on the application. For instance, in the battery field, porosity , specific surface area , particle mean equivalent diameter , and tortuosity factor along electrode thickness (definitions are provided in the section §VII-6) are the four microstructure parameters typically calculated as they are used in electrochemistry battery (macroscale) models30,31, cf. Fig. VII-1.

|  |
| --- |
|  |
| *Figure VII-1. Example of a microstructure characterization for electrode battery modeling. (Left) microstructure of a positive NMC (Nickel Manganese Cobalt oxide) electrode material is represented with a 3D array with a very large number of voxels. (Right) the microstructure is abstracted with a limited number of scalars, each with a physical or geometrical definition relevant for the chosen application (electrode battery modeling).* |

Models are, by definition, a simplification of reality. In this frame, the microstructure volume is simplified with a limited number of properties, and microstructure characterization aim is to calculate them. This approach however is restrictive: it is not because a property is not used as a parameter for a given model that it is not important for the application. For instance, in battery electrode modeling, particles are assumed to be spherical in order to derive the model equations30,31, while (i) this is obviously not true32 and (ii) several authors suggest particle morphology impact electrode performances33,34. In this case, additional microstructure parameters worth be quantifying could be particle sphericity and elongation. Another example is that standard models assume a uniform particle size distribution, while (i) electrode microstructures have more complex size distributions32 and (ii) such distributions have an impact of the electrochemical response when modeled35–37. Restricting microstructure characterization to the sole parameters used in models may then induce the bias that all the relevant microstructure parameters are considered. It is then recommended not only to quantify the microstructure properties explicitly used as model parameters, but also additional microstructure properties that we expect impact system response too. Being able to determine these additional parameters provide an incentive for modelers to incorporate them in their model, eventually producing enhanced predictions. Furthermore, being able to finer characterize microstructures allows a more in-depth discussion, as more metrics can be used to discriminate microstructures.

It is unlikely a bijection exists between a microstructure volume and a given property set due to the huge discrepancy between their cardinality (the number of elements they contain): ~103-9 for a microstructure volume and ~101 for a microstructure property set. Therefore, for one or several set of microstructure properties values, multiple microstructure volumes exist as illustrated in figure VII-2. Say otherwise, values of a given set of microstructure properties do not identify uniquely a microstructure: microstructure characterization induces a loss of information that prevents recreating identically the microstructure used to calculate the properties. As the property set cardinality is increasing, the microstructure design space is more constrained and thus the number of possible microstructure volume that matches these properties is decreasing.

|  |
| --- |
|  |
| *Figure VII-2. Bijection does not exist between a microstructure mi (or a group of microstructure M) and a property set pj (or a group of property set P). Property set are application specific. In this example is relevant for surface-type reaction (Specific surface area ), while is relevant for lineic-type reaction (triple phase boundary density length ).* |

Assuming the microstructure volume available for the microstructure characterization is a *valid* representation of the material, and that algorithms used to calculate the properties used as model parameters are *adequate*, then the properties calculated are correct. A *valid representation* is a volume that satisfies various conditions: (i) investigated volume is statistically representative of the whole material volume used in the application, (ii) image resolution is high enough to capture all the relevant geometric features that can impact the system response, and (iii) segmentation is good enough to provide a close match with the actual microstructure. In practical, these three conditions are never perfectly achieved. Although they can be evaluated: (i) and (ii) are discussed in detail in §VII-2, while (iii) can be verified both globally (a correct segmentation is supposed to provide the expected phase volume fractions) and locally through visual comparison between the grey-level and the segmented images. Unfortunately, in some cases, due to the nature of the material phases and of the specifications of the experimental setup, some phases may be not visible which induces some uncertainty in the characterization results16. An *adequate algorithm* is a method for which (i) assumptions, if any, are relevant for the investigated microstructure (e.g. an algorithm that uses a particle spherical assumption is relevant only if the microstructure has indeed near-spherical particles) and (ii) parameters, if any, are known. Condition (i) can be checked. For instance, if the algorithm uses a spherical assumption, the particle sphericity can be calculated using another algorithm, or estimated through visual inspection (as done in32, figure 22). As well, result sensitivity with assumption correctness can be estimated comparing characterization results obtained with numerically generated microstructures that differently satisfy the given assumption (e.g., generating ellipsoids with different sphericity and plotting algorithm result as function of the known sphericity). Condition (ii) is too algorithm-specific to have a generic discussion about it. Microstructure characterization is therefore limited by the difficulty to have a *valid representation* and *adequate algorithms*. Quality microstructure characterization work should pay special attention on evaluating both.

When microstructure properties are used as model parameters, and that model predictions are thereafter compared with experimental results, difference discussion should include the different source of errors in the analysis:

With ‘model assumption error’ being the cumulated error arising from the necessary simplifications of the actual system in order to being able to formulate model equations. These include geometry simplifications (e.g., particles are spherical), mathematical simplifications (e.g., non-linear equations are linearized), physic simplifications (e.g., mechanic is not considered) etc. Therefore, difference between measured and predicted value is equal to:

Experimental error can be estimated reading specifications of the experimental tools or measured (e.g. noise to signal ratio). Model parameter error can be also estimated, differently for each parameter, and model can be run between lower and upper bounds representing the parameter confidence interval. On the contrary, evaluating model assumption error is more delicate, although not impossible. For instance, predictions calculated with models of different level of simplification can be compared to discriminate the precision cost of a given model simplification. The point of this paragraph is that even if you are confident with the model parameters, a discrepancy between the experimental and the model result is still possible. It is then common to fit one or more parameters to obtain a good agreement. If the fit implies that one or several microstructure parameters are assigned to values significantly outside of their respective interval of confidence, it is overfitting. This is a hint that the model assumptions are too strong, and/or you do not have a valid representation and adequate algorithms. The definition assigned to these overfitted model parameters do not match anymore with the definition of their equivalent microstructure properties. Such parameters are then called pseudo-parameters to reflect this mismatch. For instance, if you estimate with high confidence the tortuosity factor to lie between 2 and 2.5, and that your model requires a value of 3.5 to match experimental data, then the tortuosity factor used in the model is a pseudo-tortuosity factor. The out of bound pseudo-parameter values allow accommodate the model assumption.

### Microstructure characterization and microstructure homogenization

Microstructure homogenization is a branch of microstructure characterization (as it still consists in extracting microstructure parameters from the 3D volume). The specificity of microstructure homogenization lies in how the microstructure is represented after its characterization, or simplification (cf. Fig. VII-3).

* Standard microstructure characterization, such as particle size quantification, considers the domain after simplification still as a multi-phase material, as there is no notion of particle size or specific surface area for a one-phase material. The difference with the initial 3D volume sits on the property level of complexity. In the figure below, the microstructure exhibits a wide size distribution, while its representation used for modeling only kept the mean diameter, thus neglecting the size distribution. Some models consider different particle size, so the level of simplification of the complex microstructure can vary depending on the models considered.
* Microstructure homogenization, such as effective diffusion coefficient quantification, considers the domain after simplification as a homogenous domain, i.e. a one-phase material. The idea being both the complex multi-phase microstructure and the one-phase homogenized domain responds identically at the macroscale for a given loading, e.g., the same flux for the same applied concentration or temperature gradient. Microstructure homogenization is used to determine the effective (i.e. macroscopic) material coefficient, such as diffusion coefficient2,38 or stiffness tensor39 (both that can be defined on a one-phase material) of an heterogenous domain, for which the coefficient value is known for the 100% dense phase (noted .

|  |
| --- |
|  |
| *Figure VII-3. Examples of microstructure characterization for (top) particle size and (bottom) effective diffusion coefficient. Model equations from*31 *have been used.* |

## About voxel size dependence and representative volume element analysis

### Image resolution and fractal issue

Properties exhibit different voxel size dependence, depending on they are volume properties (e.g. volume fraction, particle size), surface properties (e.g. specific surface area) or lineic properties (e.g., triple phase boundary length). We consider homogenized properties, such as effective diffusion coefficient or effective stiffness tensor to be volume properties (rule of mixture being the simplest method to determine them) even through it is an oversimplification. Several authors have investigated properties sensitivity with image resolution16,32,38–40.

Except for very coarse image resolution that would degrade the material network, voxel size impacts only mostly the interface description. Therefore volume-based properties are converging with image resolution16,32, and it is justifiable to extrapolate their value to an infinite image resolution to provide a better prediction. To do this, volume is downscaled iteratively in order to provide a curve property as a function of voxel size. The algorithm used to perform downscaling/upscaling is described in §VI-5. Note that the dependence with voxel size of a given property may be method-specific16. The explanation of why a property is increasing or decreasing with voxel size depends then on (i) the particular microstructure investigated, (ii) the property, (iii) the algorithm used to downscale the microstructure, and (iv) the method used to calculate the property.

Unlike volume properties, surface and linear properties are not converging with image resolution as they exhibit a fractal behavior40. Such issue is briefly discussed by Usseglio et al32 for battery microstructure, while the fractal issue has been thoroughly studied for solid oxide fuel cell anodes by Bertei et al.40 and is related to surface roughness. As more interface details are visible at lower voxel size, surface and lengths are expecting to diverge with image resolution. Therefore, extrapolation is not relevant. Besides, an intrinsic issue lies in the fractal property’s dimensionality: lineic fractals have a dimension between 1 and 2, while surface fractals have a fractal dimension between 2 and 3 (non-fractals have an integer dimension). Macroscale battery models typically use a morphology assumption, such as particles are spherical. Although, they rely on another, implicit, assumption that there is no surface roughness which ensure lineic and surface have integer dimensions. Surface and lineic properties absolute values obtained through microstructure characterization are not relevant for current macroscale models: only their dimension is converging, while their value is diverging. However, it is still worth it to calculate surface and lineic properties between different microstructures, at the condition they share the same voxel size, for comparison purpose. Calculating the fractal dimension is also valuable as it quantifies microstructure complexity as a ratio of the change in detail to the change in scale. Note that numerically generated microstructures are not adequate for such image resolution/fractal analysis study as surface is only refined but no new surface details are generated when generation is performed with smaller voxel size.

You can perform voxel size dependence analysis in the characterization module for each microstructure property. To do this, check the ‘Perform voxel size dependence analysis’ checkbox and choose the voxel size multiplier.

|  |  |
| --- | --- |
|  | *Figure VII-4. Graphic user interface for voxel size dependence analysis. In this example, property will be calculated with the original voxel of size µm3, but also with µm3, µm3, µm3, and µm3.* |

### The representativity issue and the concept of representative volume element

#### Definition and methodology

Microstructure scale analysis are, by definition, limited to investigate only a fraction of the material volume used for the application. For electrode batteries, it corresponds to a volume < 1 mm3, while electrode size is order of magnitude larger. Only submillimeter heterogeneities may be catch by microstructure scale analysis. While obvious, this statement is important to keep in mind as mm to cm scale local variations and defects may exist in the bulk of the electrode material, while material edge may also differ from the bulk, depending on the manufacturing process and on its quality control. Microstructure analysis can then only evaluate heterogeneities contain in the field of view and may not be representative of the whole material. Ideally, to evaluate if the measure if impacted by mesoscale heterogeneity, one would perform imaging on different sample locations.

Representative volume analysis (RVA), as defined in this toolbox, tries to answer this question: *“For a given microstructure property and a given subvolume aspect ratio, what is the minimum subvolume size that provides a relative standard deviation below a given threshold?”*. The method consists in cutting the microstructure volume into independent (i.e., non-overlapping) subvolumes of the same size and aspect ratio, and to calculate microstructure properties for each of them. The relative standard deviation is then calculated considering all the results. The process is repeated with varying subvolume size to produce the curve relative standard deviation as a function of subvolume size. When the curve crosses the relative standard deviation user-defined threshold, then the representative volume element size is found. The method is illustrated in figure VII-5. Because of the finite volume of the investigated volume, as the subvolume size is increasing, their number is decreasing. Crossing the threshold with a low number of subvolumes is less relevant from a statistical point of view, implying the confidence of the calculated RVE size is low and that a larger field of view is required. Not crossing the threshold indicates the field of view is too small to provide a RVE. Although it does not mean necessarily that the whole volume is not representative: RVA analysis can only tell if a subvolume is representative of the whole volume. This last point is important to set up the experimental imaging if determining the RVE is required. Considering a material with a particle size of ~10 µm and assuming that RVE lengths should be ~15 particle diameter (this rule of thumb is highly debatable as seen in41, but for the sake of the demonstration we will use it), then the expected RVE size is ~ µm3. If your criterion to determine the RVE is a standard deviation of 5% obtained with *at least 9 subvolumes*, then you should consider an imaging setup that would provide a field of view of ~ µm3. The relative standard deviation threshold and the minimum number of subvolumes are set by default to 5% and 4, respectively, in the module and can be modified (cf. Fig. VII-7). RVE size relation with particle size is discussed in41.

|  |
| --- |
|  |
| *Figure VII-5. Representative volume analysis method. Subvolume aspect can vary.* |

#### RVE aspect ratio

Representative volume element (RVE) size is property-dependent41,42: each property has its own RVE. Correlated (non-independent) properties share the same RVE41. Therefore, the RVE size of a microstructure is the maximum RVE size among all the properties relevant for the application. RVE size is often expressed as µm3, implicitly neglecting the volume aspect ratio. Instead RVE size should be expressed as µm3, with *a*, *b*, and *c* the dimensions of the RVE volume. Percolation-related properties, such as connectivity and tortuosity factor, are strongly dependent of the volume aspect ratio. This can be illustrated considering the extreme case of a match-like volume µm3 with y being the voxel length (i.e., a line with a section equal to the voxel section, ). Such volume has no connectivity and thus an infinite tortuosity factor. The choice of the subvolume aspect ratio then impacts not only the result of each subvolume, but also the RVE size. The toolbox offers three choice of RVE aspect ratio (cf. Fig. VII-6): (A) keeping the initial aspect ratio of the whole volume, (B) setting directly an aspect ratio for the subvolumes and (C) setting one constant dimension. These three cases are illustrated in Figure VII-7. The question is then what aspect ratio is relevant? The whole volume aspect ratio is constrained by the imaging technique and has no physical meaning. Instead, the choice of the aspect ratio for representative volume analysis is guided by application/material. For instance, battery electrode materials are very thin in one dimension (from current collector to separator). This thickness is a characteristic of the battery as it will drive the concentration gradient along the electrode thickness, therefore modelers are interested in the ionic transport property from current collector to separator. Microstructure characterization will calculate this parameter (cf. §VII-9b), then determine the representative section area µm2 considering subvolumes of size , i.e., using the Case C from the module. Note that you can stack several RVA in the module. The file Function\_get\_Subdomains.m in src \Microstructure\_characterization determines subdomains bounds depending of the selected case (A-E).

The mean value calculated from the subvolumes is not necessarily equal to the value obtained from the whole volume. Equality is achieved only for volume averaged properties that do not suffer from any edge effects for which a simple rule of mixture approach is adequate, for instance volume fractions. Effective diffusion coefficients on the other hand can be averaged only if subvolumes are arranged in parallel, and if each of them are large enough not to be affected significantly by edge effect. Example can be found in41.

|  |
| --- |
|  |
| *Figure VII-6. Subvolumes aspect ratio choice for representative volume analysis* |

|  |
| --- |
|  |
| *Figure VII-7. (Top) Case A: subvolumes and whole volume share identical aspect ratio. (Middle) Case B: subvolumes with custom aspect ratio 1:1.5:1.5. The largest subvolume that verifies this aspect ratio is first determined, and then cut into subvolumes. Not all the volume will be investigated. (Bottom) Case C: one direction dimension is fixed. (Right) the blue lines represent the subvolumes edges, for the volume division circled in red.* |

#### RVE sensitivity with field of view

RVA result must always be considered with caution, especially if the RVE size has been found with a relatively low number of subvolumes. Being able to determine a RVE size can induced a false confidence in the results: RVA performed on the same material but with different field of view can result in different RVE sizes and properties results as illustrated in Figure VII-8 and 9. RVE size is expected to increase with the field of view, as larger field of views are more likely to include more different heterogeneities, until converging. In order to build more confidence in the RVE size determination, and thus in the result relevance, RVA can be performed on different subsets of the initial field of view, to verify if RVE size is stable with the field of view. An example of such analysis is shown in figure VII-9. Porosity RVE sizes of an NMC electrode volume from the NREL open-source library (NMC-1-CAL) have been calculated considering the whole volume, and several iterations of the same volume but cropped. As expected, the larger the volume for which RVE analysis is performed, the larger the RVE size is found (although, it should converge eventually).

|  |
| --- |
|  |
| *Figure VII-8. (Left) Microstructure analysis will conclude the material has a bi-modal particle size distribution and a small RVE size indicating a high uniformity (~random spatial distribution). (Right) Analysis performed on the same material but with an initial larger field of view will indicate a tri-modal particle size distribution, the presence of crack and will likely conclude the field of view is too small to determine a RVE.* |

|  |
| --- |
|  |
| *Figure VII-9. Porosity RVE size calculated on nested volumes (smaller volumes are included in the larger volumes). Figure plotted with the correlation module. Increasing trend is noticeable.* |

#### Alternative approach (not recommended)

RVA is not uniquely defined in the literature. For the sake of completeness, two other approaches are included in the module, Case D and E (cf. Fig. VII-5 and 9). Case D consists in growing a unique subvolume from the field of view centroid. Case E consists in growing a unique subvolume modifying only one dimension, while the two others are fixed. The issue with these two approaches lies in the fact that they do not answer the representativity question as each subvolume has different size. Several options are available to control the volume increment at each new step, and it is recommended to use a percentage of the current subvolume so that the quantity dV/V0 = (V1-V0)/V0 (i.e., volume relative increment) is constant, with V1 the new subvolume and V0 the current subvolume. Property result is then plotted as function of the unique subvolume size. RVE could be determined setting a threshold on the slope. A constant subvolume increment dV implies that the quantity dV/V0 tends to 0 as V0 is increasing, which will *systematically* show a convergence of the property value with the subvolume size that can wrongly be interpreted as the signature of a RVE, as the slope will invariably tend to 0.

|  |
| --- |
|  |
| *Figure VII-10. (Top) Case D: unique subvolume is growing from the field of view center. (Bottom) Case E: unique subvolume is growing from one field of view extremity. Arrows indicates the different choices offered by the popup menu.* |

The difficulty to evaluate with confidence the RVE size illustrates well that while it is relatively easy to calculate a microstructure property (one calculation performed on the whole field of view is enough) it is much more complicated and time consuming to estimate its error (multiple calculations are required). Although that is the price to enable quality analysis you can reasonably trust. Note that in literature, the term RVE is sometimes abusively used, confused with a control volume.

Depending on the algorithm used for their generation, numerically generated microstructures are not well suited for representative volume element analysis. For instance, the stochastic algorithm presented in §V refreshes probabilities at each new particle generation to better match target values, thus artificially enforcing a high uniformity.

## Module purpose and strength

The microstructure characterization module is the main one of the microstructure analysis toolbox. Toolbox development initially started with only this module and has been progressively extended towards other tasks (modules) subsequently. While other modules have limited ambitions (e.g., the filtering and segmentation module is far from exhaustive), this one aims to establish a new standard in microstructure characterization eventually. While only few microstructure characterization methods from the literature are implemented, the real added value of the module comes from its accuracy, systematic, and in-depth analysis, its user-friendliness, and its modular structure. These points are presented more in details below.

* Accuracy analysis.

Calculating a property value is only half the story. Saying that “this microstructure has a value of x for this property” is at the best incomplete and at the worst wrong. How could you be sure about the value you are giving if you do not perform a representative volume element (RVE) and a voxel size dependence analysis? Furthermore, are you certain the way you have performed RVE analysis is relevant, as different non-equivalent approaches exist (cf. §VII-2)? The method used to calculate a given property may suffer from edge effect effectively biasing the result (e.g., §VII-5b,c,f). In such case, you should provide an estimation of the edge effect to assess if its impact is marginal and can be safely ignored or if it should raise a red flag on the result. Furthermore, the property you are trying to calculate may be obtainable through different methods (cf. §VII-5f). These methods are not equivalent most of the time as they rely on different assumptions, that may be correct or incorrect depending on each microstructure. As in many other fields, it is relatively easy to provide a ‘result’ while estimating the level of confidence (i.e., error) of its value is much harder. This module, through its automated RVE and voxel size analysis, and thanks to its relatively large choice of algorithm to calculate a given property will help you evaluating the field of view induced error, image resolution induced error, and method related error.

* Systematic analysis.

The in-depth analysis described above can be applied to all the calculated parameters if the user chooses to do. Each parameter has their own voxel size dependence profile16,32 (sometimes algorithms/methods that calculate the same property can even have a different voxel size dependence profile16) and representative volume element size41,42. Therefore, you should not rely on performing an RVE and voxel size dependence analysis on only one property, and then assume it determines the RVE size and voxel size for the investigated microstructure (i.e., extrapolating for all microstructure properties). Performing a manual RVE analysis is very time-consuming as it implies calculating the same property hundreds of times. Fortunately, the module automated it this task for you. Typically, such systematic analysis is recommended when you are dealing with a new type of microstructure and/or new algorithms you are not familiar with. In addition to reinforce confidence in your results, such systematic analysis allows you to find interesting findings, such as fractal behavior for a parameter with voxel size40 and systematic hierarchy between RVE size of different properties41.

* In-depth analysis.

Sometimes, providing a mean value with some upper and lower bounds for the confidence interval is not enough to adequately describe the complex microstructure. You may deal with a graded microstructure, for which the average result value should be complemented with a graded analysis, i.e. plotting the property value as a function of position. Some properties are better represented through a distribution function (e.g. particle size) or a standard deviation. Other properties can be derived from the initial calculation, for instance a particle identification algorithm could provide much more information than only the particle size (particle sphericity and elongation). The module automatically performs graded analysis and distribution analysis for relevant properties and calculate associated properties when adequate so that you can extract the most information from a given microstructure.

* User-friendliness.

Sometimes overlooked in open-source software development, user-friendliness is however a key aspect to hope reaching many users. Excellent software with poor interface is a recipe for a waste opportunity. The GUI should make the use of the toolbox easy. If something is not clear, please contact the author as one objective of the toolbox is to be as user-friendly as possible to streamline microstructure-related work.

* Modular structure.

The modular structure is valuable from the developer point of view as it facilitates code maintenance and future developments. Since the toolbox is open source, users also benefits from it, as they can adapt the toolbox to their needs with minimum coding, while having access to all the features of the module, such as RVE analysis (cf. §VII-7). Besides, it greatly helps code reviewing form third parties. Indeed, scientific algorithms length is kept short as all side tasks are deported in other files. The modularity structure is more detailed in §VII-6.

## How to use

### With the graphic user interface (standard use)

#### Import volumes

You can import a new volume in the first tab. The tab provides various information and allow you to setup some parameters (follow instructions):

* On the top left is displayed the name of the file loaded. A number is assigned (‘Volume numero: X) to the current volume. The number is incremented with each new loaded volume.
* On the middle left is a slice view of the current loaded microstructure. You can change the view axis with the popup menu and explore slices with the slider.
* On the top right, you can enter the initial voxel size in nanometers, and the new voxel size in nanometers. If different, upscaling or downscaling will be applied later (note that this is not used for voxel size dependence analysis). Just below, you can choose your region of interest. If you need to perform a more complex ROI selection (e.g., rotation) you should use first the filtering/segmentation module. You can also write the direction names. These names will used to label figures and results adequatly. Below is a non-interactive text section that summarizes the size of the loaded volume and of the volume that will be actually investigated.
* On the middle right, you can enter phase information (number of phases is not limited). Volume fraction is showed for each phase. You can change the color (RGB) that will modify the representation on the left, but most importantly will be used for every figure generated by the module. You can also assign a name to the phases, that will be used also to label results. Lastly, you can assign a code to the phase. You can assign different phases with the same ‘assign code’ value. In such case, these phases will be merged. The newly defined phase will use the color of the first merged phase and its name will be a concatenation of all the merged phases, separated by ‘and’ (e.g., ‘Pore’, ‘Additives’ will give ‘Pore and Additives’).
* On the bottom right, you can enter optional information about the volume. Table will be saved in an excel file and is used to keep track of the different samples/calculations. Just below, you can select the save folder (until you choose it you cannot validate your options) and write the result folder for this volume (save folder/result folder). By default, the result folder is filename\_Vol\_Xum\_Voxel\_Ynm, with X and Y, respectively, the equivalent cubic domain size and Y the new voxel size.

Once you have entered all the options, you can click on the button ‘Once steps 1-5 done, click to save your choices’ or on ‘Reset selected options and current volume’ to cancel your choice and reset the tab. The green or red text above indicates if the user entered incorrect information (e.g., text instead of number, negative voxel size, out of bound ROI, etc.). You can repeat the import process (the ‘Volume numero: X’ will be incremented) in case you want to perform a batch analysis, for which volumes will be characterized sequentially.

|  |
| --- |
|  |
| *Figure VII-11. Import tab.* |

The second tab shows all the volume you have loaded in the first tab. You can reorganize them (modifying the order of calculation value) or remove them (setting order of calculation equal to 0). Once you have done your modifications, if any, you must click on the button at the bottom to update the order of calculation.

#### Choose microstructure properties to calculate

The following tabs allow you to setup microstructure properties. There is one tab per method, meaning that microstructure properties for which several methods exist for their calculation (e.g. particle size) have several tabs. Choices are shared for all microstructure you have loaded. Properties are calculated for every phase.

The top half is common for each tab:

* The checkbox at the top give you the choice to calculate or not the given microstructure property with this method
* On the left, you can set up (or not) voxel size dependence analysis. See §VII-2a.
* On the right, you can set up (or not) representative volume element analysis. See §VII-2b.

The bottom half of the tab is specific for each method and enables the user to choose its parameters. Parameters are explained in §VII-5 where microstructure properties are introduced.

|  |
| --- |
|  |
| *Figure VII-12. A method tab. Top half is common with others method tabs, while bottom half is specific for each method.* |

#### Save options, and run calculations

In the ‘Display/save options’ tab, you can select various saving and format options for figures and results. By default, ‘Close figure once displayed and/or saved’ is checked to avoid saturating the user window with dozens, potentially hundreds of open figures. Once you have setup all your parameters, you can go to the ‘Run ALL calculations’ to characterize sequentially all the imported volumes.

### Use algorithms as standalone functions from the command window

Alternatively, you can run algorithms as standalones if desired. Open function\_microstructure\_characterization\_segmentedvolume.m (src/ Microstructure\_characterization) and go to the section CALCULATIONS to see a list of all the functions used to calculate various microstructure parameters, e.g.:

%% PARTICLE SIZE (Continuum Particle-size distribution C-PSD)

if PROPERTY.particlesize\_cpsd.todo

Function\_particle\_size\_CPSD(Phase\_microstructure, PROPERTY, OPTIONS, INFO); % Call function

end

If you open one of them or read their help, you will see that two syntaxes are available:

function [] = Function\_particle\_size\_CPSD(Phase\_microstructure, PROPERTY, OPTIONS, INFO)

%Calculate Particle size with a spherical assumption (C-PSD)

% Function\_particle\_size\_CPSD(array, PROPERTY, OPTIONS, INFO) - when use with the toolbox

% or

% Function\_particle\_size\_CPSD(array, voxelsize) - when use as a standalone function

The first syntax, that uses structure variables PROPERTY, OPTIONS, and INFO is called when the GUI is used. The second syntax can be called directly from the command window from scratch. For example:

M=function\_load\_tif('C:\Users\fussegli\Desktop\nmc-1-cal-segmented.tif');

Function\_particle\_size\_CPSD(M, 398); % Voxel size of 398 nm

Results are printed in the MATLAB command window and figure are generated, similarly when the function is used through the GUI. However, representative volume element analysis and voxel size dependence analysis are not performed when functions are used as standalone. Other calculations (e.g., distribution functions, graded analysis, etc.) are still performed although. Results are saved in a folder located in the desktop named ‘Volume characterization\_\*’ with \* the current date, and organized in subfolders as done when function is called with the GUI.

### Use raw algorithms without graphical results

Lastly, you can choose to run the method raw algorithm directly. This usage is mostly relevant for debugging/understanding. In the src/Microstructure\_characterization folder, filter files that end with algorithm (i.e. \*algorithm.m) to find them. For instance, Function\_particle\_size\_CPSD\_Algorithm.m

function [] = Function\_particle\_size\_CPSD(Phase\_microstructure, PROPERTY, OPTIONS, INFO)

[...]

for current\_phase=1:1:number\_phase % Loop over all phases

code\_tmp = INFO.phase(current\_phase).code;

binary\_phase=zeros(Domain\_size(1),Domain\_size(2),Domain\_size(3)); % Initialization

binary\_phase(Phase\_microstructure == code\_tmp) = 1;

[Particle\_size] = Function\_particle\_size\_CPSD\_Algorithm(binary\_phase); % Call algorithm

You can run it from the command window as:

M=function\_load\_tif('C:\Users\fussegli\Desktop\nmc-1-cal-segmented.tif');

solid\_phase\_id = 1;

binary\_phase = zeros(size(M));

binary\_phase(M==solid\_phase\_id)=1;

[Particle\_size] = Function\_particle\_size\_CPSD\_Algorithm(binary\_phase);

The inputs/outputs can be different for other algorithm files. Although they typically all require a binary image as input (i.e., voxel=1 for investigated phase, otherwise 0) and use the least number of parameter possible to keep the file short and thus readable. In the example above, even though particle size is calculated, the voxel size is not provided as the algorithm do not require it (voxel size=1). Result are scaled (i.e., dimensionalized) after.

### Link with other modules

#### Link with Microstructure and results visualization module

Pixel-wise defined microstructure properties, such as particle size, or cluster label, are saved in a structure named results\_visualization, which is saved in the subfolder save folder/result folder /Visualization. The visualization module will automatically find all these structures (cf. §VIII-3). The user can easily add new 3D array to be stored for future visualization (e.g. particle radius, or volume in addition to particle diameter) as explained in §VII-7c)

function [] = Function\_particle\_size\_CPSD(Phase\_microstructure, PROPERTY, OPTIONS, INFO)

[…]

for current\_phase=1:1:number\_phase % Loop over all phases

results\_visualization(current\_phase).Particle\_diameter\_CPSD = Particle\_size;

#### Link with Properties correlation module

Dozens of microstructures, each with dozens of microstructure parameters can form a large set of parameters with hundreds of values, that will be tedious to manually copy one be one in a single file for analysis. Some results are saved in a structure named results\_correlation, which is saved in the subfolder save folder/result folder/Correlation. By default, not only the property main result is saved (e.g., mean particle size) but also side results (e.g., particle side standard deviation, RVE size of particle size, etc.) allowing interesting correlation (e.g., RVE size as function of property heterogeneity, etc.). The correlation module will automatically find all these structures (cf. §IX). The user can easily add new result to be stored for future correlation as explained in §VII-7e).

function [] = Function\_particle\_size\_CPSD(Phase\_microstructure, PROPERTY, OPTIONS, INFO)

[…]

for current\_phase=1:1:number\_phase % Loop over all phases

results\_correlation(current\_phase).Particle\_diameter\_mean\_CPSD = PSD\_results(current\_phase,2);

### Results organization

Because numerous files are created for each method, a proper file management is required to keep things sorted and readable. Each result is usually saved in three formats when relevant: one excel .xlsx file, one MATLAB figure .fig file if reformatting if needed, and one .png file.

* **Save folder/result folder/** contains the excel file ‘General\_information.xls’ that stores as indicated general information about the investigated volume: input/output locations, phase name and code, domain size and directions name, voxel size, module version number, user information, and start date. In addition, it contains some meta information about the volume (material name, source, etc., that correspond to the information entered in the tab import). The excel file ‘Volume\_setup.xls’ stores parameters used to crop, up/down scale the original volume and to re-assign phases. Both files are very useful when you have to re-open old results you may have forgotten the details.
* **Save folder/result folder/Visualization** and **save folder/result folder/Correlation** contain structure files used, respectively by the visualization and the correlation module.
* **Save folder/result folder/Volume** contains both the imported volume as it is, but also the volume that is investigated (i.e., after cropping, image resolution up/down scale, phase re-assignment). Volumes are saved in a tif format with an unsigned integer 8bits data type that used very little disk space. It means the input data are saved with the outputs to keep track of a calculation and being able to reproduce it easily.
* **Save folder/result folder/Summary** contains high-level information that summarizes essential results. Basic characterizations results are saved per phase in figures ‘Results\_of\_phasename’, and in a table (Table\_summary\_results.xls). Several .mat files, one per method (Results\_propertyname\_methodname.mat), contain more detailed result. Time.xls stored the total wall clock and CPU time used for the characterization, not discriminating tasks.

|  |
| --- |
|  |
| *Figure VII-13. Example of a summary figure for a phase.* |

* **Save folder/result folder/Propertyname\_methodname** contains results specific for this microstructure property, calculated with this particular method. See §VII-5 for information specific for each method. Representative volume element analyses are saved in a subfolder (one per case).

## Microstructure properties

The module has been built with battery electrode material characterization in mind, and therefore is focusing on quantifying microstructure properties used in battery modeling, namely porosity, connectivity, tortuosity factor, specific surface and interface area, and particle size. Additional properties, interesting to evaluate image quality (level of detail) and refine description of the microstructure (particle shape, domain topology) can also be calculated. Results are illustrated with microstructures from the NREL open-source microstructure library13,or numerically generated with the microstructure generation module of this toolbox.

### Volume fraction

Results are saved in **Save folder/result folder/Volume\_fraction.** Calculation is realized with Function\_Volume\_fractions.m.

Volume fraction of phase *k* is defined as the number of voxels that belong to the phase *k* divided by the total number of voxels *N* of the domain.

|  |  |
| --- | --- |
|  | [VII-v1] |

voxel\_number = numel(Phase\_microstructure);

for current\_phase=1:1:number\_phase % Loop over all phases

code\_tmp = INFO.phase(current\_phase).code;

Numbervoxel\_phase(current\_phase,1)= sum(sum(sum(Phase\_microstructure==code\_tmp)));

Volumefraction\_phase(current\_phase,1) = Numbervoxel\_phase(current\_phase,1)/voxel\_number;

results\_correlation(current\_phase).volume\_fraction = Volumefraction\_phase(current\_phase,1);

end

Results are organized as:

|  |
| --- |
|  |
| Figure VII-14a. Volume fractions result files organization. RVE subfolders are named accordingly to their case (cf. §VII-2b), from top to bottom: one subvolume growth from center with an aspect ratio of 1:1:1 (case D), one subvolume growth from edge along direction 3, from minimum to maximum (case E), independent subvolumes of same size with constant length for 3rd axis (case C), independent subvolumes of same size with a custom aspect ratio of 1:1:1 (case B), and independent subvolumes of same size with initial aspect ratio (case A). |

Volume fractions slice per slice are also calculated slice per slice and plotted.

|  |
| --- |
|  |
| *Figure VII-14b. Example of a volume fractions plotted as a function of positions. Legend, line color, titles, and x-labels are those defined by the user in the import tab.* |
|  |
| *Figure VII-14c. Legend, line color, titles, and x-labels are those defined by the user in the import tab.* |

If a voxel size dependence analysis is asked by the user, then result is plotted:

|  |
| --- |
|  |
| *Figure VII-14d. Voxel size dependence calculated for volume fraction. Vertical dashed black line represents the initial image resolution. Dashed lines are (by default) linear interpolation. Values between parenthesis is the value extrapolated for a resolution of 0 nm. Because volume fraction is a volume averaged property, voxel size has a very limited impact on the result.* |

If one or several representative volume element analyses are asked by the user, results are plotted:

|  |
| --- |
|  |
| *Figure VII-14e. Representative volume element analysis performed for volume fraction of the active material (same analysis is performed for the other phases). (Left) means, extremums, and standard deviations. The short-dashed line at the right indicates the value calculated with the whole volume (also indicated in the legend). Numbers next to values indicate the number of subvolumes. Note that mean values are equal with the one calculated with the whole volume. (Center) relative standard deviation. Vertical dashed line indicates the RVE size for the user-defined threshold (by default set to 5%). (Right) results for each subvolumes.* |
|  |
| *Figure VII-14f. Relative standard deviations are plotted for each phase. If RVE is case C (one dimension is set constant) then figure VII-13e and f are reproduced with both the subdomain cubic root and the quadratic root of the subdomain 2D field of view for the x-axis.* |

RVE analyses performed with Cases D or E (one unique subvolume) are different:

|  |
| --- |
|  |
| *Figure VII-14g. Representative volume element analysis with one subvolume growth from center with an aspect ratio of 1:1:1 (case D). Because the whole volume has a different aspect ratio with the one choose for the subvolume, a gap exists between the whole volume size and the largest subvolume with the custom aspect ratio.* |
|  |
| *Figure VII-14h. Representative volume element analysis with one subvolume growth from volume edge along direction 3 constant (case E). (Left) x-axis is the cubic root of the subvolume size, (right) x-axis is direction 3 growing length.* |

### Connectivity

Results are saved in **Save folder/result folder/Connectivity**.Connectivities are handled with the files Function\_connectivity.m and Function\_Connectivity\_Algorithm.m.

Two voxels are considered connected if they share one common face (edges and vertices connections are ignored). A group of connected voxels is named a cluster. Cluster volumes are expressed in percents of the investigated phase. Connectivity (or percolation) has different definition, illustrated in figure VII-15a, and detailed below:

* An **isotropic definition**28,41, for which three connectivities are determined per phase: (i) the **largest connected cluster**, (ii) the sum of all **isolated clusters**, and (iii) the sum of all **unknown clusters**. Isolated clusters are not connected with the largest connected cluster and are not located at the domain’s edge. Unknown clusters are not connected with the largest connected cluster and are located at the domain’s edge so that it is unknow if they are actually connected with the largest connected cluster or not (a larger field of view would have been required). Unknow cluster is an edge effect. A large volume of unknow cluster indicates the field of view is too small for the analysis.
* A **directional definition**, for which, for each direction three connectivities are determined per phase: (i) the sum of all clusters that are connected **from the first slice to the last slice normal with the investigated direction,** (ii) the sum of all isolated clusters that are not connected with such connected clusters and that are not located at the domain’s colinear edges, and (iii) the sum of all unknown clusters that are not connected with such connected clusters and that are located at the domain’s colinear edges. The oriented definition suits better connectivity analysis of microstructure for which species transport are expected to diffuse through a particular direction – along the whole material thickness (such as the pore domain of battery electrodes).
* A **directional and oriented definition**, for which, for each direction six connectivities are determined per phase: (i) the sum of all clusters that are connected **to the first (respectively, last) slice normal with the investigated direction,** (ii) the sum of all isolated clusters that are not connected with such connected clusters and that are not located at the domain’s colinear edges, and (iii) the sum of all unknown clusters that are not connected with such connected clusters and that are located at the domain’s colinear edges. This connectivity is relevant for electronic percolation for instance, for which particles to be connected only need to be in contact with the current collector (and not necessarily with the opposite interface, i.e., the separator).
* Clusters that contain only one voxel are considered Ill-defined. Ill-defined clusters indicate either or both (i) segmentation produced noise and (ii) image resolution is too low.

|  |
| --- |
|  |
| *Figure VII-15a.* (Left) Isotropic connectivity. There is only one connected cluster (the largest, whatever it is in contact with domain’s edge). (Center) Directional connectivity, illustrated along the vertical direction. (Right) Directional and oriented connectivity, illustrated along the vertical direction, for the bottom edge. |

The built-in MATLAB functions *bwlabeln* is used to calculate connectivity with a face-to-face only connectivity (edges and vertices are ignored to establish connectivity).

Clusters = bwlabeln(binary\_array,6); % connectivty face-2-face

User can, in addition to calculate connectivity of the whole volume, calculate connectivity section per section (independently) using bottom half part of the ‘Connectivity options’ tab. Such section per section analysis is valuable, for instance, to investigate bilayer or multilayer microstructures, for which each layer may have different properties.

|  |
| --- |
|  |
| *Figure VII-15a.* Options specific to connectivity. In this example, volume is cut in three independent subvolumes along direction 3 and connectivity is calculated for each of them separately. |
|  |
| *Figure VII-15b. Connectivity result files organization.* |
| *A close up of text on a white background  Description automatically generated* |
| *Figure VII-15c. Connectivity along directions (slice per slice). Blue lines correspond to the isotropic definition, while red, orange, and magenta lines correspond to oriented definition.* |

Clusters are labeled according to their connectivity and are plotted. Cluster connectivity can be explored slice per slice more in details with the visualization module.

|  |
| --- |
|  |
| *Figure VII-15d. Cluster oriented connectivity (0=background, 1=connected clusters along direction 3 2=isolated clusters, 3=unknown clusters). Arrows have been added to the graph to pinpoint the very few isolated and unknown clusters. There are figures for each different connectivity.* |

If the user asks for section per section connectivity:

|  |
| --- |
|  |
| *Figure VII-15e. Connectivity calculated per section (here 3). There are figures for each different connectivity.* |

In Figure VII-15c, connectivity is calculated within the whole volume, and voxel connectivity is plotted as function of its location. In Figure VII-15e, connectivity is calculated for several subvolumes independently (thick sections along a direction), and the overall connectivity is displayed for each of them.

|  |
| --- |
| A close up of a map  Description automatically generated |
| *Figure VII-15f. Calculation times are also plotted, to evaluate scalability and future calculation times. Because RVA and voxel size dependence analysis were performed, there are many different points.* |

If the user requested a voxel size dependence analysis, then connected clusters connectivity (all definitions) are plotted as a function of voxel size. In addition, ill-defined cluster volume fraction, relative to the investigated phase, is also calculated, as it provides information about the quality of the image resolution.

|  |
| --- |
|  |
| *Figure VII-15g. Voxel size dependence analysis performed for ill-defined cluster. Note the increasing trend indicates more ill-defined (i.e., one-voxel size) clusters appear with coarser image resolution, as expected.* |

If one or several representative volume element analyses were requested, results are plotted for each connectivity.

|  |
| --- |
|  |
| *Figure VII-15h. Representative volume element analysis performed for (left) largest connected cluster, (center) unknown clusters and (right) isolated clusters. Note that mean values are not equal with the one calculated with the whole volume. This is due to the increasing edge effects (quantified through the unknown cluster) that decrease cluster connectivity, as seen in*41*.* |

### Tortuosity factor

Results are saved in **Save folder/result folder/ Tortuosity\_factor\_taufactor**.Tortuosity factors are handled with the file Function\_Tortuosity\_factor\_taufactor.m.

The tortuosity factor (adimensional) denotes the effect of the convoluted, tortuous, path of the phase that hinders the species diffusion or conduction along the direction *i*. In battery modeling, tortuosity almost always refers to the through-plane (i.e., along electrode thickness) pore tortuosity to represent the lithium ion diffusion within the electrolyte (i.e. within the pore domain) from the electrode-current collector interface to the electrode-separator interface. The two other diffusion directions, along the in-plane dimensions, are not considered in 1D and pseudo 2D battery model as electrolyte ionic transport is 1D. However, for mesoscale 3D models all tortuosity factors (in-planes and through-plane) are considered.

Tortuosity factor is deduced from the normalized effective diffusion coefficient (defined as the ratio between the effective diffusion coefficient along the direction *i* and the bulk, dense, diffusion coefficient ) and the porosity (cf. eq. VII-t1). Its value can be obtained through a homogenization calculation performed on a three-dimensional volume reconstruction of the microstructure2,16,38,43. The method consists in solving the Laplace equation (, i.e., stationary heat equation with a unit diffusion coefficient) within the connected network, either with finite element method38,41 of finite difference method2, with a particular set of boundaries condition applied on the two domain’s extremity faces normal with the investigated direction *i*. Then, the effective diffusion coefficient is deduced from the analysis of the calculated concentration/temperature field using the 1D Fick’s first law as detailed in38. The method suffers from edge effect due to loss of percolation at the domain’s edges (quantified through the number of unknown voxels, cf. §VII-5b), and exhibits a sensitivity with the choice of the boundary conditions38,41,42. Both effects are vanishing with larger volumes.

The homogenization calculation is an indirect determination of the tortuosity factor, as it computes first the normalized effective diffusion coefficient and then only deduces the tortuosity factor using equation VII-t1. More direct, geometric, determinations exist but rely on morphology and topology metrics more difficult to characterize32,44, some of them presented in §VII-5g,h.

Tortuosity factor is usually related with the porosity through the Bruggeman’s relationship45,46 with *p* the Bruggeman exponent (cf. eq. VII-t2) and with its empirical counterpart, the generalized Archie’s relationship47,48 (cf. eq. VII-t3). The Bruggeman exponent *p* value is analytically known for ideal particle shape, under certain conditions that limits its application range (cf. eq. VII-t2a), otherwise its value is deduced from the tortuosity factor (cf. eq. VII-t2b). The analytical Bruggeman’s law (cf. eq. VII-t2a) has been extensively used in the past, although with the combined advance of 3D microstructure-scale imaging and CPU, numerical determination of the tortuosity factor has revealed it provides a strong underestimation of the actual tortuosity factor for low porosity lithium ion battery electrodes16,49, explained by its limited range of validity hardly applicable to real microstructures46. Nowadays, the most standard relationship used, in the battery community, is the one proposed by Thorat48 (cf. eq. VIII-t3). To establish it, at least two doublets are required. The interest of such microstructure-tortuosity relationships is to (i) tune microstructure to lower tortuosity factor and thus improve diffusion and (ii) predict tortuosity factors for a wide range of porosity which is particularly valuable for modeling. Note that many other microstructure-tortuosity relationships, that consider additional microstructure properties such as constriction and sinuosity, exist in the litterature32.

|  |  |
| --- | --- |
|  | [VII-t1] |
|  | [VII-t2a] |
|  | [VII-t2b] |
|  | [VII-t3] |

Tortuosity factor is calculated using Taufactor2, from Dr. Samuel Cooper, with a finite-difference based approach, using fixed (i.e., Dirichlet) boundary conditions. Previous work has shown that tortuosity factors calculated with Taufactor are converging with values obtained with a finite element approach16. Calculation is done with the Taufactor *TauFactor* function.

for current\_phase=1:1:number\_phase % Loop on every phase

code\_tmp = INFO.phase(current\_phase).code; % The code of the phase

binary\_phase = zeros(Domain\_size(1),Domain\_size(2),Domain\_size(3));

binary\_phase( Phase\_microstructure==code\_tmp )=1;

voxel\_number = sum(sum(sum(binary\_phase==1)));

% Volume fraction

volume\_fraction\_total(current\_phase,:)=voxel\_number/prod(Domain\_size);

for current\_direction=1:1:number\_dimension % Loop on every analysed direction

% Call tortuosity algorithm (cf. Tau factor manual)

if current\_direction==1

Taufactor\_result = TauFactor('InLine',1,0,0,binary\_phase,[0 0 0;0 0 0;1 0 0],[1 1 1]);

if Tau\_factor\_result.Tau\_W1.Tau == Inf % No percolation path. 65535 is default value for inf tortuosity factor

Tau\_factor\_result.Tau\_W1.Tau = NaN;

end

Tortuosity\_factor(current\_phase,current\_direction)=Tau\_factor\_result.Tau\_W1.Tau;

elseif current\_direction==2

Tau\_factor\_result = TauFactor('InLine',1,0,0,binary\_phase,[0 0 0;0 0 0;0 1 0],[1 1 1]);

if Tau\_factor\_result.Tau\_W2.Tau == Inf

Tau\_factor\_result.Tau\_W2.Tau = NaN;

end

Tortuosity\_factor(current\_phase,current\_direction)=Tau\_factor\_result.Tau\_W2.Tau;

elseif current\_direction==3

Tau\_factor\_result = TauFactor('InLine',1,0,0,binary\_phase,[0 0 0;0 0 0;0 0 1],[1 1 1]);

if Tau\_factor\_result.Tau\_W3.Tau == Inf

Tau\_factor\_result.Tau\_W3.Tau = NaN;

end

Tortuosity\_factor(current\_phase,current\_direction)=Tau\_factor\_result.Tau\_W3.Tau;

end

% Effective diffusion coefficient

Effective\_diffusion\_coefficient(current\_phase,current\_direction) = 1\*volume\_fraction\_total(current\_phase,1)/Tortuosity\_factor(current\_phase,current\_direction);

tau = Tortuosity\_factor(current\_phase,current\_direction);

eps = volume\_fraction\_total(current\_phase,1);

Bruggeman\_exponent(current\_phase,current\_direction) = 1 - log(tau)/log(eps);

end

end

User can, in addition to calculate tortuosity factor of the whole volume, calculate tortuosity factor section per section (independently) using bottom half part of the ‘Tortuosity factor (tau factor) options’ tab – similarly with connectivity.

If a voxel size dependence analysis is asked by the user, both tortuosity factor, Bruggeman exponent, and normalized diffusion coefficient are plotted as function of voxel size. As well, if RVA is asked, RVE size are plotted for tortuosity factor, Bruggeman exponent, and normalized diffusion coefficient.

|  |
| --- |
|  |
| *Figure VII-16a. Tortuosity factor result files organization.* |
| *A screenshot of a cell phone  Description automatically generated* |
| *Figure VII-16b. (Top) Volume fraction, tortuosity factor, Bruggeman exponent, and normalized effective diffusion coefficient. (Bottom) Coefficients anisotropy.* |

### Specific surface area

Specific surface area of phase *i* (m-1) is the phase surface normalized by the phase volume or the domain volume (both definitions are used). It is commonly used as a scaling factor for the electrochemical reaction that occurs at the solid electrolyte active interface in macroscopic models. Specific surface area obtained from microstructure characterization should be considered with great caution, due to a fractal issue discussed in §VII-2a.

|  |  |
| --- | --- |
|  | [VII-s1] |

#### Direct method

Results are saved in **Save folder/result folder/Specific\_surface\_direct**.Specific surface area are handled with the file Function\_Specificinterface\_direct.m, and calculated with Function\_Specificsurface\_direct\_Algorithm.m. Surface area can be simply calculated by adding all the voxels faces located at the boundary between the investigated phase and the complementary phase38,41,50 (direct method). It is well known the discretization of the medium in cuboids induces an overestimation of the surface area calculated with this method41,50–52. For instance, for ideal non-overlapping spheres, a corrective factor of 2/3 can be used to correct the overestimation. Note that this corrective factor is aimed only to correct the overestimation induced by the voxel discretization and not the unknown surface roughness. Particles of NMC and graphite electrodes are typically oblate spheroid (i.e., ellipsoid of revolution with two identical diameters larger than the third diameter: )32 for which a corrective factor can be deduced as described here. The *voxel-based* numerical surface area of an oblate spheroid is given by eq. VII-s2a. Note that it corresponds to the surface projection of the ellipsoid along each axis. The theoretical surface area of an oblate spheroid can be approximated using eq. VII-s2b53.

|  |  |
| --- | --- |
|  | [VII-s2a] |
|  | [VII-s2b] |

We can then deduce the expression of the corrective factor C as:

|  |  |
| --- | --- |
|  | [VII-s2c] |

The expression of the corrective factor is plotted in figure VII-17a. For the extreme case short diameter over long diameter equals 0 (i.e., a=b, c=0), the geometry is no more a volume but a two-dimensional ellipsoid. Since the voxel-based numerical value correspond to the sum of the 2D projections of the volume, it matches with the theoretical value for this extreme case.

|  |
| --- |
|  |
| *Figure VII-17a.* Corrective factor as a function of ellipsoid short diameter over long diameters ratio. |

You can choose the value of the corrective factor in the ‘specific surface area (direct) options’ tab, by default set to 2/3 (which corresponds to non-overlapping spherical particles). Surface area can be normalized with the phase volume or with the domain volume.

|  |
| --- |
|  |
| *Figure VII-17b.* Options specific to specific surface area. |

Calculation is performed on a binary matrix (i.e., voxel=1 if it belongs to the investigated phase, 0 otherwise) where the logical exclusive-OR (xor in MATLAB) is detect adjacent voxels for which one belongs to the phase and the other not.

% Detection of the faces normal to the direction 1

Face\_normal\_1 = xor( binary\_phase(1:Current\_Domain\_size(1)-1,:,:) , binary\_phase(2:Current\_Domain\_size(1),:,:));

% Summation of all these faces

sum1 = sum(sum(sum( Face\_normal\_1 )));

File organization is as below:

|  |
| --- |
|  |
| *Figure VII-17c. Specific surface area result files organization.* |

Specific surface area are also plotted along directions. Following a similar mathematical approach used to calculate distribution functions, the curve f(x) is calculated and plotted such as: with L the domain length. Although f(x) is not a probability density function as its dimension is µm-1.

|  |
| --- |
| *A screenshot of a cell phone  Description automatically generated* |
| *Figure VII-17d. Specific surface area plotted along one axis. Because the volume has only two phases and that we normalized with domain volume, both phase has the same specific surface area. Values noted in the legend are the specific surface calculated on the whole volume. Because we are plotting the function f(x), both have similar values.* |

### Specific interface area

Specific interface area (m-1) of phase *i* and *j* is the interfacial area between these two phases normalized by the domain volume. Specific interface area is especially relevant for microstructures with more than two phases. For instance, in lithium ion battery it can be used to quantify the active interface area between pore and active material particles, while considering a third solid phase (additives). Specific interface area obtained from microstructure characterization should be considered with great caution, due to a fractal issue discussed in §VII-2a.

|  |  |
| --- | --- |
|  | [VII-i1] |

Results are saved in **Save folder/result folder/ Specific\_interface\_direct**.Specific surface area are handled with the file Function\_Specificinterface\_direct.m. and calculated with Function\_Specificinterface\_direct\_Algorithm.m. Interface area is calculated for each phase-phase interface permutation. Interface area are calculating by adding all the voxels faces located at the boundary between the two investigated phases. Similarly with the specific surface area direct method, a corrective factor can be applied to correct the interface area overestimation induced by the cuboid representation. Note that interfacial area is not calculated if the number of phase (including pore) is not superior to 2. For bi-phase microstructure, please calculate the specific surface area instead. File organization is as below:

|  |
| --- |
|  |
| *Figure VII-18a. Specific interfacial area result files organization* |

Similarly with specific surface area, specific interface area are also plotted along directions. Following a similar mathematical approach used to calculate distribution functions, the curve g(x) is calculated and plotted such as: with L the domain length. Although g(x) is not a probability density function as its dimension is µm-1. A three-phase domain is used for illustration.

|  |
| --- |
|  |
| *Figure VII-18b. Three phases material (import tab). Additive phase has been numerically generated using the generation module.* |
| *A screenshot of a cell phone  Description automatically generated* |
| *Figure VII-18c. Specific interface area plotted along one axis. Values noted in the legend are the specific interface area calculated on the whole volume. Because we are plotting the function g(x), both have similar values.* |

### Particle size

Three-dimensional volume reconstructions of lithium ion battery electrodes obtained with computed tomography usually do not show distinct particles, but rather a unique connected cluster that do not allow for a straightforward determination of the particle size32,41. Indeed, there is simply not a unique definition of what is a particle within a fully connected cluster. Particle size calculation is therefore a somewhat ill-defined problem as the object to quantify, ‘particle’, is not defined. Because of this definition issue, a large variety of numerical methods has been developed in the literature. Short review of methods is available in32 along with a comparison of diameter predictions between them.

#### Spherical assumption, continuum Particle Size Distribution (c-PSD) and particle level description

Results are saved in **Save folder/result folder/Particle\_size\_Cpsd.** Particle sizes are handled with the file Function\_particle\_size\_CPSD.m. and calculated with Function\_particle\_size\_CPSD\_Algorithm.m.

* The spherical assumption approach consists in attributing for each voxel of the investigated phase, the diameter of the largest sphere that (i) contains it and (ii) does not overlap with the complementary phase41,54,55. Spheres are allowed to overlap between each other (thus the adjective continuum). Because the c-PSD algorithm relies on a spherical assumption, it provides a strong underestimation of the actual diameter32.
* The particle size field c-PSD is used to deduce another metric, noted , that quantifies the particle level of description of the phase *V*. The particle level of description indicates if the image resolution is high enough to describe accurately the particle of the investigated phase *V*. To calculate it, the volume sum of all the particles with a one-voxel-size is normalized with the phase volume:

|  |  |
| --- | --- |
|  | [VII-p1] |

The particle level description criterion is then deduced as done in41:

|  |  |
| --- | --- |
|  | [VII-p2] |

A value near 1 indicates that almost every particles are described with more than one voxel, while a low value indicates a significant ratio of particles are ill-described suggesting the image resolution is too coarse. Voxel size dependence analysis can be used to identify adequate image resolution.

File organization is as below:

|  |
| --- |
|  |
| *Figure VII-19a. Particle size, spherical assumption, result files organization* |

The particle size distribution is calculated with the file Function\_probability\_density.m (src\Miscellaneous), using a moving average filter on the cumulative function to smooth its derivate and avoid a noisy distribution function.

|  |
| --- |
| A close up of a map  Description automatically generated |
| *Figure VII-19b. Particle size distribution of the solid phase. Black line corresponds to the raw cumulative function, while the red line corresponds to the smoothed cumulative function. Peak near the small particle diameter is an artifact of the method (many tiny irrelevant particles are located at the phase edge) and should not be considered.* |
| *A screenshot of a cell phone  Description automatically generated* |
| *Figure VII-19c. Pore size visualized on three slices. Notice the field c-PSD is continuous (particle are not identified distinctly).* |
| *A close up of a map  Description automatically generated* |
| *Figure VII-19d. Particle level of detail as a function of voxel size. At the initial image resolution, around 10% of the phase volume is described with one-voxel size particle.* |

#### Euclidean distance map fitting method (EDMF).

Results are saved in **Save folder/result folder/Particle\_size\_dmap.** Particle sizes are handled with the file Function\_particle\_size\_distancemap.m. and calculated with Function\_particle\_size\_distancemap\_Algorithm.m.

The method introduced in32 consists in fitting the diameter of a sphere so that its Euclidean distance map cumulative function matches the one calculated on the complex microstructure. Note that the distribution function of the Euclidean distance map is not the distribution of the particle size. This method only provides the mean particle diameter, and not its distribution. Similarly, the graph plotting distance along axis position are the distance to surface distance, and not the particle diameter.

|  |
| --- |
|  |
| *Figure VII-20a. Particle size, EDMF, result files organization* |
| A screenshot of a cell phone  Description automatically generated |
| *Figure VII-20b. Euclidean distance map illustrated on slices of the solid phase* |
| *A close up of a map  Description automatically generated* |
| *Figure VII-20c. Euclidean distance map cumulative function of a sphere is fitted to match the Euclidean distance map cumulative function calculated on the solid domain to determine the particle mean diameter.* |

#### Watershed method, discrete Particle Size Distribution (d-PSD)

BETA: algorithm is bug-free to author’s knowledge but is very slow. It is recommended to use it with small domain or to downscale the image resolution. Nevertheless, it was fast enough to characterize 3D electrode volumes as done in32. Voxel size dependence and RVE analysis not yet implemented. Method usable through the GUI for whole volume analysis only.

Watershed56 is a standard method for particle identification/segmentation. Method is illustrated on lithium ion battery electrode in32,41.

You can visualize the watershed method by calling directly the algorithm function using a 2D array as described below (visualization will slow down the calculation and is not representative of the true algorithm speed):

M=function\_load\_tif('C:\Users\fussegli\Desktop\nmc-1-cal-segmented.tif');

solid\_phase\_id = 1;

binary\_phase = zeros(size(M));

binary\_phase(M==solid\_phase\_id)=1;

binary\_phase\_2D = binary\_phase(:,:,50); % Choose any slice

customfunction = true;

cpsd\_refining = true; % Correct oversegmentation

details\_convergence = true; % Write algorithm progression in the MATLAB command window

visualize\_2D = true; % Create figure and video illustrating the algorithm progression and result

[D\_PSD\_particle\_size,Label\_lake] = Function\_Discrete\_particle\_size\_watershed\_immersion\_algorithm(binary\_phase\_2D,cpsd\_refining,customfunction,details\_convergence,visualize\_2D);

The code above will generate figures *VII-21a-c.*

|  |
| --- |
|  |
| *Figure VII-21a. Flooding progression illustrated on a 2D slice of an NMC electrode.* |
|  |
| *Figure VII-21b. Particle identification on a 2D slice using the watershed algorithm, after over segmentation correction.* |
|  |
| *Figure VII-21c. Particle labeling and size (equivalent diameter) on a 2D slice using the watershed algorithm, after over segmentation correction.* |

* Because watershed method is gradient based, it usually suffer from over-segmentation or over-identification due to the presence of concavities on the particle surfaces (e.g. non-smooth interfaces), which induce a noisy gradient image and generate a lot of irrelevant, oddly shaped small particles. Correct watersheds lines can be then lost in a mass of irrelevant ones, even if the gradient image has been previously filtered. Over-segmentation is discussed in length in the literature32. Over segmentation is corrected using the method introduced in41 that discards particles assigned with a diameter lower than the one obtained with a c-PSD algorithm and reassign their voxels to adjacent particles, assuming that the smallest possible geometric feature that can be considered as a particle is the largest sphere and everything below is an artifact (i.e., assuming c-PSD gives the particle size lower bound)32,41. The method employed here is also used for the other d-PSD method, Pseudo-Coulomb Repulsive field (PCRF). Over segmentation correction is illustrated on the figure below:

|  |
| --- |
|  |
| *Figure VII-21d. Watershed lines before and after over segmentation correction illustrated for the pore domain of an NMC electrode* |

#### Pseudo-Coulomb Repulsive field (PCRF) method, discrete Particle Size Distribution (d-PSD)

BETA: algorithm is bug-free to author’s knowledge but is very slow. It is recommended to use it with small domain or to downscale the image resolution. Nevertheless, it was fast enough to characterize 3D electrode volumes as done in32. Voxel size dependence and RVE analysis not yet implemented. Method usable through the GUI for whole volume analysis only.

Method is illustrated on lithium ion battery electrode in32.

You can visualize the PCRF method by calling directly the algorithm function using a 2D array as described below (visualization will slow down the calculation and is not representative of the true algorithm speed):

M=function\_load\_tif('C:\Users\fussegli\Desktop\nmc-1-cal-segmented.tif');

solid\_phase\_id = 1;

binary\_phase = zeros(size(M));

binary\_phase(M==solid\_phase\_id)=1;

binary\_phase\_2D = binary\_phase(:,:,50); % Choose any slice

cpsd\_refining = true; % Correct oversegmentation

exponent\_law = 3; % Coefficient k of the pseudo Coulomb law

max\_dist = 40; % PCRF local value is calculated on a restricted field of view 2\*max\_dist;2\*max\_dist;2\*max\_dist centered on the local position to reduce CPU time

details\_convergence = true; % Write algorithm progression in the MATLAB command window

visualize\_2D = true; % Create figure and video illustrating the algorithm progression and result

[D\_PSD\_particle\_size, Label\_lake, Repulsive\_matrix, Repulsive\_matrix\_sign] = Function\_Discrete\_particle\_size\_PCRF\_algorithm (binary\_phase\_2D,cpsd\_refining,details\_convergence,visualize\_2D,exponent\_law,max\_dist);

|  |
| --- |
|  |
| *Figure VII-22a. (top left) Binary image, (center) Pseudo-Coulomb repulsive field along vertical direction and (right) Pseudo-Coulomb repulsive field along horizontal direction. The Pseudo-Coulomb repulsive field push dropped imaginary charged points far from the phase edges and particle bottlenecks, eventually enabling particle identification after analyzing all charged points trajectory.* |
|  |
| *Figure VII-22b. Particle labeling and size (equivalent diameter) on a 2D slice using the PCRF algorithm, after over segmentation correction.* |
|  |
| *Figure VII-22c. PCRF method generates less over segmentation compared with watershed for reasons explained in*32 *and is then a more reliable method.* |

### Particle morphology deduced from particle identification

Both Watershed and PCRF method calculate particle aspect ratio and particle sphericity as explained in32.

### Domain topology deduced from particle identification

Both Watershed and PCRF method calculate geometric tortuosity and constriction factor as explained32. Constriction factor can then be deduced as detailed in32.

## Module organization

### File hierarchy

This section is mostly valuable if you plan to modify the module. From a purely end-user point of view, you can skip it. The module organization is illustrated with the figure below.

|  |
| --- |
|  |
| *Figure VII-3. High-level organization chart of the characterization module. Green files are outputs. In addition to the MATLAB m files in src\Main\_menu and src\Microstructure characterization, other files common with other modules are located in src\Miscellaneous.* |

The fields of the MATLAB structures OPTIONS, INFO, and PROPERTY are determined in microstructure\_characterization\_GUI.m, by the user interactions with the module GUI. OPTIONS controls save, format and figure options. Most OPTIONS fields are common for all volumes, except those for loading and saving locations. INFO contains information about phases name and code, directions name, voxel size and region of interest, in addition to general comments about the investigated volume. INFO fields are different for each volume. Lastly, PROPERTY controls all property parameters, RVE analysis parameters, and voxel size dependence analysis parameters. PROPERTY fields are common for all volumes. Essentially, the GUI is used to fulfill these three structures. The file Function\_propertytobecalculatedA\_method1 is detailed in the next section.

### Typical file organization

To explain the organization of a Function\_propertytobecalculatedA\_method1.m, we will use as template the file Function\_particle\_size\_CPSD.m used to calculate particle size through a continuum approach and using a spherical assumption. In this section we only focus on the file organization, not the algorithms (explained in §VII-6).

* Comments lines immediately after the first one indicate the two possible syntax to call the function: through the toolbox, or as a standalone. The variable ‘Phase\_microstructure’ is the 2D or 3D array representing the segmented volume to be quantified.
* %% DEFAULT VALUES section will set the structures OPTIONS, INFO, and PROPERTY with default values in the case the function is called as a standalone.
* %% DATE section is self-explanatory.
* %% FOLDER section creates sub folders, named with the convention propertytobecalculatedA\_method1. Folder separator “\” and “/” are selected depending on the code is running on Windows or not.
* %% INFO section gets the domain size (in voxels) of the microstructure. If the microstructure data is an image (2D array), we enforce the 3rd dimension size to be 1, as code often asks for this value. Number of phases, of voxels and voxel size is also extracted from the INFO structure.
* %% INITIALIZE RESULTS (USE FOR CORRELATION and VISUALIZATION) section initializes the structure results\_correlation and results\_visualization that are used in the correlation and visualization module, respectively. The structure results\_correlation stores scalar values (e.g., mean particle size) while the structure results\_visualization stores 2D or 3D array (e.g. local particle size). While results\_correlation is used by every Function\_propertytobecalculatedA\_method1.m files, results\_visualization is only used when results can be visualized voxel-wise. Some file, such as Function\_Volume\_fractions.m, does not have the results\_visualization structure.
* %% DISPLAY section prints in the MATLAB command window what property is calculated, and with what method.
* %% ALGORITHM ON WHOLE VOLUME section is specific to each file, although it follows the same organization for every file, as described below with a pseudo code.

%% CALCULATION

Get sarting times, both wall clock and CPU.

Initialize one or several arrays that will store main results.

Set parameters for smoothing distribution functions, if any.

Distributions functions are calculated in Function\_probability\_density.m, while smoothing is performed in function\_smooth\_movingaveragefilter.m, both files located in the src/ Miscellaneous folder. Complete lists of arguments are detailed in the file comments.

Loop over each phase.

Select code of the current phase.

Create a binary array, =1 for voxel that belong to the current phase, 0 otherwise.

Call method algorithm on the binary array.

Method algorithm are named according to the convention: Function\_propertytobecalculatedA\_method1\_Algorithm.m

Perform side calculations, if any (in this case the particle level description metric).

Side calculations are performed outside of the algorithm file to keep the algorithm file short. Besides, since the algorithm is called several times for RVE and voxel size dependence analysis and that you may not need the side calculations for these tasks, it will save time.

Perform basic statistics analysis (minimum, maximum, mean, standard deviation and relative  
 standard deviation) if relevant, and store the results in the previously initialized arrays.  
 Perform advanced statistics analysis (distribution functions), if relevant, and store  
 the results in the previously initialized arrays.

Store whatever scalar result values you would like to correlate later in the structure  
 results\_correlation. Store whatever 2D or 3D voxel-wise results, if any, you would like to  
 visalualize later in results\_visualization.

End loop

Measure elapsed time.

Typically, the average and standard deviation are stored in the correlation structure, but you can add other values.

%% TABLES

Create table that contains number of voxels, CPU and wall clock time.

The time structrure, named Table\_time, will be updated with new triplets (voxel number, CPU time, wall clock time) if RVE and/or voxel size dependence analysis will be performed.

Create one or several tables for main results.

Create one or several tables for advanced statistics analysis (distribution functions), if any.

Tables are stored in new structure named Results\_propertyormethodname (here Results\_cpsd). New table will be stored in this structure as the code progresses.

%% SAVE TABLES

Tables are saved in a excel file (one table per sheet) in the save folder.

%% DISPLAY

Tables are printed in the MATLAB command windows

* %% ADDITIONAL RESULTS ON THE WHOLE VOLUME section is specific to each file, although files are sharing same pieces of codes:

%% CUMULATIVE AND DISTRIBUTION FUNCTIONS PLOT

Is used for plotting distribution functions (see function\_probability\_distribution\_figure.m in src/ Miscellaneous). Minimum adjustments are required for each file. Figures are saved in the save folder.

%% ALONG DIRECTIONS

Is used for plotting properties results as a function of location (see Function\_along\_direction.m in src/ Miscellaneous). Figure are saved in the save folder, while results are stored in a table, within the structure Results\_propertyormethodname. Minimum adjustments are required for each file.

%% PARTICLE DIAMETER MAP

This section is specific to this file. It will create 2D slices of the particle size and save the figure.

* %% IMAGE RESOLUTION SENSITIVITY ANALYSIS section automates the voxel size dependence analysis: microstructure is up/down scale several times according to the user parameters selected in the GUI (stored in the structure PROPERTY), and properties are plotted as a function of the voxel size. The array property\_voxelsizedependence is a 2D or 3D array, with rows being the results for each voxel size (1st column is the voxel size, subsequent columns are phase results). The third axis is used to store additional results. Image scaling is performed with function\_scale\_array.m in src\Microstructure\_characterization.

%% EXTRAPOLATION TO 0 nm

Property is extrapolated to a 0 nm voxel resolution, using a polynomial of order ‘interpolation\_voxelsize\_order’. The extrapolated value is stored in the results\_correlation structure so that user can choose later to perform correlation both with non-extrapolated and extrapolated values.

%% MANAGING RESULTS

Results are organized in table, one table per result.

%% DISPLAY TEXT RESULTS

Tables are printed in the command windows.

%% SAVE RESULTS

Tables are stored within the structure Results\_propertyormethodname. Results are saved in an excel file Propertyname\_methodname\_voxel\_size\_dependence.xls (here, D50\_Cpsd\_voxel\_size\_dependence.xls).

%% FIGURES

The function Function\_create\_figure\_voxelsizedependence is called for each parameter to be plotted as a function of voxel size.

%% FIGURES 2 (DISTRIBUTION)

The function\_probability\_distribution\_size\_figure is called for each parameter distribution function to be plotted for different voxel size. Not every method uses it.

* %% REPRESENTATITVE VOLUME ELEMENT (RVE) ANALYSIS section performs representative volume element analysis. The whole section is repeated for each RVE case (A-E) selected by the user. Despite its complexity, this part is very uniform among characterization files, most changes consist in changing structure field to match with the current property/method.

The structure PROPERTY contains the RVA parameters. The first subsection fulfills the structure RVEparameters from PROPERTY, in a similar way for all files: simple replace the field with the current property/method in PROPERTY.particlesize\_cpsd.RVE. Results are stored within a subfolder, one for each RVE case. Function\_get\_Subdomains determines bounds of all subdomains for the RVE case considered (A-E), and the subvolume information is stored in the structure RVE.info.

%% ALGORITHM

Method algorithm is called for each subvolume. Results are stored within the variable Property\_eachsubdomain. When several results are saved, additional dimension are added to the variable (see file function\_connectivity.m for example)

%% STATISTICAL ANALYSIS and RVE SIZE

The result analysis is perfomed in the file Function\_subdomains\_statistical\_analysis.m (src\Microstructure\_characterization). Property\_subdomains\_statistics contains for each RVE size, the number of subvolume and basic statistics (mean, extremums, standard deviation). RVE size are stored withing the variable Size\_RVE. The RVE size can be found inferior, equal, or superior to a domain size, respectively if subdomains sizes are, too large, adequate, or too small. Two size are considered, the first (k\_size=1) corresponds to the cubic root of the RVE size. The second (k\_size=2) corresponds to the square root of the RVE 2D field of view when one dimension if fixed (case C). RVE size are stored in the results\_correlation structure, so that RVE size can be correlated with other metrics.

%% Function\_subdomains\_manage\_results

The file Function\_subdomains\_manage\_results.m (src\Microstructure\_characterization) creates table to organize the many results from the RVA. RVE.results contains result for each subdomain, RVE.phase.statistics contains RVA statistics results, and RVE.sizeX contains RVE size. Lastly RVE.parameters contains all parameters of the current RVA case.

%% TEXT DISPLAY AND SAVE RESULTS

This section is handled by the file Function\_subdomains\_display\_and\_save.m (src\Microstructure\_characterization). Statistics (table RVE.phase.statistics) and RVE size (table RVE.sizeX) are printed in the command window. All fields of the structure RVE are then saved in an excel file, propertyname\_RVE.xlsx. RVA results are saved in a different subsolfer for each RVA case (A-E).

%% FIGURES

Once figure parameters are entered the file Function\_create\_figures\_RVE.m (src\Microstructure\_characterization) is called to print and save the RVE result figures. Only fields propertynameunit and Wholevolume\_results must be changed for another method.

Once all RVE cases have been calculated, the structure RVE is stored in the result structure Results\_cpsd.

* %% ENDING FUNCTION

Calculation time is plotted and saved in excel file using the function function\_time\_figure.m (src\Microstructure\_characterization).

## User-modification of the characterization module

Please follow instructions below to incorporate new algorithms or modifying existing ones.

### Integrate a new algorithm in the toolbox

There are several advantages incorporating your own algorithm in the characterization module: statistical analysis (distribution function), graded analysis (parameter evolution along direction), voxel size dependence analysis and representative volume element analysis are already coded in the toolbox. Furthermore, it provides visualization and correlation tools. Therefore, you can focus on your core algorithm and let the toolbox doing all these generic tasks.

#### Prepare your algorithm

Incorporating an algorithm within any GUI required first to identify all the parameters. A GUI is essentially a user-friendly way to enter algorithm parameters. Once your algorithm input/output architecture is fixed, it is then worth it to integrate within a GUI. First, you will have to convert your code in a function. To be coherent with the other toolbox algorithms and keep short enough the code, please use the minimum number of parameters in your function. Also, please name this function using the naming convention: Function\_propertytobecalculated\_method\_Algorithm.m, for instance:

[Particle\_size] = Function\_particle\_size\_CPSD\_Algorithm(binary\_phase);

Copy the new function Function\_propertytobecalculated\_method\_Algorithm.m in the folder \Microstructure\_analysis\_toolbox\src\Microstructure\_characterization\.

#### Create function that will call your algorithm in the toolbox

You then need to create a new function, hierarchically above of the one you have created in the previous paragraph, that will call your algorithm and integrate it with all the side calculations, such as RVE. Please name it Function\_propertytobecalculated\_method.m, for instance:

[] = Function\_particle\_size\_CPSD(Phase\_microstructure, PROPERTY, OPTIONS, INFO)

The arguments are (almost) always ‘Phase\_microstructure’, ‘PROPERTY’, ‘OPTIONS’, and ‘INFO’. It is recommended to use existing functions as a template. If your new algorithm calculates a scalar (such as volume fraction), use Function\_Volume\_fractions.m as template. If the property is anisotropic, use Function\_Tortuosity\_factor\_taufactor.m as template. If you calculate a pixel-wise information (such as particle size), use Function\_particle\_size\_CPSD.m as a template. You should consider the function could be used as a standalone. That’s the purpose of the very first section (%% DEFAULT VALUES), that allows user to call directly the function from the MATLAB command window, skipping the whole GUI. Open Function\_Specificsurface\_direct.m to see an example. The standalone syntax to call it is Function\_Specificsurface\_direct(array, voxelsize, corrective\_factor), instead of Function\_Specificsurface\_direct(array, PROPERTY, OPTIONS, INFO) when called through the GUI. You will have to modify the following lines in to adapt it to your code:

if nargin == 3 % Minimum number of parameter + volume

voxel\_size = PROPERTY;

corrective\_factor\_specificsurface = OPTIONS;

clear PROPERTY OPTIONS

[…]

% Parameter

PROPERTY.specificsurfacearea\_directmethod.correctivefactor = corrective\_factor\_specificsurface;

else % Incorrect number of argument

disp 'Error calling Function\_Specificsurface\_direct. Wrong number of argument.'

help Function\_Specificsurface\_direct

end

Parameter specific to an algorithm are stored within the PROPERTY structure, with the naming convention: PROPERTY.propertyname\_methodname.parametername. Then you will have to adapt the rest of the function to your code. If you have selected the good template, few changes will be required, mostly variable names. Copy the new function Function\_propertytobecalculated\_method.m in the folder \Microstructure\_analysis\_toolbox\src\Microstructure\_characterization\. Pay special attention to the structure results\_visualization and results\_correlation as they are doing the link respectively with the visualization and the correlation module, see sections c and e. You will have also to modify the file function\_summary\_onevolume.m, see section d.

#### Update the GUI

The last step consists in updating the GUI itself. Open microstructure\_characterization\_GUI.m. Copy-paste the following codes (choose the one that correspond to your template) and replace the text. First the PROPERTY default parameters:

% Default parameters for specific interface area (direct method)

PROPERTY.specificinterfacearea\_directmethod.todo = true;

PROPERTY.specificinterfacearea\_directmethod.voxel\_size\_dependence.todo = true;

PROPERTY.specificinterfacearea\_directmethod.voxel\_size\_dependence.voxel = [2 3 4 5];

PROPERTY.specificinterfacearea\_directmethod.number\_RVE = 1;

PROPERTY.specificinterfacearea\_directmethod.RVE(1).name = 'Independant subvolumes of same size + keep initial aspect ratio (A)';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).savename = 'SubInitialAR';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).type = 'A';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).divisions = [2 3 4 5];

PROPERTY.specificinterfacearea\_directmethod.RVE(1).subs2 = true;

PROPERTY.specificinterfacearea\_directmethod.RVE(1).subs4 = true;

PROPERTY.specificinterfacearea\_directmethod.RVE(1).Aspectratio = 'n/a';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).Constantdirection = 'n/a';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).Growthdirection = 'n/a';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).Growthperstep = 'n/a';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).firstuniquevolume\_size='n/a';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).firstuniquevolume\_unit='n/a';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).Growthrelativeto = 'n/a';

PROPERTY.specificinterfacearea\_directmethod.RVE(1).threshold\_std = default\_threshold\_std;

PROPERTY.specificinterfacearea\_directmethod.RVE(1).threshold\_numbersubvolumes = defaut\_threshold\_numbersubvolumes;

default\_correctivefactor\_spidirect = 2/3;

PROPERTY.specificinterfacearea\_directmethod.correctivefactor = default\_correctivefactor\_spidirect;

Create tab, with name following the convention property name (method):

tab\_specificsurfacearea = uitab('Parent', table\_group\_1,'BackgroundColor',background\_tab, 'Title', 'Specific surface area (direct) options');

Select a color for the tab. Method that calculate the same property should use the same color.

tab\_specificsurfacearea.ForegroundColor =[0 0.3922 0];

Then copy-paste the whole section used to populate the template tab, for instance for the specific surface area calculated with the direct method, that all these lines:

%%

%% TAB SPECIFIC SURFACE AREA (DIRECT)

%%

[…]

%%

%% TAB the next section (method)

%%

You will have to rename all GUI and callback objects. The GUI object below the annotation lines control the parameter for this method, and then differ from method to method. You may have to erase or create GUI object to adjust them to your algorithm parameters. Your algorithm is now integrated within the toolbox, congratulations!

### Modify an existing algorithm

If you want to modify an existing algorithm for whatever reasons (e.g., algorithm is too slow), you can implement your modifications quite easily. Method algorithms are named using the following convention: ‘Function\_propertytobecalculated\_method\_Algorithm.m’. For instance, the algorithm to calculate the particle size with a continuum particle size (c-PSD) method is ‘Function\_particle\_size\_CPSD\_Algorithm.m’. You do not need to modify other files used for plotting, RVE analysis or other tasks. The basic input/output structure is:

[Particle\_size] = Function\_particle\_size\_CPSD\_Algorithm(binary\_phase)

With binary phase a 3D array, with voxels being equal to 1 for the investigated phase, and 0 for the complementary volume. You should use the minimum number of parameters to keep the algorithm file short enough to be readable, and to be coherent with the other toolbox’s algorithms. For instance, in this case the voxel size is not even used (the algorithm is adimensional with a unit voxel size). The script just above the algorithm Function\_particle\_size\_CPSD.m scales afterwards the particle size:

Function\_particle\_size\_CPSD(Phase\_microstructure, PROPERTY, OPTIONS, INFO)

[…]

[Particle\_size] = Function\_particle\_size\_CPSD\_Algorithm(binary\_phase); % Call algorithm

[…]

Particle\_size = Particle\_size\*voxel\_size/1000; % nm->um

If your script uses the same parameters in the same manner of the legacy algorithm, no other modifications should be required. If you use less parameters, you must manually comment the lines that use such superfluous parameters. If you use more parameters, you can either hard coded them in the script, or you can control their value through the GUI. An example of GUI-controlled parameter can be found for the specific surface area calculation, for which a corrective factor is used. Open the file microstructure\_characterization\_GUI.m and search for the line

PROPERTY.specificsurfacearea\_directmethod.correctivefactor = default\_correctivefactor\_spdirect;

Parameters are stored within the PROPERTY structure, following the syntax PROPERTY.properyname\_methodname.parameter (note that parameters shared among various algorithms, such as the voxel size, are stored in the INFO structure). The parameter value is controlled through a edit box MATLAB GUI object:

Edit\_spdirect\_correctivefactor = uicontrol('Parent', tab\_specificsurfacearea,'Style', 'edit','FontSize',font\_size\_small\_GUI,'FontName',font\_name\_GUI,'String',default\_correctivefactor\_spdirect,'BackgroundColor','w','HorizontalAlignment','center','Units','normalized','Position', [pos\_x\_start 0.35-0.3\*pos\_delta\_y 3.5\*pos\_delta\_x 0.3\*pos\_delta\_y],'Callback', @edit\_spdirect\_correctivefactor\_Callback);

function edit\_spdirect\_correctivefactor\_Callback(~,~)

PROPERTY.specificsurfacearea\_directmethod.correctivefactor = str2double(Edit\_spdirect\_correctivefactor.String);

end

You will have to use a similar code to add your new parameter.

### Save a 3D array to be used in the visualization module

You can easily save new results to be later visualized through the ‘Microstructure and results visualization’ module. First, let us have a look on how existing array results are currently saved, for instance the particle size calculated with the spherical assumption method. To do so, open the file ‘Function\_particle\_size\_CPSD.m’ and search for the line:

for current\_phase=1:1:number\_phase

[…]Particle\_size is calculated for the current phase

results\_visualization(current\_phase).Particle\_diameter\_CPSD = Particle\_size;

end

Here, ‘Particle\_size’ is a 3D array with ‘Particle\_size(x,y,z)’ the diameter of the phase numbered ‘current\_phase’. As a reminder, ‘current\_phase’ is the MATLAB index number of the phase, starting from 1, and not the phase code itself. At the end of the script, the ‘results\_visualization’ structure is saved as:

save([Current\_folder 'Visualization\_particlediameter\_CPSD'],'results\_visualization','-v7.3');

Let us say we want to visualize also the particle radius. To do this, the only modification you would have to perform is to add the line in the ‘Function\_particle\_size\_CPSD.m’ file:

for current\_phase=1:1:number\_phase

[…]Particle\_size is calculated for the current phase

results\_visualization(current\_phase).Particle\_diameter\_CPSD = Particle\_size;

results\_visualization(current\_phase).Particle\_radius\_CPSD = Particle\_size/2;

end

Note that you are free to name the new field (in this example, Particle\_radius\_CPSD) as you wish. Although, to keep syntax coherent, the recommended field name should be written as ‘parametername\_methodname’. Now, run the microstructure characterization toolbox, make sure that ‘Calculate particle size with C-PSD method’ is checked in the GUI for this example. Once finished, run the microstructure visualization toolbox, go to tab ‘Volume’ and click on ‘Choice 2: import a volume result’ and select the root folder of your calculation. The script will read all the fields of the structure results\_visualization for you to choose. You should then have the following choice:

|  |
| --- |
|  |
| *New visualization choice ‘Particle\_radius\_CPSD’ is now available in the popup menu.* |

Note that the new choice corresponds to the new structure field added to results\_visualization. Select the phase, and then plot it.

|  |  |
| --- | --- |
|  |  |
| *Visualization with (left) ‘Particle\_diameter \_CPSD’ and (right) ‘Particle\_radius\_CPSD’ option. Note the difference in the colormap scale.* | |

### Save a new result in the summary table

We will keep with the radius example. Still in the file ‘Function\_particle\_size\_CPSD.m’ add the line:

Table\_cpsd = table(INFO.phasename,PSD\_results(:,1),PSD\_results(:,2),PSD\_results(:,3),PSD\_results(:,4),PSD\_results(:,5),...

'VariableNames',{'Name' 'Min' 'Mean' 'Max' 'Std' 'Std\_percents'});

Table\_radius = table(INFO.phasename,PSD\_results(:,1)/2,PSD\_results(:,2)/2,PSD\_results(:,3)/2,PSD\_results(:,4)/2,PSD\_results(:,5),...

'VariableNames',{'Name' 'Min' 'Mean' 'Max' 'Std' 'Std\_percents'});

Basically, you need to create a new table and write the minimum, mean, maximum, standard deviation and relative standard deviation of the new result. In this example, we can simply divide by two the diameter result (except for the relative standard deviation which is unchanged). Then save the new table in the result structure as:

Results\_cpsd.Table\_cpsd = Table\_cpsd;

Results\_cpsd.Table\_radius = Table\_radius;

At the end of the script, the result structure is saved in the summary folder:

save([Current\_folder 'Results\_particlediameter\_CPSD'],'Results\_cpsd')

Now open the file function\_summary\_onevolume.m and search for the string comparison that correspond to the result file name used above, and add the lines within:

if strcmp(current\_result,'Results\_particlediameter\_CPSD.mat')

[…]

line\_table=line\_table+1;

Propertyname(line\_table) = {'Equivalent radius'}; % Name of your choice

Propertymethod(line\_table) = {'C-PSD'}; % Name of the method

T = datamat.Results\_cpsd.Table\_radius; % Table name

for current\_phase=1:1:number\_phase

array = T{current\_phase,2:end};

PropertyMin(line\_table,current\_phase) = {num2str(array(1),string\_precision)}; % Min

PropertyMean(line\_table,current\_phase) = {num2str(array(2),string\_precision)}; % Mean

PropertyMax(line\_table,current\_phase) = {num2str(array(3),string\_precision)}; % Max

PropertyStd(line\_table,current\_phase) = {num2str(array(4),string\_precision)}; % Standard deviation

PropertyUnit(line\_table,current\_phase) = {'[um]'}; % Unit

PropertyStdpercent(line\_table,current\_phase) = {num2str(array(5),string\_precision)}; % Standard deviation in percents of the mean  
 end

Note that you must be coherent with the structure and table name: they must be the same used in ‘Function\_particle\_size\_CPSD.m’ (here ‘Results\_cpsd.Table\_radius’). Write the correct unit (here the radius is expressed in micrometers). Now, run the microstructure characterization toolbox, make sure that ‘Calculate particle size with C-PSD method’ is checked in the GUI for this example. Once finished, open the summary folder of the calculation root folder and open one of the image file. You should see:

|  |
| --- |
|  |
| *Result summary image has a new line ‘Equivalent radius’.* |

Open the excel file ‘Table\_summary\_results.xls’. The table has been updated too.

|  |
| --- |
|  |
| *Table\_summary\_results excel sheet has a new line ‘Equivalent radius’.* |

### Save a result to be used in the correlation module

We will keep with the radius example. Still in the file ‘Function\_particle\_size\_CPSD.m’ add the line:

for current\_phase=1:1:number\_phase

[…]PSD\_results is calculated for the current phase

results\_correlation(current\_phase).Particle\_diameter\_mean\_CPSD = PSD\_results(current\_phase,2);

results\_correlation(current\_phase).Particle\_radius\_mean\_CPSD = PSD\_results(current\_phase,2)/2;

end

At the end of the script, the structure is saved in the correlation folder:

save([Current\_folder 'Correlation\_particlediameter\_CPSD'],'results\_correlation')

# Microstructure and results visualization

This module enables the user to visualize 3D data, customize visualization, and save it both in static images and in videos, in a user-friendly way. It is particularly valuable for presenting/sharing microstructure data with people not familiar with tif file and/or visualization software such as ImageJ: instead of sharing a tif file, you can make a video of the microstructure data and incorporate it in a PowerPoint you share. There are currently three different visualization types:

* Visualize a 3D tif file (cf. §VIII-1).
* Visualize the relevance of a segmentation comparing grey-level and segmented volumes side by side (cf. §VIII-2).
* Visualize pixel-wise results (such as particle size) obtained from the microstructure characterization module (cf. §VIII-3).

## Tiff data (grey-level and segmented volumes)

Procedure is illustrated step-by-step in the following figures. The input file is a 3D tif file.

|  |
| --- |
|  |
| *Figure VIII-1a. Step 1: select volume to visualize.* |
|  |
| *Figure VIII-1b. Step 2 and 3: select voxel size, 3D slices option and create figure.* |
|  |
| *Figure VIII-1c. Visualization interface.* |

You can explore with ease each direction independently using sliders. On the top right, you can change the colormap (here, ‘copper’ is selected). You can also enforce the minimum value (here the pore background) to be plotted in white or in black. You can display the colorbar and specify colormap bounds with the following options: global: lowest volume value corresponds to darkest color, highest volume value corresponds to brightest color, local: lowest slice value corresponds to darkest color, highest slice value corresponds to brightest color, and custom: manually assign value for darkest and highest colors.

|  |
| --- |
|  |
| *Figure VIII-1d. Color options. Default min-max of the custom color bar are the global min-max of the volume.* |

On the bottom right, you can choose options for saving figures. First select a save folder and write the filename. Simply click on save figure for a static picture. For a video, choose the framerate (here 25), then click to save video. By default, the format video is mpeg-4 with a MATLAB video quality of 100. Please note that the GUI is not visible for saved pictures and videos.

|  |
| --- |
|  |
| *Figure VIII-1e. Figure and video saving options.* |

If you want to compare side-by-side 2 or more 3D volumes, you can call directly the standalone function *Microstructure\_comparison\_visualization\_interface* in the command window (cf. §XI for example).

## Comparing grey-level and segmented volumes

Evaluating segmentation often requires a visual inspection. The second tab of this module allows you to compare side by side a grey-level image and its segmented version. Both tif files must share the same dimension. In addition, an overlay is displayed to help checking if the segmentation is a good match for the volume. The user can choose the slice orientation and customize the phase colors. Picture and video can be saved (GUI objects are modified accordingly).

|  |
| --- |
|  |
| *Figure VIII-2a. Step 1: select grey-level and segmented images.* |
|  |
| *Figure VIII-2b. Figure and video saving options. Top left: grey-level slice, top-right: segmented slice, bottom left: linear combination of the two images (overlay).* |

## Microstructure characterization result

Voxel-wise data is information defined, as indicated by its name, locally for each voxel. For example, particle size, particle label, cluster (connectivity) label are voxel-wise. Not every microstructure property is voxel-wise: properties defined over the whole volume, such as volume fraction or tortuosity factor, are not. Some voxel-wise microstructure properties calculated with the microstructure characterization module can be visualized with this module. For more details on how to choose what properties can be visualized, see §VII-7b and search for the MATLAB structure results\_visualization. Unlike the two previous sections, you need first to calculate microstructure properties on a volume with the microstructure characterization module before visualization. In the first tab, select the second choice ‘Choice 2: import a volume result’. Then choose the save folder used with the microstructure characterization module.

|  |
| --- |
|  |
| *Figure VIII-3a. Step 1: select result to visualize.* |
|  |
| *Figure VIII-3b. You must select the folder you have set as ‘save folder’ in the microstructure characterization module. In this case, the folder circled in red.* |

The module will then find automatically all results stored specifically for visualization (no hard-coded choice). Choose what properties you want to see, then for what phase.

|  |
| --- |
|  |
| *Figure VIII-3c. Step 2: Select what property to visualize. Only parameters already calculated are shown.* |
|  |
| *Figure VIII-3d. Step 3: Select for which phase the parameter will be displayed.* |

Note that the property names corresponds to the structure field, e.g. :

results\_visualization(current\_phase).Particle\_diameter\_CPSD = Particle\_size;

The phase names correspond to the ones you have set in the microstructure characterization module. Then write voxel size, and property unit.

|  |
| --- |
|  |
| *Figure VIII-3e. Step 4 and 5: select voxel size, parameter unit (here micrometers for particle size), 3D slices option and create figure.* |

Once you have finalized your selection and create the figure, you can tune and save the visualization (the options are similar with those of §VIII-1).

|  |
| --- |
|  |
| *Figure VIII-3f. Example of visualization results. Figure title is volume name, property name, phase name.* |
|  |
| *Figure VIII-3g. Example of cluster labeling (connectivity) visualization.* |

# Properties correlation

This module enables the user to import various microstructure property values determined on multiple microstructures in order to plot them as a function of each other (i.e., a correlation matrix). It is particularly valuable for summarizing data obtained on various microstructures and to establish correlation between dependent microstructure properties. Note that to generate such property results, the microstructure characterization module must be used first. At least two microstructures must have been characterized before importing their data in the correlation module. Results that can be imported are saved in the subfolder ‘correlation’ of each result folder generated with the microstructure characterization module (cf. §VII-4d). The user can add new property results to be correlated as indicated in §VII-7e.

Procedure is illustrated step-by-step in the following figures.

|  |
| --- |
|  |
| *Figure IX-1. Step 1: select the result folder from a previous microstructure characterization* |
|  |
| *Figure IX-2. Step 2: select the phase for which you want to import a property result you want to correlate. The phase name (here, ‘Pore’ and ‘Graphite’ are those entered in the import tab of the microstructure characterization module).* |
|  |
| *Figure IX-3. Step 3 and 4: Select properties you want to correlate.* |

The names reported in the Parameter name are those used in the ‘Result\_correlation’ MATBAL structure, e.g., in Function\_Tortuosity\_factor\_taufactor.m (src\Microstructure\_characterization):

results\_correlation(current\_phase).(['Tortuosity\_' num2str(current\_direction) '\_' str\_direction]) = Tortuosity\_factor(current\_phase,current\_direction);

% Str\_direction is the direction name entered in the microstructure characterization import tab.

|  |
| --- |
|  |
| *Figure IX-4. Step 5: Name accordingly parameters (names will be used for figure). You have to do it only one time.* |

Then repeat steps 1-4 for each microstructure you would like to import. It is not required that each microstructure has all the microstructure properties. In the figure above, for instance, one RVE value was not available for the first volume. Once done, you can choose your plotting options and create the figure with the corresponding button.

|  |
| --- |
|  |
|  |
| *Figure IX-5. (Top) plotting options, and (bottom) figure created. On the top right the Kendal’s tau ranking value is indicated (first value is obtained considering all data points, while value in parenthesis is obtained by first calculating the coefficient within each group and then takes its average).* |

The Kendal rank correlation coefficient57 (also called Kendall’s tau coefficient) is also calculated for each property doublet. It is a non-parametric measure of the ordinal association, or rank correlation, between two variables. Any pair and are said to be concordant if they share the same rank (i.e., if and or if and). Otherwise they are said to be discordant. If or they are neither concordant nor discordant. The Kendall’s tau coefficient is then defined as:

|  |  |
| --- | --- |
|  | [IX-1] |

If the two properties share the same ranking (i.e. when *x* is increasing, so does *y*), then . Inversely, if their ranking is the reverse of the other (i.e. when x is increasing, y is decreasing), then . Both cases indicate a strong correlation between the two properties. If , then it means the properties are independent: no relationship is expected to exist between them. If volumes are sorted per group, the ranking coefficient is also calculated within each group, and then its average value among all groups is calculated. This is relevant for establishing two parameters are correlated when such correlation is microstructure specific, for instance for tortuosity factor and porosity. Kendall’s tau coefficient is calculated with Function\_Kendall\_tau\_ranking.m (src/Properties\_correlation).

|  |
| --- |
|  |
| *Figure IX-6. Correlation map using Kendal’s tau ranking (more data points are required to provide a relevant correlation analysis).* |

You can tailor your plotting changing the GUI options, for instance:

|  |
| --- |
|  |
| *Figure IX-7. Plotting per volume instead of per group to identify who’s who.* |

You can also visualize in the MATLAB command window or export in an excel file the correlation matrix with the corresponding buttons, valuable to build a database for instance.

|  |
| --- |
|  |
| *Figure IX-8. Correlation matrix exported in excel.* |

# Create mesh for FEM

**BETA**: Iso2mesh may crash generating meshes (intersecting cells error). Workaround are discussed in the text. Nevertheless, it is possible to mesh full-cell geometry with dozens of millions of cells, enough for RVE scale electrochemical simulation as shown at the end of this section.

The module is built around Iso2mesh3 that need to be installed first.

* Installation:

Copy <https://github.com/fangq/iso2mesh> in your computer and add the folder in your MATLAB path. Or download from <https://github.com/fangq/iso2mesh>. Make sure to choose the binary adequate for your OS (Windows, Unix, or MacOS).

* For details about Iso2mesh, read <http://iso2mesh.sourceforge.net/cgi-bin/index.cgi>

Current version of the toolbox is using Iso2mesh 2018 v1.9

## Purpose of the module and restrictions

The module enables you to create volumetric tetrahedron-based mesh for half and full-cell. It is using constrained Delaunay tetrahedralization (CGAL) for surface mesh extraction, Laplacian, Laplacian-HC, and Low-pass filters for surface mesh smoothing, and Tetgen for volumetric mesh generation and adaptative mesh resolution. The meshing is done phase per phase with conforming meshes at the interfaces and also for the whole cell with a unique mesh.

The module has been tested considering only two-phases material per electrode (pore and one solid phase), with both phases being nearly 100% connected, which is typical for Lithium ion battery electrodes computed tomography 3D volumes. Note that Iso2mesh is capable to produce mesh with n-phases materials. The module could be updated to address n-phase materials with non-connected phases.

## Utilization

Module is illustrated with an NMC electrode (half-cell configuration) performed on a laptop (4 cores, 16 GB RAM, <10 minutes meshing time). Larger domain sizes typically require a workstation with a lot of RAM. Set the location of your save folder in the first tab and then follow instructions below.

* Step 1: Import tif files.

In the ‘Microstructures’ tab, first use the top left popup menu to select the cell material, between ‘Left electrode’, ‘Separator’, and ‘Right electrode’. The left/right terminology indicates the position along the first axis of the electrode using the separator as central location. Then click on ‘New/reset electrode’ and choose in the newly visible popup menu if you wish to model a heterogenous (porous) material or a homogenous one. Homogenous representation is relevant for modeling a reference electrode (i.e. a dense plate) or a microstructure that exhibits features/particle size much smaller compared with the other microstructures considered for the cell. This is typically the case for the separator, for which pores are order of magnitude smaller compared with NMC/graphite electrodes. Meshing materials with order of magnitude difference feature size would add a too high constraint on the mesh.

If you choose ‘Homogenous medium’, you only have to enter the length in number of voxel.

|  |
| --- |
|  |
| *Figure X-1a. For a homogenous medium, only the length (along cell thickness) in voxel is required.* |

If you choose ‘Imported heterogenous medium’, you have access to more options. First, import the tif file (‘Click to import volume’). It has to be a 3D tif segmented file. Left table shows volume fractions and is updated if you subsequently modify the Region of Interest (ROI) or perform upscaling or downscaling. Then, set your ROI and microstructure orientation. You can swap axis (you *must* set the first axis as the through-plane direction, i.e. along the thickness of the electrode) and flip axis. More complex ROI selection (such as rotation) can be performed in the filtering/segmentation module if needed. You can then upscale or downscale the volume. Upscaling/downscaling is especially important when you want to mesh a full cell, for which imaging of the anode and of the cathode may have been done at different image resolutions. In such case you must rescale them so that they share the same voxel size. Downscaling is also interesting to ease the meshing process. Once done for this material, you can visualize the microstructure to check you are satisfied with your choices. Then click on the ‘save electrode’ button and repeat for the other materials.

Subsequent steps are for heterogenous case only. Step 4: import the tif (segmented) volume.

|  |
| --- |
|  |
| *Figure X-1b. For a heterogenous medium* |
|  |
| *Figure X-1c. Visualize microstructure* |

* Optional Step: Generate separator geometry.

If you do not want to use an homogenous representation for the separator, and if you do not have a tif file for its geometry, you can generate it in the ‘Generate separator’ tab. Look for file Function\_generate\_strips.m and Function\_generate\_connectedplates.m for details.

|  |
| --- |
|  |
| *Figure X-2. (optional) Separator deterministic geometry generation* |

* Step 2: Morphology opening and cell assembly.

First select the voxel size in nm. Then you need to check if dimensions are matching. If you are working in a full-cell configuration, anode and cathode may have different in-plane dimension. If this is the case, text will be displayed in red to warn the user, and you can fix the issue by clicking on the ‘crop in-plane dimensions of larger domains’ to automatically fix it. For a better control, you should crop volumes in the ‘microstructures’ tab.

You can then perform two morphology opening microstructure independently for each microstructure (but only for the heterogenous ones). The first (optional) is a standard erosion and dilatation that will simplify the surface. It increases the meshing process chance of success, especially for very complex geometry.

function [Phase\_microstructure] = Function\_erosion\_dilatation(Phase\_microstructure,code,complementary\_code)

% EROSTION AND DILATATION

% Opening(Image) = Dilation( Erosion (Image) )

Domain\_size=size(Phase\_microstructure); % Domain size

% Create binary matrix

binary\_phase=zeros(Domain\_size(1),Domain\_size(2),Domain\_size(3));

binary\_phase(Phase\_microstructure == code) = 1;

% Distance map

distance\_map = bwdist(~binary\_phase,'chessboard');

% Erosion

binary\_phase(distance\_map<=1)=0;

% Distance map

distance\_map = bwdist(binary\_phase,'chessboard');

% Dilatation

binary\_phase(distance\_map<=1)=1;

% Reassign

Phase\_microstructure=zeros(Domain\_size(1),Domain\_size(2),Domain\_size(3))+complementary\_code;

Phase\_microstructure(binary\_phase==1)=code;

end

The second will convert each phase in a unique cluster and will ‘clean’ the geometry (highly recommended – module not tested otherwise). First, isolated clusters (e.g. close porosity) of both phases are assigned to the surrounding phase. As a result, each phase is a 100% connected cluster. This geometry simplification impacts very few Lithium ion battery electrodes computed tomography images, as phase connection is typically >99% while it help simplifying subsequent electrochemical modeling. Then voxels with a line-to-line or a vertex-to-vertex connection with a neighbor voxel of the same phase are detected and assigned to the complementary phase. This ensures voxels of the same phase are connected only face-to-face, which will make easier the meshing process while improving the mesh quality. The two steps are performed sequentially in a while loop until both phases are 100% connected and all voxels are face-to-face connected. See Function\_cleanmicrostructure.m, Function\_clean\_microstructure\_onephase.m and Function\_clean\_microstructure\_algorithm.m files for details. If the image resolution is too coarse, the volume fraction listed in the table may change significantly, indicating the microstructure is degraded. For a fine enough image resolution, the change is insignificant. You can check it in the MATLAB command window:

Microstructure vertece-vertece and line-line dangerous connections removed

Number of voxels altered: 5714

Thus, 0.403 percents of the initial number of voxel

You will then need to assign a unique integer (not zero) for each phase of the whole cell. For instance, in the figure below: left reference electrode (homogenous medium) is noted 1, separator (homogenous medium) is noted 2, right electrode electrolyte is noted 3, and right electrode active material is noted 4. The maximum number of phase is currently 6: 'Left electrode solid', 'Left electrode: electrolyte', 'Separator: solid', 'Separator: electrolyte', 'Right electrode: solid', and 'Right electrode: electrolyte' which corresponds to a full cell configuration with both electrodes and separator represented as an heterogenous medium.

Once all phases assigned, click on the ‘Assemble cell’ that will create the cell 3D array, and then on the ‘Visualize cell’ to see it. If you are satisfied with, click on the ‘Save cell and go on’ button. The cell 3D array is also saved (Array\_cell.tif).

|  |
| --- |
|  |
| *Figure X-3a. Assemble cell from the electrodes and the separator microstructures* |
|  |
| *Figure X-3b. Visualize cell. Half-cell with from top to bottom reference plate, separator, and NMC electrode (then, a 4-phase domain).* |

* Step 3: Surface smoothing and mesh density control parameters

Some Iso2mesh options are accessible form the ‘Iso2mesh options’ tab. See file mesh\_generation\_withIso2mesh.m to see functions syntax with the parameters set in this tab, and the Iso2mesh documentation (<http://iso2mesh.sourceforge.net/cgi-bin/index.cgi?Doc/FunctionList>) for more details.

By default, only the cgalmesh option is available to create the surface mesh (‘simplify’ option is less effective or does not work and is then not proposed in the GUI). Radbound can be lowered to refine the surface geometry, useful when the microstructure surface is very complex.

More choices are available for the smoothing algorithm. From Iso2mesh documentation: “Based on [Bade2006], 'Lowpass' method outperforms 'Laplacian-HC' in volume preserving and both are significantly better than the standard Laplacian method”. From various testing, ‘Laplacian’ produces better looking geometry (cf. §X-4) but with a poorer element quality (needle-like tetrahedron) compared with the ‘Lowpass’ method. Besides, ‘Laplacian’ slightly shrinks the domain volume, while ‘Lowpass’ preserves it. You can tune the surface smoothing with the algorithm parameter available in the adjacent table. ‘Laplacian’ is then ideal for illustration purpose, while ‘Lowpass’ provides more robust mesh for FEM.

The last set of options are for the volumetric mesh generation, that allow you to control the mesh density. Maxvol sets the maximum tetrahedron volume: a large value will allow Iso2mehs to generate large tetrahedron at the bulk while using smaller tetrahedron near the phase surface.

|  |
| --- |
|  |
| *Figure X-4a. Iso2mesh options* |
|  |
| *Figure X-4b. Mesh density control. Using a high value for ‘maxvol’ enables fine cells at the interface (important to catch gradients induced by interfacial reactions) and large cells in the phase bulk in order to keep low the problem size.* |

* Step 4: Create the mesh

On the next tab, click on ‘Click to create mesh’ to call Iso2mesh. If no error are produced, then the MATLAB command window should display a text similar to:

creating surface and tetrahedral mesh from a multi-domain volume ...

Volume/Surface Mesh Generation Utility (Based on CGAL 5.0)

(modified for iso2mesh by Qianqian Fang and Peter Varga)

http://iso2mesh.sf.net

RNG seed=1648335518

Mesh sizes are (label=size) (1=1000)

node number: 625722

triangles: 2451552

tetrahedra: 3470327

regions: 4

surface and volume meshes complete

- SURFACE MESH CREATED with v2s: number of region 4

: number of holes 0

list of interior points for all sub-region, [x,y,z]:

5.2653 36.4604 18.5528

17.8195 44.5183 9.4624

73.0275 163.9179 109.0669

73.5917 99.2220 62.9688

generating tetrahedral mesh from closed surfaces ...

creating volumetric mesh from a surface mesh ...

volume mesh generation is complete

The number of region is displayed:

Number of region 5

region numerotation:

0

1

2

3

4

number of element per region:

209 # Only 209 cells? Region 0 is an artifact to be corrected.

270065

274890

3047933

2064185

Pay special attention to the first region (numerated 0 by Iso2mesh). For our example, we should have only 4 regions (cf. Fig. X-3b) and not 5. Iso2mesh by default assigns to the region 0 cells it did not resolve correctly (it is a bug say simply, or I have incorrectly used Iso2mesh!). Click on ‘inspect region’ to be sure of the issue. Follow instructions displayed in the GUI and click in ‘Correct region’. Incorrect cells will be assigned to adjacent regions, and result displayed in the MATLAB command window:

- Pass 1. Check incorrect region with region 4, number of incorrect cell 208

- Pass 1. Check incorrect region with region 4, number of incorrect cell 0

- Pass 1. Check incorrect region with region 4, number of incorrect cell 0

- Pass 1. Check incorrect region with region 3, number of incorrect cell 0

- Pass 1. Check incorrect region with region 2, number of incorrect cell 1

- Pass 1. Check incorrect region with region 2, number of incorrect cell 0

- Pass 1. Check incorrect region with region 2, number of incorrect cell 0

- Pass 1. Check incorrect region with region 1, number of incorrect cell 0

- Pass 2. Check incorrect region with region 4, number of incorrect cell 0

- Pass 2. Check incorrect region with region 4, number of incorrect cell 0

- Pass 2. Check incorrect region with region 3, number of incorrect cell 0

- Pass 2. Check incorrect region with region 2, number of incorrect cell 0

- Pass 2. Check incorrect region with region 1, number of incorrect cell 0

Number of region 4

region numerotation: # Now we have the expected 4 regions.

1

2

3

4

number of element per region:

270065

274891

3047933

2064393

After correction, you need to re-inspect region before moving one. Note that if you are working with small domains, there is usually no incorrect region at all. The problem only arises for intermediate to large domains.

|  |
| --- |
|  |
| *Figure X-5a. Create mesh tab* |
|  |
| *Figure X-5b. Figures generated with ‘Inspect region’. Numeration starts at 1. (Left) Region 1 is incorrect. (Right), region 5 (solid phase) is correct.* |
|  |
| *Figure X-5c. Region number 1 is incorrect. Enter the value and click ‘Correct regions’.* |

You then need to assign region number with cell materials to make sure mesh files will correspond to the expected regions.

|  |
| --- |
|  |
| *Figure X-5d. Assign regions to each phase. First select correct values within the popup menus, then click on ‘Validate assignment’ and repeat for each phase. Once done, click on the button ‘Assign solid and electrolyte’.* |
| *A close up of a piece of paper  Description automatically generated* |
| *Figure X-5e. Electrolyte mesh after assignment: ‘separator: electrolyte’ + ‘right electrode: electrolyte’.* |

Once done, you can save the meshes.

## Re-create the mesh in a dedicated FEM software

Mesh information is saved in the folder ‘Mesh\_data’. Of importance’s are the following files:

* Nodes\_\*.mat with \* being the domain (e.g. Right\_electrode for the solid phase of the right electrode). The file contains the variable ‘node\_region’ which is a n x 3 array, n being the number of nodes of the material and the three columns being the node coordinates.
* Tetrahedron\_\*.mat with \* being the domain. The file contains the variable ‘elem\_’ which is a m \* 4 array, m being the number of tetrahedron cell with the column being the cell connectivity. For instance, elem\_(7,:) = 189962 191889 189588 587522 indicates cell (tetrahedron) number 7 have four nodes, numerated 189962, 191889, 189588, and 587522. node\_region(189962,:) contains the coordinates of the first node.

You can re-create mesh for each phase with these two files. Note that facets and node at phase interface are doubled in this representation (with meshes being conformal at the interface). This is suitable for models that use a segregated approach (i.e. solving domain sequentially in a Picard-type self-converging numerical approach).

* Alternatively, node.mat and Tetrahedron.mat contain the whole cell information (no doublons) to mesh the whole cell. You will also need Subdomains.mat which is a m \* 1 array, with m being the total number of cell, that indicate the cell phase belonging, and facets.mat which is a k \* 1 array, with k being the total number of facets, that indicate the facets phase belonging. It uniquely marks the facets belonging to the interface between electrodes and electrolytes as well as the electrolytes/current collector boundary.

This second approach is suitable for models that use a monolithic approach (i.e. solving the whole cell in one step).

Verteces\_coordinate\_interface\_EL\_RightAM.mat and Verteces\_coordinate\_interface\_LeftAM\_EL.mat contains the coordinates of all nodes at the interface solid-electrolyte for the right electrode and the left electrode.

### Creating the mesh for a FEM model using FEniCS

FEniCS is an open-source (LGPLv3) computing platform for solving partial differential equations. The syntax is Python. The code below indicated how to create meshes for each phase, which is relevant for a segregated model, or for homogenization calculations.

First load the node and cell connectivity information generated with the mesh module:

from dolfin import \* # Dolfin library

from mshr import \* # Mesh library

import scipy.io as spio # Import MATLAB.mat array

import h5py # Import MATLAB.mat array

[…]

**def load\_mat(path,variable\_name):**

**try:**

res = spio.loadmat(path)[variable\_name]

**except NotImplementedError:**

# raise NotImplementedError('Please use HDF reader for matlab v7.3 files')

dict = {}

f = h5py.File(path,*'r')*

**for k, v in list(f.items()):**

dict[k] = np.array(v)

res = dict[variable\_name]

res = res.transpose()

**return res**

Node\_Electrolyte = load\_mat(Node\_Electrolyte\_path,*'node\_region')*

Node\_Left\_electrode = load\_mat(Node\_Left\_electrode\_path,*'node\_region')*

Node\_Right\_electrode = load\_mat(Node\_Right\_electrode\_path,*'node\_region')*

Tetrahedron\_Electrolyte = load\_mat(Tetrahedron\_Electrolyte\_path,*'elem\_')*

Tetrahedron\_Left\_electrode = load\_mat(Tetrahedron\_Left\_electrode\_path,*'elem\_')*

Tetrahedron\_Right\_electrode = load\_mat(Tetrahedron\_Right\_electrode\_path,*'elem\_')*

Then reconstruct the mesh, node per node, and cell per cell.

def create\_mesh(node\_,tetrahedroncell\_):

number\_vertices=len(node\_) # Number of vertices

number\_cells=len(tetrahedroncell\_) # Number of cells

mesh = Mesh() # Create an empty mesh object

editor = MeshEditor() # Select the editor

if version\_check[dolfin.\_\_version\_\_]==version\_check['2016.1.0']:

editor.open(mesh, 3, 3) # (mesh, topological dimension, geometrical dimension)

else:

editor.open(mesh, 'tetrahedron', 3, 3, 1) #

# (mesh, cell type, topological dimension, geometrical dim, polynomial degree)

editor.init\_vertices(number\_vertices) # Set number of vertices

editor.init\_cells(number\_cells) # Set number of cells

# Set vertex location (vertex id,x,y)

for vertex\_id in range(number\_vertices):

x\_ = node\_[vertex\_id][0] # Vertex coordinate 0

y\_ = node\_[vertex\_id][1] # Vertex coordinate 1

z\_ = node\_[vertex\_id][2] # Vertex coordinate 2

vertex\_id=int(vertex\_id) # The vertex id must be an integer

if version\_check[dolfin.\_\_version\_\_]>=version\_check['2018.1.0']:

editor.add\_vertex(vertex\_id, Point(x\_, y\_, z\_)) # Add the vertex

else:

editor.add\_vertex(vertex\_id, x\_, y\_, z\_) # Add the vertex

# Set cell (cell id, vertices id), for tetrahedrons

for cell\_id in range(number\_cells):

v0 = tetrahedroncell\_[cell\_id][0] # Vertex indice 0

v1 = tetrahedroncell\_[cell\_id][1] # Vertex indice 1

v2 = tetrahedroncell\_[cell\_id][2] # Vertex indice 2

v3 = tetrahedroncell\_[cell\_id][3] # Vertex indice 3

cell\_id=int(cell\_id); v0=int(v0); v1=int(v1); v2=int(v2); v3=int(v3)  
 # The ids must be integers

if version\_check[dolfin.\_\_version\_\_]>=version\_check['2018.1.0']:

editor.add\_cell(cell\_id, [v0, v1, v2, v3]) # Add the cell

else:

editor.add\_cell(cell\_id, v0, v1, v2, v3) # Add the cell

editor.close() # Close the editor

return mesh

# Create electrolyte mesh

mesh\_electrolyte\_separator = create\_mesh(Node\_Electrolyte,Tetrahedron\_Electrolyte)

# Create active material of the left electrode mesh

mesh\_left\_activematerial = create\_mesh(Node\_Left\_electrode,Tetrahedron\_Left\_electrode)

# Create active material of the right electrode mesh

mesh\_right\_activematerial = create\_mesh(Node\_Right\_electrode,Tetrahedron\_Right\_electrode)

The variables ‘mesh\_\*’ are FEniCS mesh objects.

## Example of mesh created with the module

Figures below show some lithium ion battery cell meshes generated with this module.

|  |
| --- |
|  |
| *Figure X-6a. Electrolyte mesh of a full cell NMC/separator/graphite 6-phases domain. Electrodes geometry from computed tomography, separator generated with the module.* |
|  |
| *Figure X-6b. Electrodes from computed tomography. Meshes have been generated with the ‘Laplacian’ option, resulting in a very smooth surface. Color is z-axis location.* |
|  |
| *Figure X-6c. A very tortuous graphite electrode meshed with the module.* |
|  |
| *Figure X-6d. Various test geometries meshed with the module.* |
|  |
| *Figure X-6e. Fast charge FEM electrochemical simulation performed on a mesh generated with this module. Electrolyte concentration is displayed.* |
|  |
| *Figure X-6f. Zoom on a FEM electrochemical simulation showing mesh details. Solid concentration is displayed.* |

## Common Iso2mesh error and workaround

Most common error with Iso2mesh is "Two subfaces ... are found intersecting each other". Workarounds are:

* Reduce domain’s size (through cropping or downscaling).
* Apply morphology opening (erosion + dilatation) to simply surface detail.
* Decrease the radbound value (e.g. 0.5 instead of default 1.0). Warning: this will result in a much more refined mesh, thus it is very CPU/RAM expensive).
* Using the lowpass smoothing method with a small number of iteration (e.g. 1) and a small useralpha value (e.g. 0.5).

# Useful Standalone Functions

Functions presented below can be used as standalone. For more details, please open them with the MATLAB editor.

* src\Miscellaneous\function\_save\_tif

Save a 2D or 3D array in a tif file (one unique tif file even for a 3D volume) that you can later load in MATLAB with function\_load\_tif.m or in a third-party software such as ImageJ.

function\_save\_tif(array3D, pathname)

* src\Miscellaneous\function\_load\_tif

Load a tif file in a 3D MATLAB array with a user-defined format (e.g., uint8, default uint16).

[array,outcome] = function\_load\_tif(path,datatype\_array)


Or

[array,outcome] = function\_load\_tif(path)

* src\Miscellaneous\Microstructure\_basic\_visualization\_interface.m

Use for simple 2D slice interactive visualization.

M=function\_load\_tif('C:\Users\fussegli\Desktop\Tifs\Example\nmc\_bridge.tif');  
Microstructure\_basic\_visualization\_interface(M)



* src\Microstructure\_comparison\_visualization\_interface.m

Based on Microstructure\_basic\_visualization\_interface code but expanded to visualize n files side by side for comparison sake. Arrays do not need to be of the same size (the slider is based on the largest dimension among the arrays).

A=function\_load\_tif('C:\Users\fussegli\Desktop\nmc-1-cal\_generatedCBD\_bridge.tif');

B=function\_load\_tif('C:\Users\fussegli\Desktop\nmc-1-cal\_generatedCBD\_Energy\_w0.001.tif');

C=function\_load\_tif('C:\Users\fussegli\Desktop\nmc-1-cal\_generatedCBD\_Energy\_w0.999.tif');

D=function\_load\_tif('C:\Users\fussegli\Desktop\graphite-5-cal-blackisporepluscbd.tif');

E=function\_load\_tif('C:\Users\fussegli\Desktop\Bi\_layer.tif');

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| S=size(\*) | A | B | C | D | E |
| S(1) | 301 | 301 | 301 | 248 | 240 |
| S(2) | 301 | 301 | 301 | 251 | 240 |
| S(3) | 251 | 251 | 251 | 961 | 240 |

Microstructure\_comparison\_visualization\_interface(A, B, C, D, E);



Number of row and columns is automatically determined, spacings between axes is parametrized within the function and can be easily modified.

* src\Miscellaneous\Function\_Writetable.m

Use to save multiple MATLAB table in a csv file.

clear DATA\_writetable

DATA\_writetable.sheet(1).name='Excel\_sheet1'; % Name of first excel sheet

DATA\_writetable.sheet(1).table=Table\_1;

% A MATLAB table (see <https://www.mathworks.com/help/matlab/ref/table.html>)

DATA\_writetable.sheet(2).name='Whatever\_name'; % Do not use empty space or too long name

DATA\_writetable.sheet(2).table=Another\_MATLAB\_table;

[…]% Add others sheets

Folder = ‘C:\Users\fussegli\Desktop\’;

filename = 'example';

Function\_Writetable(folder,filename,DATA\_writetable)

* src\Miscellaneous\ function\_remove\_emptyandspecialcharacter\_string.m

Use to remove or replace specific characters (e.g., ‘ ‘ ',' ‘-‘) you would not like to use for filename when saving.

[ str\_new ] = function\_remove\_emptyandspecialcharacter\_string(str\_old)

# Knows issues/Frequently Asked Questions

* Image is uniform after saving or while modifying it with the filtering/segmentation module:

Try changing the data type before saving/modifying the image. Recommended is uint8 or uint16. If problem persists, edit file src\Miscellaneous\function\_save\_tif.m.

* MATLAB does not respond or crash during microstructure characterization, with no error displayed.

You may have reached MATLAB's maximum name length of 63, which can occur if your main folder is already long. When this occurs, MATLAB, unfortunately, does not always show a warning and stalls indefinitely while trying to save a file. Try using a short name main folder (such as C:\Calc\).

* MATLAB fails to save table in an excel file:

Warning: File not found or permission denied

> In Function\_Writetable (line 40)

In Function\_Specificinterface\_direct (line 209)

In function\_microstructure\_characterization\_segmentedvolume (line 474)

In microstructure\_characterization\_GUI/pushbutton\_runallcalculations\_Callback (line 2947)

Error using Interface.000208DA\_0000\_0000\_C000\_000000000046/SaveAs

Invoke Error, Dispatch Exception:

Source: Microsoft Excel

Description: Cannot access ‘your\_file.xls'.

Help File: xlmain11.chm

Help Context ID: 0

Error in Function\_Writetable (line 44)

ExcelWorkbook.SaveAs(full\_path\_xls,1); % Save it

Open Task Manager and kill all EXCEL process. Manually delete your\_file.xls and retry.

* MATLAB fails to generate mesh (‘Click to create mesh’ button)

creating surface and tetrahedral mesh from a multi-domain volume ...

Error using fallbackexeext (line 37)

The following executable:

C:\Users\fussegli\Documents\GitHub\Microstructure\_analysis\_toolbox\src\Create\_mesh\_for\_FEM\iso2mesh-2018-linux64\iso2mesh\bin\cgalmesh.exe is missing. Please download it from https://github.com/fangq/iso2mesh/tree/master/bin/ and save it to the above path, then rerun the script.

Error in cgalv2m (line 50)

exesuff=fallbackexeext(exesuff,'cgalmesh');

Error in vol2mesh (line 54)

[node elem,face]=cgalv2m(vol,opt,maxvol);

Error in v2m (line 18)

[node,elem,face]=vol2mesh(img,1:size(img,1),1:size(img,2),1:size(img,3),opt,maxvol,1,method,isovalues);

Error in v2s (line 21)

[no,tet,el]=v2m(uint8(img),isovalues,opt,1000,method);

Error in mesh\_generation\_withIso2mesh (line 46)

[nodes\_coordinates,triangular\_faces,regions,holes]=v2s(tmp,isovalues\_,opt,method\_surfacemesh);

Error in microstructure\_meshing\_GUI/generatemesh\_Callback (line 2616)

[node,elem,face] = mesh\_generation\_withIso2mesh(cell\_array, options); % Create volumetric mesh

Error while evaluating UIControl Callback.

Your installation of Iso2mesh is incorrect. Download Iso2mesh (make sure you have the correct library for your OS) and add it to the MATLAB path.

# References

## Getting started with microstructure analysis

Algorithms presented in this toolbox have been utilized in16,32,41

You can find below a selection of references sorted by topics you can read to get into microstructure analysis:

* *Image segmentation*. Review of segmentation methods can be found in22,23.
* *Microstructure numerical generation*. Generation methods for active materials are described in14,15, and for additive phases in8,18
* *Representative Volume Element*. RVE size being parameter specific is discussed in 41,42.
* *Voxel size dependence analysis*. Example of voxel size dependence analysis can be found in 16,32,38. Fractal nature of some parameter is discussed in 32,40.
* *Particle size*. Impact of particle size on battery electrode performances is discussed in35–37.
* *Particle anisotropy/non-spherical shape.* Impact of particle shape on effective diffusion coefficient is discussed in 32,34.
* *Tortuosity factor*. Homogenization method is well explained in38. Impact of boundary conditions and edged effects are detailed in41. Finite difference method (used in this toolbox) is introduced in2. Comparison between finite element and finite difference calculations is discussed in16 (see supplementary materials). Experimental determination of tortuosity factor are detailed in48,49 Comparison between numerical and experimental determination of tortuosity factor is also discussed in16. Re-derivation of the Bruggeman analytical relationship along with a discussion on its limitations can be found in46
* *Sinuosity and constrictivity*. Geometric interpretation of tortuosity factor is discussed in length in32,44,58
* *Electrochemical macroscale modeling (use microstructure properties)*. Most macroscale electrochemical battery models use the pseudo-2D formulation originally proposed by Newman and coworkers30. A more recent writing of these equations can be found in K. Smith articles31,59.
* *Meshing*.
* *Electrochemical microstructure scale modeling (use microstructure mesh)*. Look at60.

## Documentation references

1. NREL’s Computer-Aided Engineering for Electric Drive Vehicle Batteries (CAEBAT). *NREL’s Computer-Aided Engineering for Electric Drive Vehicle Batteries (CAEBAT)* https://www.nrel.gov/transportation/caebat-microstructure-applications.html.

2. Cooper, S. J., Bertei, A., Shearing, P. R., Kilner, J. A. & Brandon, N. P. TauFactor: An open-source application for calculating tortuosity factors from tomographic data. *Softwarex* **5**, 203–210 (2016).

3. Fang, Q. & Boas, D. A. Tetrahedral mesh generation from volumetric binary and grayscale images. *2009 Ieee Int Symposium Biomed Imaging Nano Macro* 1142–1145 (2009) doi:10.1109/isbi.2009.5193259.

4. Crosby, K. Column Converter for Excel,  MATLAB Central File Exchange. *Column Converter for Excel,  MATLAB Central File Exchange* https://www.mathworks.com/matlabcentral/fileexchange/28343-column-converter-for-excel (2020).

5. Jan. DataHash, MATLAB Central File Exchange. *DataHash, MATLAB Central File Exchange* https://www.mathworks.com/matlabcentral/fileexchange/31272-datahash.

6. Tanaka, M. Noise Level Estimation from a Single Image, MATLAB Central File Exchange. *Noise Level Estimation from a Single Image, MATLAB Central File Exchange* https://www.mathworks.com/matlabcentral/fileexchange/36921-noise-level-estimation-from-a-single-image (2020).

7. Altman, Y. ScreenCapture - get a screen-capture of a figure frame or component. *ScreenCapture - get a screen-capture of a figure frame or component* https://www.mathworks.com/matlabcentral/fileexchange/24323-screencapture-get-a-screen-capture-of-a-figure-frame-or-component (2021).

8. Mistry, A., Smith, K. & Mukherjee, P. P. Secondary Phase Stochastics in Lithium-ion Battery Electrodes. *ACS Applied Materials & Interfaces* (2018) doi:10.1021/acsami.7b17771.

9. Conder, J., Marino, C., Novák, P. & Villevieille, C. Do imaging techniques add real value to the development of better post-Li-ion batteries? *Journal of Materials Chemistry A* **6**, 3304–3327 (2018).

10. Pietsch, P. & Wood, V. X-Ray Tomography for Lithium Ion Battery Research: A Practical Guide. *Annual Review of Materials Research* **47**, 1–29 (2016).

11. Eastwood, D. S. *et al.* The application of phase contrast X-ray techniques for imaging Li-ion battery electrodes. *Nuclear Instruments and Methods in Physics Research Section B: Beam Interactions with Materials and Atoms* **324**, 118–123 (2014).

12. Xu, C. S. *et al.* Enhanced FIB-SEM systems for large-volume 3D imaging. *Elife* **6**, e25916 (2017).

13. NREL battery Microstructures Library. *null* https://www.nrel.gov/transportation/microstructure.html (2020).

14. Moussaoui, H. *et al.* Stochastic geometrical modeling of solid oxide cells electrodes validated on 3D reconstructions. *Comp Mater Sci* **143**, 262–276 (2018).

15. Gayon-Lombardo, A., Mosser, L., Brandon, N. P. & Cooper, S. J. Pores for thought: generative adversarial networks for stochastic reconstruction of 3D multi-phase electrode microstructures with periodic boundaries. *Npj Comput Mater* **6**, 82 (2020).

16. Usseglio-Viretta, F. L. *et al.* Resolving the Discrepancy in Tortuosity Factor Estimation for Li-Ion Battery Electrodes through Micro-Macro Modeling and Experiment. *Journal of The Electrochemical Society* **165**, A3403–A3426 (2018).

17. Mistry, A. N., Smith, K. & Mukherjee, P. P. Electrochemistry Coupled Mesoscale Complexations in Electrodes Lead to Thermo-Electrochemical Extremes. *Acs Appl Mater Inter* **10**, 28644–28655 (2018).

18. Hein, S. *et al.* Influence of Conductive Additives and Binder on the Impedance of Lithium-Ion Battery Electrodes: Effect of Morphology. *J Electrochem Soc* **167**, 013546 (2020).

19. Mistry, A., Smith, K. & Mukherjee, P. P. Stochasticity at Scales Leads to Lithium Intercalation Cascade. *Acs Appl Mater Inter* **12**, 16359–16366 (2020).

20. Perona, P. & Malik, J. Scale-space and edge detection using anisotropic diffusion. *null* **12**, (1990).

21. Buades, A., Coll, B. & Morel, J.-M. A Non-Local Algorithm for Image Denoising. *null* doi:10.1109/cvpr.2005.38.

22. Khan, M. A Survey: Image Segmentation Techniques. *International Journal of Future Computer and Communication* 89–93 (2014) doi:10.7763/IJFCC.2014.V3.274.

23. Wirjadi, O. Survey of 3D Image Segmentation Methods. *Berichte des Fraunhofer ITWM Tech. Rep* (2007).

24. Julie, V. *et al.* 3D phase mapping of solid oxide fuel cell YSZ/Ni cermet at the nanoscale by holographic X-ray nanotomography. *null* **243**, (2013).

25. Otsu, N. A Threshold Selection Method from Gray-Level Histograms. *null* **9**, (1979).

26. Pizer, S. M. *et al.* Adaptive histogram equalization and its variations. *Computer Vision, Graphics, and Image Processing* **39**, 355–368 (1986).

27. Zuiderveld, K. *Contrast Limited Adaptive Histograph Equalization.* (1994).

28. Joos, J., Ender, M., Rotscholl, I., Menzler, N. H. & Ivers-Tiffée, E. Quantification of double-layer Ni/YSZ fuel cell anodes from focused ion beam tomography data. *Journal of Power Sources* **246**, 819–830 (2014).

29. Usseglio-Viretta, F. L. E. Optimization of the performances and the robustness of an electrolyser at high temperatures. *Grenoble Alpes University* (2015).

30. Doyle, M. Modeling of Galvanostatic Charge and Discharge of the Lithium/Polymer/Insertion Cell. *Journal of The Electrochemical Society* **140**, 1526 (1993).

31. Smith, K. & Wang, C.-Y. Power and thermal characterization of a lithium-ion battery pack for hybrid-electric vehicles. *Journal of Power Sources* **160**, (2006).

32. USSEGLIO-VIRETTA, F. L. E. *et al.* Quantitative relationships between pore tortuosity, pore topology, and solid particle morphology using a novel discrete particle size algorithm. *J Electrochem Soc* (2020) doi:10.1149/1945-7111/ab913b.

33. Singh, M., Kaiser, J. & Hahn, H. Thick Electrodes for High Energy Lithium Ion Batteries. *J Electrochem Soc* **162**, A1196–A1201 (2015).

34. Ebner, M., Chung, D., García, E. R. & Wood, V. Electrodes: Tortuosity Anisotropy in Lithium‐Ion Battery Electrodes (Adv. Energy Mater. 5/2014). *Advanced Energy Materials* **4**, (2014).

35. Röder, F., Sonntag, S., Schröder, D. & Krewer, U. Simulating the Impact of Particle Size Distribution on the Performance of Graphite Electrodes in Lithium‐Ion Batteries. *Energy Technol-ger* **4**, 1588–1597 (2016).

36. Meyer, M., Komsiyska, L., Lenz, B. & Agert, C. Study of the local SOC distribution in a lithium-ion battery by physical and electrochemical modeling and simulation. *Appl Math Model* **37**, 2016–2027 (2012).

37. Lee, K. & Kum, D. The Impact of Inhomogeneous Particle Size Distribution on Li-ion Cell Performance Under Galvanostatic and Transient Loads. *2016 Ieee Transp Electrification Conf Expo Asia-pacific Itec Asia-pacific* 454–459 (2016) doi:10.1109/itec-ap.2016.7512997.

38. Laurencin, J. *et al.* Characterisation of Solid Oxide Fuel Cell Ni–8YSZ substrate by synchrotron X-ray nano-tomography: from 3D reconstruction to microstructure quantification. *null* **198**, (2012).

39. Delette, G. *et al.* Thermo-elastic properties of SOFC/SOEC electrode materials determined from three-dimensional microstructural reconstructions. *International Journal of Hydrogen Energy* **38**, 12379–12391 (2013).

40. Bertei, A. *et al.* The fractal nature of the three-phase boundary: A heuristic approach to the degradation of nanostructured solid oxide fuel cell anodes. *Nano Energy* **38**, 526–536 (2017).

41. Usseglio-Viretta, F. & Smith, K. Quantitative Microstructure Characterization of a NMC Electrode. *ECS Transactions* **77**, 1095–1118 (2017).

42. Kanit, T., Forest, S., Galliet, I., Mounoury, V. & Jeulin, D. Determination of the size of the representative volume element for random composites: statistical and numerical approach. *null* **40**, (2003).

43. Tjaden, B., Brett, D. J. & Shearing, P. R. Tortuosity in electrochemical devices: a review of calculation approaches. *International Materials Reviews* 1–21 (2016) doi:10.1080/09506608.2016.1249995.

44. Holzer, L. *et al.* The influence of constrictivity on the effective transport properties of porous layers in electrolysis and fuel cells. *J Mater Sci* **48**, 2934–2952 (2013).

45. Bruggeman, D. Berechnung verschiedener physikalischer Konstanten von heterogenen Substanzen. I. Dielektrizitätskonstanten und Leitfähigkeiten der Mischkörper aus isotropen Substanzen. *Annalen der Physik* **416**, (1935).

46. Tjaden, B., Cooper, S. J., Brett, D. J., Kramer, D. & Shearing, P. R. On the origin and application of the Bruggeman correlation for analysing transport phenomena in electrochemical systems. *Current Opinion in Chemical Engineering* **12**, 44–51 (2016).

47. Archie, G. E. The Electrical Resistivity Log as an Aid in Determining Some Reservoir Characteristics . *Dallas Meeting* (1941).

48. Thorat, I. V. *et al.* Quantifying tortuosity in porous Li-ion battery materials. *Journal of Power Sources* **188**, 592–600 (2009).

49. Landesfeind, J., Hattendorff, J., Ehrl, A., Wall, W. A. & Gasteiger, H. A. Tortuosity Determination of Battery Electrodes and Separators by Impedance Spectroscopy. *J Electrochem Soc* **163**, A1373–A1387 (2016).

50. Usseglio-Viretta, F. *et al.* Quantitative microstructure characterization of a Ni–YSZ bi-layer coupled with simulated electrode polarisation. *Journal of Power Sources* **256**, 394–403 (2014).

51. Joos, J. *et al.* Detailed Microstructure Analysis and 3D Simulations of Porous Electrodes. *null* **35**, (2011).

52. Rajon, D. A., Patton, P. W., Shah, A. P., Watchman, C. J. & Bolch, W. E. Surface area overestimation within three‐dimensional digital images and its consequence for skeletal dosimetry. *null* **29**, (2002).

53. Weisstein, E. Oblate Spheroid. *MathWorld--A Wolfram Web Resource* https://mathworld.wolfram.com/OblateSpheroid.html.

54. Gelb, L. D. & Gubbins, K. Pore Size Distributions in Porous Glasses:  A Computer Simulation Study. *Langmuir* **15**, 305–308 (1999).

55. Münch, B. & Holzer, L. Contradicting Geometrical Concepts in Pore Size Analysis Attained with Electron Microscopy and Mercury Intrusion. *null* **91**, (2008).

56. Beucher, S. & Lantuejoul, C. Use of Watersheds in Contour Detection. *International Workshop on Image Processing: Real-time Edge and Motion Detection/Estimation, Rennes, France* (1979).

57. KENDALL, M. G. A NEW MEASURE OF RANK CORRELATION. *Biometrika* **30**, 81–93 (1938).

58. Holzer, L. *et al.* Redox cycling of Ni–YSZ anodes for solid oxide fuel cells: Influence of tortuosity, constriction and percolation factors on the effective transport properties. *Journal of Power Sources* **242**, 179–194 (2013).

59. Smith, K. A., Rahn, C. D. & Wang, C.-Y. Control oriented 1D electrochemical model of lithium ion battery. *Energy Conversion and Management* **48**, 2565–2578 (2007).

60. Allen, J. M., Chang, J., Usseglio-Viretta, F. L. E., Graf, P. & Smith, K. A Segregated Approach for Modeling the Electrochemistry in the 3-D Microstructure of Li-Ion Batteries and Its Acceleration Using Block Preconditioners. *J Sci Comput* **86**, 42 (2021).